## Slide 1: Pushing Nb performance
Alexander Romanenko
SRF’2015 Tutorials
12 Sep 2015

## Slide 2
Part I: brief overview of past limitations + progress in fundamental understanding of previously encountered phenomena
Part II: new discoveries

## Slide 3
PART I: Brief overview of past limitations + progress in fundamental understanding

## Slide 4: Detailed look at Q(E) curve portions – Q slopes
quench

## Slide 5: Q(E) curve and goals of SRF research
Increase Q => decrease required power
Increase max Eacc => decrease accelerator length
Typical ILC-prepared cavity at T=2K
Q=const/Rs
Average surface resistance
Surface magnetic
field B
Bpeak~160 mT
Where does Q go at very low fields?

## Slide 6
Limits to the achievable gradient

## Slide 7: Niobium surface structure
Advancements driven by scientific understanding

## Slide 8: High gradient – possible limitations
Multipacting
  Multiple impact electron amplification
Field emission
  Emission and acceleration of electrons by the surface electric fields
Quench
  Localized loss of superconductivity followed by a quickly spreading normal zone consuming all of the available RF power within < 1ms
  Currently still the ultimate limit to gradients

## Slide 9: Multipacting
Understood since ~1980s
  Essentially non-issue in elliptical cavities
  Typical long processing times (hours to days) to achieve the required gradient in lower beta cavities of more complicated shapes (quarterwave, spoke, half-wave resonators)
    Still usually can be processed

## Slide 11: Field emission
Field emission

## Slide 12: Museum of Known Field Emitters 0.5 to 10 microns Note the sharp features on the Particles.
(a) Sub-micron field emitting particles found on sample prepared with 9-cell cavity
(b) Al particle found at a field emission site in the dc field emission scanning apparatus and subsequently analyzed with the SEM
(c) Field emitting particle found with thermometry followed by dissection of a 1.5 GHz cavity. Carbon, oxygen, iron, chromium, and nickel were among the foreign elements detected

## Slide 13: Solution to field emission – high pressure water rinsing (100 atm), and an ultra-clean assembly => remove field emitters and preserve cleanliness

## Slide 14: Quench
Currently the hard limit on achievable cavity gradient
Initial “spark” can be thermal (heating above Tc) or magnetic (local critical field exceeded)
  In any case normal spreading zone emerges
Frequently driven by some sort of defect
  High gradient ones remain to be identified/found
  Accompanied by “pre-heating”
    Frequently not the case of N doped => different nature of quench

## Slide 15: Thermal breakdown
Overheating of the defect area above Tc
Solution -> Raise thermal conductivity -> use high purity niobium

## Slide 16: Quench – some new aspects
Decreased quench levels in N doped cavities are not associated with pre-heating
  Interesting fundamental problem to understand
Currently -> PPMS etc suggest decreased field of first penetration for heavier doping

## Slide 17: Superheating Field – ultimate limit as perceived now
Flux free Meissner state is stable up to Hc1
Favorable for flux to be deep in bulk above Hc1
BUT surface energy barrier allows metastable state Ultimate SRF limit: superheating field Hsh
Vortex state
Meissner state (metastable)
Meissner state
(Note: Magnetization curve for H increasing only)
Notes: Flux free Meissner state is stable up to Hc1
Favorable for flux to be deep in bulk above Hc1
BUT surface energy barrier allows metastable state! Ultimate limit: “superheating” field Hsh

## Slide 18: Cavity performance limitations – progress in understanding
#2: origin of the “high field Q slope”
#3: mechanism of the “120C baking”
#4: N doping to increase Q by a factor of >2
120C bake
Electropolished cavity
#1: microscopic mechanism of “Q-disease”
Too much H absorbed
f =1.3 GHz, T = 2K

## Slide 19: BUT FIRST
  Rs(T) = RBCS(T) + Rresidual
Fundamental part described by Bardeen-Cooper-Schrieffer (BCS) theory
Residual resistance due to other contributions
Surface resistance
Q ~ 1/Rs

## Slide 20: BCS resistance
Bauer- Review of surface resistance models –TD note

## Slide 21
Experimental decomposition of Rbcs(H) and Rres(H)

## Slide 22: Motivation
Cavity Q0 is a function of both temperature (T) and surface magnetic field H
  Q slopes
Temperature dependence of Rbcs for all treatments is well-understood -> thermally excited quasiparticles give Rbcs ~ 1/T*exp(-D/kT) at all RF fields (gap etc may change though)
Q = G/<Rs>, where <Rs> = Rbcs(T) + Rres
Crucial question – how does Rs(B) emerge from its components Rbcs(B) and Rres (B)?

## Slide 23: How to decompose the BCS and residual at all fields?
Obtain as many Q(B,T) measurements as practical at ALL fields (not only at a single low field)
At each fixed field fit corresponding Q(T) to extract Rres
  Also gives Rbcs(T) = Rs(T)-Rres
Or simply measure the lowest T Q(E) curve and take it as residual -> frequently an excellent approximation
Bath temperature
A. Romanenko and A. Grassellino
Appl. Phys. Lett. 102, 252603 (2013)

## Slide 24: Plethora of insight – standard treatments
High field Q slope is due to Rres
Medium field Q slope is a combination of both Rres and Rbcs
Low field Q slope is due to Rres
Rbcs decreases but becomes strongly field dependent after 120C
A. Romanenko and A. Grassellino, Appl. Phys. Lett. 102, 252603 (2013)

## Slide 25: Is RF surface temperature increase significant?
It was suggested that a “thermal feedback” may cause a slope in the Q0(E) curve since Rbcs(T)~1/T*exp(-const/T) – strongly T-dependent
  Trf increasing at higher fields=> Rbcs(Trf) increases => slope
Only thermal simulations based on Rs(H) from RF measurements were reported in the literature
  Kapitza resistance has a big uncertainty
Cavity wall
Trf
Helium bath @ Tbath
B
Heat flux= ½ Rs*H2
Trf > Tout > Tbath
Tout
Tout we can measure by T-mapping independently => only thermal conductivity needed to find Trf

## Slide 26
Heating is negligible, Rbcs increase with field is a genuine effect
Thermal feedback does not explain the medium field Q slope
From combined T-map/RF measurements

## Slide 27: NOW RECALL: Only surface ~40-100 nm matter
Niobium
3mm
Liquid Helium at T=2K
Vacuum with RF fields
Ba=B0eiwt
~10 cm cavity length
Nb2O5
Bin
3-5 nm
l(0)~40 nm
Inner surface nanostructure within ~ 40-100 nm completely determines RF losses in the cavity
Ba=B0eiwt
L

## Slide 28: Progress in fundamental understanding utilizing advanced techniques
Microscopic details of Q-disease
Cause of the “high field Q slope”
Mechanism of 120C baking

## Slide 29: Topic #1: microscopic details of Q disease
#1: microscopic mechanism of “Q-disease”
Q-disease was proposed in the past to be caused by excess hydrogen, which forms non-superconducting niobium hydrides upon cooldown
  Remedy found – 600-800C vacuum anneal to degas hydrogen
  Microscopic details never established
Q disease
Nb-H phase diagram
Cavity cooling

## Slide 30: Microscopic mechanism of Q-disease
Possible to observe directly hydride formation in H-reach niobium samples using the cryostage in the laser confocal scanning microscope
F. Barkov et al, Phys. Rev. ST Accel. Beams 15, 122001 (2012)
F. Barkov et al, J. Appl. Phys. 114, 164904 (2013)

## Slide 31
T=210K
Large phase starts to dissolve
T=260K
Hydrides gone, dislocation skeleton (deformation) remains on the surface
T=160K
T=100K
Hydrides first appear
T=300K
T=140K
Second (smaller) phase of hydride forms
T=6K
T=180K
50 um
First cooldown

## Slide 32
160K
140K
100K
6K
300K
Hydrides form much easier and at a higher temperature at both the “skeleton” left behind in the first cryocycle and at the locations of the second phase => cannot avoid Q-disease at 2nd cooldown
More “skeleton”
Second phase now growing larger
190K
180K
300K
Hydrides (both phases) now appear at higher T
Second cooldown

## Slide 33: Small phase does NOT form in 120C baked niobium
F. Barkov et al, J. Appl. Phys. 114, 164904 (2013)
Suggested possible involvement of H in the high field Q slope as well

## Slide 34: Progress in fundamental understanding
Microscopic details of Q-disease
Cause of the “high field Q slope”
Mechanism of 120C baking

## Slide 35: Topic #2: origin of the “high field Q slope”
#2: origin of the “high field Q slope”
Electropolished cavity
#1: microscopic mechanism of “Q-disease”
Too much H absorbed
Hypothesis: can it be the Q-disease “in miniature” – same mechanism, but nanohydrides instead of micron-size ones?
Need free H near surface and enough time to precipitate during cooldown

## Slide 36: Near-surface H present even after 600-800C degasing
Almost impossible to remove all near-surface hydrogen
Q-disease is eliminated by the 600-800C H degassing (bulk H content drastically reduced), but the near-surface H-rich layer remains
A. Romanenko and L. V. Goncharova, 2011 Supercond. Sci. Tech. 24, 105017

## Slide 37: There is enough time for diffusion-controlled precipitation
Integrate the H diffusion over the time spent in the precipitation temperature range T < 160K => Diffusion length > 1 um
All free near-surface H has enough time to precipitate into normal conducting hydrides upon cooldown

## Slide 38: Nanohydrides form upon cooldown
Not 120C baked sample
“fast” cooldown
T= 300K
Interstitial hydrogen
~50 nm
Oxide
T= 2K
Niobium hydrides
(non-superconducting)
Oxide

## Slide 39: Proximity effect model of the “high field Q slope”
FH
Cumulative distribution function of proximity-controlled breakdown fields of hydrides
Shape is determined by the distribution of hydride critical fields Hb
Rs~ R0 + Rn * FH(Ha)
Normal conducting hydrides of size d become superconducting by proximity effect up to the field Hb ~ 1/d
Q disease
High field Q slope
Excellent fits
H
A. Romanenko, F. Barkov, L. D. Cooley, A. Grassellino, Supercond. Sci. Technol. 26 (2013) 035003

## Slide 40: Temperature mapping
Array of 576 thermometers attached to the outside cavity walls allows mapping wall dissipation

## Slide 41: Investigating cutouts
Extract samples from cavity walls locations identified by temperature mapping -> direct correlation of RF losses with material structure

## Slide 42: TEM search for nanohydrides on cutouts
Look at this area with subnanometer resolution in TEM at room AND T<100K temperatures
TEM
Y. Trenikhina et al, J. Appl. Phys. 117, 154507 (2015)
Identify samples based on T-map

## Slide 43
Bulk of Nb
Lift out from the bulk
Sample on a Cu grid
TEM sample preparation with focused ion beam IB – powerful method to fully analyze cross-section
~10 μm
~3 μm
Pt protective layer
Cu grid
SEM images during the FIB sample preparation

## Slide 44
HRTEM imaging
Cold (baked)
Hot (not baked)
HRTEM: complicated defect structure in both cutouts
Pt layer
Pt layer

## Slide 45
Room T phase in Hot and Cold spot
[113]
[011]
[-111]
Hot (not baked) and Cold (baked) spot at room T
SAD, NED, SEND: only Nb at room T
H in solid solution (α-phase)
[100]
Nb a=3.33Å
@room T

## Slide 46
β
ε
ε+β
β
ε
ε
β
β
ε
ε
ε+β
ε+β
ε
ε
ε
ε
ε
ε
ε
ε
ε
ε
ε
ε+β
ε+β
ε
ε+β
β
_
_
_
_
Hot (not baked) spot at 94K
120°C baked stop at 94K
Nb+ε(Nb4H3)
Nb+β(NbH)
Nb +ε,β
Nb hydrides precipitation
Cryogenic T comparison of cavity cutouts
Nb
NO Nb hydrides precipitation
Nb
SEND: diffraction mapping with low intensity beam

## Slide 47
NED: Nb hydrides precipitation in all cutouts,
amount and/or size of NbHx is different
44%-68% probed
spots
~84-130 out
of 192 spots
26%-29%
probed spots
~49-55 out
of 192 spots
Hot (not baked) at 94K
Cryogenic T investigations of cavity cutouts
NED: diffraction with brighter beam, better S/N
120°C baked stop at 94K

## Slide 48
Pt protective layer
Nb bulk
Nb oxide
[001]
~10 μm
~3 μm
Cu grid
SEM of FIB sample
FIB sample and TEM image
TEM of FIB sample
200 nm
Pt protective layer

## Slide 49
grain 1
grain 2
In addition: grain boundaries comparison
SEM image of GB
HRTEM image of GB: Hot
Nb2O5

## Slide 50
HRTEM: No visible Nb2O5 oxide layer along GB
Cold
Hot
Grain boundaries comparison
Nb2O5

## Slide 51: TEM evidence for nanohydrides
Direct nano-area electron diffraction (NED) phase characterization of the surface of the SRF cavity cutouts before and after in situ mild vacuum bake at room temperature and at 94K
Room T: BCC Nb patterns, NO additional phases
[-111]
[-112]
94K: stoichiometric Nb hydride phases!
Nb oxides
Nb bulk
NED probe
40 nm
TEM diffraction on cavity cutouts confirms the existence of nanohydrides
Supports the proximity effect model
Measurements performed at Univ. of Illinois Urbana-Champaign
Y. Trenikhina et al, J. Appl. Phys. 117, 154507 (2015)

## Slide 52: Progress in fundamental understanding
Microscopic details of Q-disease
Cause of the “high field Q slope”
Mechanism of 120C baking

## Slide 53: Topic #3: mechanism of the 120C baking
#2: origin of the “high field Q slope”
#3: mechanism of the “120C baking”
120C bake
Electropolished cavity
#1: microscopic mechanism of “Q-disease”
Too much H absorbed

## Slide 54: Muon spin rotation at PSI (Switzerland)
Bµ
Contains physics
aG(t) ~ Muon Spin Polarization
Frequency – field amplitude
Damping – field non-uniformity

## Slide 55: Muon spin rotation – measure B(z) directly
B(z)
z
0
Superconductor in the Meissner State
Bext
l

## Slide 56: 120C bake leads to strong Meissner screening changes
Heat treatment at 120C leads to the strong increase in the penetration depth
  Consistent with the depth-dependent mean free path decrease
Is also the first ever confirmation of non-locality in bulk niobium
  Textbook example
A. Romanenko, A. Grassellino, F. Barkov, A. Suter, Z. Salman, T. Prokscha,
Appl. Phys. Lett. 104, 072601 (2014)
Baked at 120C
Unbaked

## Slide 57: Positron annihilation Doppler broadening spectroscopy
S parameter corresponds to positron annihilation with valence electrons, W-> core electrons
S is sensitive to open-volume defects, W-to chemical surrounding at the annihilation site
Increase in S parameter indicates presence of vacancy defects

## Slide 58: Positron annihilation studies on cavity cutouts
A. Romanenko, C. J. Edwardson, P. G. Coleman, P. J. Simpson, Appl. Phys. Lett. 102, 232601 (2013)
BCP
EP
Large grain
Fine grain
Positron annihilation spectroscopy: 120C baking results in “doping” of the first ~50 nm from the surface with vacancies
  So-called superabundant vacancy formation mechanism manifested in niobium [Y. Fukai and N. Okuma, Phys. Rev. Lett. 73, 1640 (1994)]
Collaboration with Bath University (UK) and Western University (Canada)

## Slide 59: Effect of 120C baking
T= 300K
Free interstitial hydrogen
~50 nm
Oxide
120C baking
T= 300K
Hydrogen is trapped by vacancies
Oxide

## Slide 60: Effect of 120C baking
“fast” cooldown
Cooling down of 120C baked niobium
T= 2K
No/smaller hydrides are formed due to significant portion of hydrogen trapped
Oxide
T= 300K
Oxide

## Slide 61: TEM -> further evidence for 120C baking effect
Room T: BCC Nb patterns, NO additional phases
Hot spot: 44-68% of probed spots
[-111]
[-112]
Baked spot: 26-29% of probed spots
[001]
[011]
94K: stoichiometric Nb hydride phases
Nb oxides
Nb bulk
NED probe
40 nm
120C baking leads to the decrease in size/density of the nanohydrides
Measurements performed at Univ. of Illinois Urbana-Champaign

## Slide 62
PART II: New Discoveries

## Slide 63
Nitrogen doping

## Slide 64: Nitrogen doping: a breakthrough in Q
Standard state-of-the art preparation
This was the highest Q possible up to 2012
Record after nitrogen doping – up to 4 times higher Q!
A. Grassellino et al, 2013 Supercond. Sci. Technol. 26 102001 (Rapid Communication) – highlights of 2013
1.3 GHz

## Slide 65: Nitrogen doping
Injection of small nitrogen partial pressure at the end of 800C degassing-> drastic increase in Q
T=2K
A. Grassellino et al, 2013 Supercond. Sci. Technol. 26 102001 (Rapid Communication) – selected for highlights of 2013

## Slide 66: N Doping – small deviation from standard ILC treatment
Example from FNAL 2/6 doping process:
Bulk EP
800 C anneal for 2 hours in vacuum
2 minutes @ 800C nitrogen diffusion
800 C for 6 minutes in vacuum
Vacuum cooling
5 microns EP
Cavity after Equator Welding
EP 140 um
Ethanol Rinse
External 20 um BCP
Short HPR
800C HT Bake
RF Tuning
EP 40 um
Ethanol Rinse
Long HPR
Final Assembly
Long HPR
Helium Tank Welding Procedure
VT Assembly
HPR
HOM Tuning
Ship to DESY
Leak Check
120C bake
XFEL
X
A. Grassellino et al, 2013 Supercond. Sci. Technol. 26 102001 (Rapid Communication)

## Slide 67: Material level understanding

## Slide 68: “Production” recipe for LCLS-II – 9-cells for prototype cryomodule(s)
A. Grassellino et al, IPAC’15

## Slide 69: Statistics for two doping recipes on 1.3 GHz 9-cells
Data from Cornell/Jlab/FNAL
16 MV/m
2.7e10
Recipe 2/6
Recipe 20/30
<Q>=3.24e10
<Emax>=16.3 MV/m
Emaxmedian=16.5MV/m
Data from FNAL/JLab
<Q>=3.6e10
<Emax>=22.2 MV/m
Emaxmedian=22.8MV/m

## Slide 70: “Reversed” field dependence of RBCS
Rs(T) = RBCS(T)+Rres
A. Grassellino et al, 2013 Supercond. Sci. Technol. 26 102001 (Rapid Communication)
Origin of the anti-Q-slope

## Slide 71: What is BCS missing?
B.P. Xiao, C. Reece, M. J. Kelley from JLab and College of William and Mary
  Momentum of Cooper pairs leads to an inversed field dependence of RBCS?
  [B.P. Xiao et al, Physica C 490 (2013) 26-31]
A. Gurevich from ODU
  Time-dependent density of states leads to the effect?
  [A. Gurevich, Phys. Rev. Lett. 113, 087001 (2014)]

## Slide 72: Muon spin rotation – nitrogen doping
Ba = 25 mT
Use variable energy muons, which stop in the first ~100nm
BCP and EP unbaked -> strong screening, excellent fit provided by the clean limit Pippard/BCS model
EP+120C bake-> strongly suppressed m.f.p., gradient of the m.f.p. from the surface, dirty limit
N-doped -> intermediate m.f.p., no gradient
mfp ~ 2 nm at the surface, increasing deeper
~15 nm - no screening
mfp~40 nm
mfp > 400 nm

## Slide 73: Non-equilibrium superconductivity – another possible mechanism?
Quasiparticle distribution deviates from thermal equilibrium and changes the “BCS” surface resistance
  Photon absorption (surface resistance source) is the cause of deviation
P. J. de Visser et al, Phys. Rev. Lett. 112, 047004 (2014)
Effect in Al:

## Slide 74: Doping of 650 MHz -> Q=7e10 at 2K, 17 MV/m
Applying N doping to 650 MHz cavities leads to much higher Qs than with EP+120C
Should be further improved if 1.3 GHz results are directly scaled -> Q~1e11 at 2K
1-cell
Doping for other frequencies -> a lot to be explored

## Slide 75
Meissner expulsion strongly affected by cooling

## Slide 76: Proposed role of thermal currents in thermal cycling effect on Q
J.-M. Vogt, O. Kugeler, and J. Knobloch, Phys. Rev. ST Accel. Beams 16, 102002 (2013)
Thermal currents were proposed to play a major role in change of the residual resistance of a dressed BCP cavity due to thermal cycling
  Original recommendation – cool down slow and uniform through Tc to minimize the effect

## Slide 77: FNAL discovery – Meissner expulsion
A. Romanenko, A. Grassellino, O. Melnychuk, D. A. Sergatskov, J. Appl. Phys. 115, 184903 (2014)
By only varying the “speed” of cavity cooling through Tc=9.25K the residual surface resistance can be systematically and reversibly varied
Single grain EP
Fine grain EP
N doped

## Slide 78: Meissner effect
Normal
Superconducting

## Slide 79: Magnetic probes – key diagnostics
H=5mG
Field enhancement
due to Meissner effect – ambient flux expulsion
Fluxgate
magnetometers
mG
Fluxgate magnetometers and thermometers on cavities during fast/slow cooldowns allowed us to discover the subtle underlying effect

## Slide 80: Typical same magnetic probe reading for fast/slow cooling
Efficient flux expulsion
Poor flux expulsion

## Slide 81: FNAL: Minimizing residual resistance (maximize Q) by avoiding the ambient magnetic flux to be trapped
Flux expelled efficiently
Flux mostly trapped
Same cavity, just cooled differently through 9.2K
2K, 1.3 GHz

## Slide 82: Differences between fast/slow
#1: Difference in geometry of transition

## Slide 83: Driving parameter of expulsion
Temperature difference at the phase front (dT/dx)
A. Romanenko, A. Grassellino, A. C. Crawford, D. A. Sergatskov, and O. Melnychuk, Appl. Phys. Lett. 105, 234103 (2014)

## Slide 84: Observing fast and slow cooldown dynamics

## Slide 85: Fast and slow cooldown dynamics captured
Fast from 300K
Slow from 12K
M. Martinello, M. Checchin - PhD work
Top
Bottom

## Slide 86
Fast cooldown

## Slide 95
Slow cooldown – encircling normal areas

## Slide 128: Utilizing new physics for record high Qs
Combination of nitrogen doping and efficient flux expulsion =>
Record high Q >1e11 up to 28 MV/m in SRF cavities
A. Romanenko, A. Grassellino, A. C. Crawford, D. A. Sergatskov, and O. Melnychuk, Appl. Phys. Lett. 105, 234103 (2014)
Ambient magnetic fields are fully expelled
1.5K, 1.3GHz 1-cell

## Slide 129
One more limit to push..!

## Slide 130: FINAL: Non-accelerator applications: SRF for qubits
Single photons vs MV/m
  Ultralow field and temperature limit
    We did not explore it in SRF before
Where does the “low field Q slope” end?
What is the Q at single-photon field levels?

## Slide 131: Final remarks
Exciting times – a lot to study/discover
I hope you will now be better prepared for the fundamental R&D talks and hot topics

## Slide 132: Acknowledgments
All previous tutorial speakers
FNAL SRF science team