## Slide 1: Production of 67Cu at the TR-Flex Cyclotron
Santiago Brühlmann1,2, Martin Walther1, Martin Kreller1, Hans-Jürgen Pietzsch1, Torsten Knieß1, Klaus Kopka1,2
1 Helmholtz-Zentrum Dresden-Rossendorf, Institute of Radiopharmaceutical Cancer Research,
Bautzner Landstraße 400, 01328 Dresden, Germany
2 Faculty of Chemistry and Food Chemistry, School of Science, Technical University Dresden,
01062 Dresden, Germany
August 22nd, 2022
Helmholtz-Zentrum Dresden-Rossendorf · Radiopharmaceutical Cancer Research · www.hzdr.de

## Slide 2: Motivation and Introduction
Production of 67Cu at the TR-Flex Cyclotron

## Slide 3: Introduction
Radiological properties1:
    β--emitter: mean energy 141 keV
    γ-emitter: 184.6 keV (48.7%), 93.31 keV (16.1%), i.a.
    Half-Life: 61.83 h
  Matched Pair of the β+-emitter 64Cu
  Production routes:
    Cyclotron-based
    Nuclear reactor based
    Photo nuclear reaction
  (Pre)clinical studies in the GBq-range 67Cu2
  Currently commercially 67Cu available from IOTRON (research grade)3
Copper-67 as a Theranostic Radionuclide
IAEA Nuclear Data Services, https://www-nds.iaea.org/, last accessed on 04.07.2022.
The production, separation, and use of 67Cu for radioimmunotherapy: a review. N. A. Smith, D. L. Bowers, and D. A. Ehst. Applied Radiation and Isotopes 70.10 (2012): 2377-2383.
IOTRON Medial Inc. https://www.copper67.com/, last accessed on 04.07.2022.

## Slide 4: Motivation
Copper-67 production
Advantages of the 70Zn(p,α)67Cu Reaction:
Suitable for small Cyclotrons
No co-production of other Copper RN
Small quantities of byproducts
Some technical aspect should be taken into account…

## Slide 5: Workflow
Two target alternatives: electrodeposited 70Zn and [70Zn]ZnO
Irradiation conditions based on tests and simulations
Radiochemical separation based on solid phase extraction
Expensive target material forces the implementation of a recycling strategy
Closed Loop Strategy
Target Construction
Target Irradiation
Radio-chemical Separation
Target Recycling
Product QA
Target Design

## Slide 6: Results
Production of 67Cu at the TR-Flex Cyclotron

## Slide 7: Results
    Electrodepositing on Gold subtract (disc)
    Electrodepositing bath:
      Zn2+ concentration around 15 g/dm3
      NH4SO4 as electrolyte
      Starting pH around 2
    Magnetic stirrer
    Electrochemical yield: 50-65%
    Surface density: around 1.13-1.46 g/cm2
Zinc Electrodepositing
Electrodeposited 70Zn target from previous baths.
Electrodeposited 70Zn target with the new technique.

## Slide 8: Results
Irradiations carried out at the Cyclotron TR-FLEX with the 30°configuration.
    Irradiation parameters based on simulations:
    Activation simulations to estimate proton beam energy
    Irradiation simulations to estimate the maximal beam current
      Based on the COMSOL Software1
      Parametric study of materials and currents
Target Irradiation I
Possibility of production of 67Cu at a small-sized Cyclotron via the (p,α)-reaction on enriched 70Zn. S. Kastleiner, H.H. Coenen and S.M. Qaim, Radiochim. Acta 84 (1999), 107-110
Target irradiation configuration at the TR-FLEX Cyclotron: 90° and 30°.
COMSOL Multiphysics, https://www.comsol.com/, last accessed on 04.07.2022.

## Slide 9: Results
Thermal contact (TC) between disc and electrodeposited target
Proton beam profile: broad or concentrated
Target Irradiation II: Metal Target
Axial (parallel to the beam) temperature profile of a electrodeposited 70Zn Target. Proton beam current: 60 µA.
Lateral (normal to the beam) temperature profile of a electrodeposited 70Zn Target. Proton beam current: 60 µA.
Electrodeposited 70Zn target (E07) after irradiation
with 45 µA for 4 h. Beam profile not optimized.
Electrodeposited 70Zn target (E10) after irradiation
with 60 µA for 4 h. Optimized beam profile.

## Slide 10: Results
Different backing disc and foil materials
Different [70Zn]ZnO masses
Target Irradiation III: Oxide Target
Melted Aluminum foil (T03), irradiated with 70 µA.
Irradiated [70Zn]ZnO target with Niobium foil. Current: 40 µA.
Axial (parallel to the beam) temperature profile of [70Zn]ZnO targets with different backing and foil materials and ZnO masses.
Lateral (normal to the beam) temperature profile of [70Zn]ZnO targets with different backing and foil materials and ZnO masses.

## Slide 11: Results
Radiochemical Separation
    Separation carried out with Copper-selective resin
      Target dissolution – 6M HCl
      Gallium retention in TK-400 resin
      Neutralization – 12M NaOH / 1M NaOAc
      Column load and rinse – 0.01M HCl
      Copper elution – 6M HCl
        1 ml volume
        90-95% 67Cu Activity
        67Ga impurities below quantification
Gamma-spectrometry of the [67Cu]CuCl2 fraction with a Canberra HPGe detector.

## Slide 12: Results
    Further purification of Zn material
    Precipitation of Zn(OH)2:
      Addition of 6M NaOH until pH 9
      Centrifugation, separation of the supernatant and further washing
      Drying of the precipitate
      Annealing
    Recovery efficiency 95%
    NaCl content estimated below 0.5% in weight
Target recycling
Precipitated and centrifugated [70Zn]Zn(OH)2.
Drying of the [70Zn]Zn(OH)2.
[70Zn]ZnO recovered after annealing.

## Slide 13: Results
Yields – First Irradiation Set
Target ID | Target Mass [mg] | Energy [MeV] | Current [µA] | Irr. Time [h] | A 67Cu [MBq] | A 67Ga [MBq] | Yield 67Cu [MBq/µA h]
Metal 70Zn Target |  |  |  |  |  |  | 
E00 | 109 | 17.5 | 50 | 4 | 30.3 | 65.4 | 0.151
E02 | 134 | 17.5 | 50 | 4 | 286 | 325 | 1.43
E04 | 129 | 17.5 | 60 | 3.33 | 170 | 135 | 0.841
E06a | 134 | 17.5 | 50 | 4 | ~73.3 | - | -
E05 | 167 | 17.5 | 40 | 4 | 111 | 99.1 | 0.700
E07 | 141 | 17.5 | 45 | 4 | 158 | 140 | 0.872
[70Zn]ZnO Target – 9 mm circle area |  |  |  |  |  |  | 
T01 | 10 | 17.5 | 30 | 120 | 5.24 | 2.06 | 0.087
T02 | 10 | 17.5 | 90 | 30 | 3.87 | 1.54 | 0.086
T03a | 50 | 18 | 70 | 15 | 6.40 | 2.19 | 0.365
T04 | 40 | 17.2 | 30-60 | 195 | 41.1 | 10.37 | 0.305
a. Target partially melted.

## Slide 14: Results
Optimized beam profile
ESA quantified by titration with 1,4,8,11-tetraazacyclotetradecane-N,N’,N’’,N’’’-tetraacetic acid (TETA)
Yields and Effective Specific Activities (ESA) – Second Irradiation Set
Target Number | Target Mass [mg] | Energy [MeV] | Current [µA] | Irr. Time [h] | Activity [MBq] | Yield [MBq/µA h] | Specific Activity [GBq/µmol]
Metal 70Zn Target |  |  |  |  |  |  | 
E08 | 159 | 17 | 45-60 | 6 | 328 | 1.06 | 10
E09b,c | 156 | 17 | 60 | 5 | 122 | 0.41 | 5.6
E10c | 154 | 17 | 60 | 4 | 200 | 0.83 | 3.8
[70Zn]ZnO Target |  |  |  |  |  |  | 
T05 | 100 | 17.2 | 40-60 | 5.75 | 220 | 0.70 | 21.8
b. Due to communication problems the beam profile was not as broad as in the other irradiations.
c. Target partially melted.

## Slide 15: Outlook
Production of 67Cu at the TR-Flex Cyclotron

## Slide 16: Conclusions & Future Steps
    Couple hundred MBq of 67Cu were produced from 70Zn electrodeposited targets and ZnO targets, expecting to reach the GBq range with longer irradiation times. Two targets proposals should be considered:
      Electrodeposited 70Zn target:1.0 MBq/µA h and 6.5 GBq/µmol
      [70Zn]ZnO target: 0.70 MBq/µA h and 21.8 GBq/µmol
    [67Cu]CuCl2 product solution free of other radionuclides
    Recycling yield about 95%: reduction of the production costs

## Slide 17: Thank you for your attention!