## Slide 1: 68Ga Production from liquid target: Determination of solubility of ZnCl2 in HCl solutions
Mátyás FodorI,II
Zoltán Szűcs PhDII
IDoctoral School of Chemistry, University of Debrecen, Debrecen, Hungary
IIRadiochemical Laboratory, Institute for Nuclear Research, Debrecen, Hungary

## Slide 2
68Ga is a positron emitting radioisotope
It is produced:
  by the 68Zn(p,n) 68Ga reaction in cyclotrons
  from 68Ge generators via electron capture decay
t1/2 for 68Ga is 67.8 minutes
Gamma energies are 511keV, 1077keV and 1883keV(2)
It is well suited for PET diagnostics, and is routinely used
Normally solid Zn targets are employed for production(3)
68Ga’s role in nuclear medicine
(1)

## Slide 3: Production from liquid target
Literature mentions
production using Zn(NO3)2 solution(4)
Problems with this approach:
Zn(NO3)2 has worse solubility (in water) than ZnCl2(5,6)
For equal masses of solids, Zn(NO3)2 has less Zn2+ ions than ZnCl2
More target nuclei for irradiation when using ZnCl2
 | Molar mass (g/mol) | Zinc/100g (g)
ZnCl2 | 136.3 | 48.0
Zn(NO3)2 | 189.4 | 34.5

## Slide 4
Our goal is to develop a method with the following key parameters:
  68Ga production via cyclotron
  using a liquid target
  68Zn enriched ZnCl2 in HCl solution
Production from liquid target
An example of a liquid target system, based on(7)
Target
[68Zn]ZnCl2 solution
He gas
/[68Zn]ZnCl2 recovery
Syringe
IBA Synthera+
LOAD position
[68Zn]ZnCl2 solution to target, overflow waste can optionally be recovered...

## Slide 5
Our goal is to develop a method with the following key parameters:
  68Ga production via cyclotron
  using a liquid target
  68Zn enriched ZnCl2 in HCl solution
Production from liquid target
An example of a liquid target system, based on(7)
Target
[68Zn]ZnCl2 solution
He gas
/[68Zn]ZnCl2 recovery
Syringe
IBA Synthera+
UNLOAD position
[68Ga]GaCl3 solution to IBA Synthera+ panel, for radiolabeling
(Future work...)

## Slide 6
Benefactors:
Faster purification compared to solid targets
Fewer steps required (no need to dissolve a solid target)
Easily automated, compared to solid target systems (utilizing existing systems, eg. 18F)
Determination of ZnCl2 solubility in HCl solutions
(8)
Solid target
Liquid target

## Slide 7
Benefactors:
Faster purification compared to solid targets
Fewer steps required (no need to dissolve a solid target)
Easily automated, compared to solid target systems (utilizing existing systems, eg. 18F)
Problems:
Any liquid target will have fewer “useful” nuclei to irradiate, compared to solid targets
An optimum in concentration needs to be found, to generate highest activity
We need solubility data for different HCl concentrations
Determination of ZnCl2 solubility in HCl solutions
Recently purchased IBA Synthera+ system

## Slide 8
Preparation of ZnCl2 from metallic Zn was attempted
Zn metal in cc. HCl solution was dissolved
Evaporation to dryness failed
Even leaving the solution on the hotplate on 100°C (212°F) over the weekend yielded a thick syrup, not solid crystals
Determination of ZnCl2 solubility in HCl solutions – initial failures

## Slide 9
Experiments were continued with anhydrous ZnCl2 purchased from a manufacturer
The solids were protected from moisture in the air
This was done via storing the container in a vacuum desiccator above P2O5, and measuring the solids into screw-cap vials, in a glovebox under Ar atmosphere
Determination of ZnCl2 solubility in HCl solutions - challenges
vacuum desiccator
glovebox under Argon atmosphere

## Slide 10
First, solubility was measured on ambient temperature, with continuous stirring
HCl solution was added dropwise
Temperature of the solution has risen greatly when the HCl solution was added to the solids
As solubility is temperature dependent, this led to inaccurate results
To counter this, a water bath and stirring was employed
1.
1. ZnCl2 solution in HCl acid
2. stirring bar
3. hotplate with magnetic stirring
4. screw-cap vial with the sample
3.
2.
4.
Determination of ZnCl2 solubility in HCl solutions – more failures...

## Slide 11
The measurements were carried out as shown on the diagram
Experimental temperatures were 20-80°C (68-176°F)
HCl concentrations were 1-12M
The temperature of the water bath fluctuated as much as ±10°C (± 18°F)
To counter this, a thermometer controlled hotplate was chosen
1.
4.
2.
3.
1. hotplate with magnetic stirring
2. water bath
3. stirring bars
4. screw-cap vial with the sample
5. thermometer
6. display of the hotplate’s
temperature
6.
5.
Determination of ZnCl2 solubility in HCl solutions – final adjustments

## Slide 12
With this new, improved setup, the experiments were carried out again
Temperature was more stable, in the range of ±2°C(±3°F) (measured with a calibrated thermometer)
The thermometer was placed as close to the vials as possible
Solution was allowed to warm up to the waterbath’s temperature
Overall, much better results
1.
4.
2.
3.
5.
1. hotplate with magnetic stirring
2. water bath
3. stirring bars
4. screw-cap vial with the sample
5. thermometer connected to the
hotplate
6. display of temperature
6.
Determination of ZnCl2 solubility in HCl solutions – measurement

## Slide 13
Every measurement was repeated at least 3 times
First, solubility was determined at 23°C (73°F) for different acid concentrations
Solubility was highest in 3M HCl solution, with 274±18g solids dissolved in 100ml
Chart: ZnCl2 solubility at 23°C
| 1 | 3 | 6 | 9 | 12
 | 250 | 274 | 245 | 252 | 220
Determination of ZnCl2 solubility in HCl solutions – the results

## Slide 14
Next, the water bath was heated to 50°C (122°F)
As expected, solubility increased
The highest solubility was 356±16g/100ml in 6M acid solution
Determination of ZnCl2 solubility in HCl solutions – the results
Chart: ZnCl2 solubility at 23°C
| 1 | 3 | 6 | 9 | 12
 | 250 | 274 | 245 | 252 | 220
Chart: ZnCl2 solubility at 50°C
| 1 | 3 | 6 | 9 | 12
 | 343 | 342 | 356 | 310 | 265

## Slide 15
Finally, 6M HCl solution was chosen and solubility was tested at different temperatures
As expected, solubility increased with temperature
Above 60°C (140°F), HCl evaporation became prevalent, as liquid drops appeared at the neck of the vial
This made measurements inaccurate
Determination of ZnCl2 solubility in HCl solutions – the results
Chart: ZnCl2 solubility at 50°C
| 1 | 3 | 6 | 9 | 12
 | 343 | 342 | 356 | 310 | 265
Chart: ZnCl2 solubility in 6M HCl solution
| 0 | 20 | 40 | 50 | 60 | 80
 | 149 | 253 | 271 | 356 | 390 | 401

## Slide 16
I’ve found that HCl solutions dissolve less ZnCl2 than pure water
Despite this, 6M and more dilute HCl solution can still dissolve great amounts of ZnCl2
6M solution might be ideal as it is anisotropic
Following experiments will include the design, and pressure test of the liquid target, and irradiation of [68Zn]ZnCl2 solution
By the optimal irradiation parameters, suggested Szelecsényi et al, the proton beam with energy range 4.5-14 MeV (metal Zn, thickness is 460μm) during 1 hour irradiation can produce 5.76 GBq activity. The dilution of Zn atoms up to 10 mol% still can guarantee the radioactivity of 68Ga in range of GBq.(9)
Determination of ZnCl2 solubility in HCl solutions – conclusions

## Slide 17
Special thanks for the Doctoral School of Chemistry, University of Debrecen.
This work was supported by the project TKP2021-NKTA-42 financed by the National Research, Development and Innovation Fund of the Ministry for Innovation and Technology, Hungary.
Acknowledgements

## Slide 18
Thank you for listening
Referenses:
1Maecke, H. R., & André, J. P. (n.d.). 68Ga-PET Radiopharmacy: A Generator-Based Alternative to 18F-Radiopharmacy. PET Chemistry, 215–242.
2Benešová M, Reischl G. Production of radionuclides: Cyclotrons and reactors. In: Signore A, editor. Nuclear Medicine and Molecular Imaging. Oxford: Elsevier; 2022. p. 52-65.
3Recommended cross sections with estimated uncertainties for the 68Zn(p,n)68Ga reaction [Internet]. https://www-nds.iaea.org/: IAEA; 2018 [updated 2018 Aug; cited 2022 Jul 21].
4International Atomic EA. Gallium-68 cyclotron production. International Atomic Energy Agency (IAEA): 2019. p. 17-21.
5Zinc chloride [Internet]. National Center for Biotechnology Information: PubChem; 2022 [updated 2022-07-15; cited 2022-07-22]. Available from: https://pubchem.ncbi.nlm.nih.gov/compound/ZINC-chloride#section=Solubility. 6Zinc nitrate [Internet]. National Center for Biotechnology Information: PubChem; 2022 [updated 2022-07-16; cited 2022-07-22]. Available from: https://pubchem.ncbi.nlm.nih.gov/compound/ZINC-nitrate#section=Solubility. 7International Atomic EA. Gallium-68 cyclotron production. International Atomic Energy Agency (IAEA): 2019. p. 21. 8International Atomic EA. Gallium-68 cyclotron production. International Atomic Energy Agency (IAEA): 2019. p. 4. 9Szelecsényi, F., Boothe, T.E., Takács, S., Tárkányi, F., Tavano, E.: Evaluated cross section and thick target yield data bases of Zn+p processes for practical applications. (1998) Applied Radiation and Isotopes, 49 (8), pp. 1005-1032.