## Slide 1: Alpha Irradiation of Germanium Metal Targets for Production of High Specific Activity 72Se/72As: Challenges Associated with Thick Target Preparation
Sean Tanzey1, Eric Dorman1, Ezgi Yalcintas Bethune1, Robert Smith1, A. Lake Wooten1, Greg Felsted2, Peter Pauzauskie2, Marissa Kranz1, David Argento1, Robert Emery1, Heather M. Hennkens3,4, Silvia S. Jurisson3, Dmitri G. Medvedev5, Cathy S. Cutler5, D. Scott Wilbur1, Yawen Li1
Department of Radiation Oncology, University of Washington, Seattle, WA, USA
Department of Materials Science & Engineering, University of Washington, Seattle, WA, USA
Chemistry, University of Missouri, Columbia, MO, USA
Research Reactor, University of Missouri, Columbia, MO, USA
Collider Accelerator Department, Brookhaven National Laboratory, Upton, NY, USA
18th Workshop on Targetry and Target Chemistry

## Slide 2
Arsenic-72: PET isotope with a 26 hr half-life and Eß+max = 2.5 MeV
  Produced directly from natural germanium (natGe) with proton irradiation.
    Multiple As radioisotopes produced that cannot be separated
  Decay product of Selenium-72 parent (t1/2 = 8.4 d)
    Produced from the 70Ge(α,2n)72Se
Has a theranostic isotope pair As-77
Potential for making As-72 generator after
isolation of Se-72
Selenium-72/Arsenic-72
Y. Feng, et al., Applied Radiation and Isotopes, 2019, 143, 113–122
Example generator system
Ga-68
2

## Slide 3
Se-72 produced from 18-50 MeV alpha
Coproduction of Se-73 and Se-75 at 20-30 MeV
Se-73 half-life is 7.15 h (28x less than Se-72 half-life)
Se-75 half-life is 119.8 d and decays to stable As-75
Cross-Section Data
Chart: 70Ge(α,x)72,73,75Se
| 16.7 | 17.600000000000001 | 18.399999999999999 | 19.3 | 20.2 | 21.8 | 23.2 | 23.8 | 24.6 | 25.1 | 26 | 26.4 | 27.7 | 28.3 | 28.9 | 29.5 | 30.1 | 30.7 | 31.4 | 32 | 32.5 | 33.1 | 33.6 | 34.1 | 34.700000000000003 | 35.299999999999997 | 35.700000000000003 | 36.700000000000003 | 37.700000000000003 | 38.6 | 39.5 | 40.5 | 41.5 | 42.4 | 44.3 | 45.2 | 46
Se-72 | 6 | 26 | 32 | 44 | 78 | 104 | 160 | 248 | 224 | 272 | 299 | 342 | 382 | 381 | 407 | 425 | 423 | 392 | 421 | 403 | 425 | 400 | 430 | 400 | 416 | 361 | 416 | 403 | 344 | 290 | 279 | 241 | 220 | 177 | 147 | 126 | 101
Se-73 | 78 | 122 | 182 | 188 | 250 | 354 | 370 | 464 | 496 | 572 | 531 | 526 | 579 | 486 | 460 | 336 | 298 | 222 | 139 | 116 | 90 | 61 | 54 | 45 | 38
Se-75 | 106 | 235 | 372 | 319 | 502 | 700 | 603 | 647 | 722 | 700 | 616 | 640 | 500 | 394 | 323 | 312 | 198 | 194 | 143 | 179 | 118 | 125 | 84 | 78 | 68 | 69 | 55 | 74 | 52 | 43 | 28 | 21 | 27 | 22 | 22 | 21 | 17.8 | 13.9 | 16.7 | 16.7 | 13
3
Dmitriev, P.P., et al. At Energy, 1973, 34, 499–500

## Slide 4: Previous Work
4

## Slide 5
47.3 MeV α-beam at 120 µAh
Max beam current: 20 µA
Enriched Ge-70 metal powder
Graphite attenuation: 47.3 to 34.8 MeV
Degradation of graphite layer during irradiation
Graphite-Encased Germanium Target
3 mm
25.4 mm
1.5 mm
Graphite powder
Ge metal powder
Graphite powder
13 mm
With Ethan Balkin
Y. Feng, et al., Applied Radiation and Isotopes, 2019, 143, 113–122
5

## Slide 6
47.3 MeV α-beam at 22 µAh
Max beam current: 20 µA
Aluminum attenuation: 47.3 to 44 MeV
Hole burned through Al layer
Na-24 and Na-22 produced in Al cover making it difficult to work with
Aluminum-Covered Germanium Target
3 mm
25.4 mm
1.5 mm
Aluminum
Ge metal powder
Graphite powder
13 mm
Al
mp = 660 °C
ρ = 2.7 g*cm-3
Thermal Conductivity = 239 W*m-1 * K -1
6

## Slide 7: Current Work
7

## Slide 8
47.3 MeV α-beam at 5 µA for 15 minutes
47.3 MeV α-beam at 10 µA for 15 minutes
Na-22 found in all Si discs
  Majority in 1st disc and the least amount in 5th (last) disc
Silicon wafer irradiation test
3 mm
25.4 mm
Si disc
Si disc
Si disc
Si disc
Si disc
12 mm
1 mm
Si
mp = 1,410 °C
ρ = 2.3 g*cm-3
Thermal Conductivity = 130 W*m-1 * K -1
Isotopes Observed | t1/2 (h) | Total | Target Holder | Disk 1 | Disk 2 | Disk 3 | Disk 4 | Disk 5
Al-28 | 0.037 | N.A. | 21% | 79% | 0% | 0% | 0% | 0%
Mg-28 | 20.9 | 39.6 nCi | 32% | 68% | < 1% | < 1% | < 1% | 0
Be-7 | 1274.9 | 37.1 nCi | 0% | 80% | 20% | < 1% | 0 | 0
Na-24 | 15 | 4086 nCi | 60% | 39% | 1% | 0 | 0 | 0
Na-22 | 22791.8 | 2.6 nCi | 67% | 33% | 1% | < 1% | < 1% | < 1%
HPGe analysis 2 h after EOB
8

## Slide 9
3-piece target design
  Aluminum 6061
  Metal-metal contact interfaces
  Warped at pressure needed to press Ge
  Could not hold vacuum
Target Design
2-piece target design
  Aluminum 6061
  O-ring placed between two pieces
  Withstands pressure needed to press Ge
  Holds vacuum
With Bob Smith
9

## Slide 10: Target Preparation
Press 2 Al discs at 10 MPa for 1 min
  0.2 mm thick/Al disc (0.38-0.4 mm total thickness)
Press 170 mg Ge powder at 10 MPa for 10 min
  Captures 20-41 MeV alphas
  Press ~90 mg of Ge powder 2x
  Ge pellet density does not reach actual density
    3.2 g/cm3 vs 5.5 g/cm3
Place Si disc on top and screw down lid with O-ring
Thermal Conductivity (W*m-1 * K -1)
Al
239
Ge
59.9
Si
130
10

## Slide 11
47.3 MeV α-beam at 5 µAh
Max beam current: 7 µA
Si wafer removed with gravity
  Some Ge bonded to Si disc post-irradiation
80% of germanium pellet recovered using spatula
Silicon Window Germanium Target
47.3 MeV α-beam at 6 µAh
Max beam current: 15 µA
Had difficulty removing material where “burn” spot was and had trouble fully dissolving material
Target material thought to have melted possibly due to overfocusing of beam
11

## Slide 12: Releasing Agent
Want something that will form a thin film, be resistant to high temperatures, water/carbon/silicon based
Boron Nitride (BN)
  High temperature release coating from Miller-Stephenson
  Thermal Conductivity:
    751 W/(m*K) (Cai et al., Sci. Adv. 2019; 5:eaav0129)
    550 W/(m*K) (Yuan et al., Comm. Phys, 2019, 2:43)
  100% non-flammable aerosol formulation
12

## Slide 13: Boron Nitride (BN) Release test
Optimal spray for 3 seconds 6 inches from surface
  Let dry for 3-5 minutes before touching/pressing
Germanium targets prepared w/ & w/o BN on aluminum
  Targets subjected to 250 °C and vacuum
Weight: 64 mg 66 mg
Thickness: 0.2 mm 0.22 mm
w/o BN
w/ BN
w/ BN
w/o BN
13

## Slide 14
47.3 MeV α-beam at 10 µA for 15 minutes
Target prepared with BN release agent and preheating Ge (105 °C overnight)
Hole burned through Si, losing 24.5 mg of material (Ge and Si)
Si disc needed to be removed with spatula
  Majority of germanium was bonded to Si when removed
Silicon Window Germanium Target with BN
14

## Slide 15
Raman shifts of Ge-O and Ge-water peaks
Measured Raman shifts of germanium samples
Raman Spectroscopy Analysis
15
P.K. Giri, S.Dara, Journal of Nanomaterials, 2012, 2012, 905178

## Slide 16
Hot spots in Ge layer match with turbulent flow inside cooling cup
Thermal Modeling
Inlet
Si
Ge
Al
Al: 1734.29 °C Cooling Water: 68.49 °C Ge: 1076.59 °C Si: 668.82 °C
Ge mp = 938 °C
With David Argento, Marissa Kranz, and Rob Emery
16

## Slide 17
New cooling cup shows a 10x decrease in max temperatures reached in germanium and silicon layers
Thermal Modeling
Al: 107.1 °C Cooling Water: 52.08 °C Ge: 134.65 °C Si: 138.47 °C
Inlet
outlet
Si
Ge
Al
With David Argento, Marissa Kranz, and Rob Emery
17

## Slide 18
Multiple target configurations are susceptible to target failures
  Graphite sandwich
  Aluminum cover
  Silicon cover
Silicon is promising for multiple reasons
  Good thermal properties
  Low production of radioisotopes
  Easily removable
Boron Nitride allows for easy removal of germanium pellet post-irradiation
Thermal Modeling shows sufficient cooling can be achieved with new cooling cup
Summary
18

## Slide 19: Acknowledgements
Thermal Modeling
  Marissa Kranz
  Rob Emery
  David Argento
Target Preparation and irradiation
  Bob Smith
  Eric Dorman
University of Washington Physics Machine Shop
  Bob Scott (manager)
WTTC18 Committee Travel Bursary
This research is supported by the U.S. Department of Energy Isotope Program, managed by the Office of Science for Isotope R&D and Production
  DE-SC0020159 (8/1/2019 – 7/31/2021)
  DE-SC0018662 (6/1/2018 – 5/31/2020)
19
18th Workshop on Targetry and Target Chemistry

## Slide 20: Thank you!

## Slide 21: Supplemental

## Slide 22
Se-72 emits 45.9 keV gamma in Compton scattering region of HPGe spectra
Se-72 quantity based on transient equilibrium with daughter, As-72
As-72 emits 834 (81% Iγ) and 630 (8.1% Iγ) keV gamma that can be distinguished
Gamma Analysis

## Slide 23
Predicted production rate using natGe: 28 µCi/µAh
E0 = 20 MeV
E1 = 41 MeV
Summary
Target | Max beam current (µA) | Total Charge (µAh) | Production Rate (µCi/µAh)
Graphite encased | 20 | 120 | 62.2
Graphite covered | 10 | 15 | 17.8
Aluminum cover | 20 | 22 | 6.7
Si cover 1 | 5 | 4.5 | 37
Si cover 2 | 12 | 6 | 26.4
Si cover 3 | 10 | 2.95 | 16.4

## Slide 24
Data for thermal contact resistance to be used in Ansys for better thermal modeling
Test different target configurations to see how each layer effects heat transfer
  Fully Assembled Target
  Target without Si cover
  Target without Ge layer
  Target base
Thermal Contact Testing

## Slide 25
47.3 MeV α-beam at 5 µAh
Other Radioisotopes Observed
47.3 MeV α-beam at 6 µAh
 | Yield at EOB (µCi) | Production Rate (µCi/µAh)
As-74 | 67 | 15
As-72 | 3779 | 840
As-71 | 90 | 20
Ge-75 | NA* | NA*
Se-75 | 24 | 5
Ge-69 | 191 | 43
 | Yield at EOB (µCi) | Production Rate (µCi/µAh)
As-74 | 37.2 | 8.3
As-72 | 2206.1 | 490.2
As-71 | 156.0 | 34.7
Ge-75 | NA | NA
Se-75 | 22.7 | 5.1
Ge-69 | 136.3 | 30.3