## Slide 1
Electroplating and recycling chromium targets for 52Mn production
Margarita Chernysheva, Kendall Barrett, Todd Barnhart, Jonathan Engle

## Slide 2
Production of 52gMn from natCr targets
2

## Slide 3
Previously used hydraulically pressed natCr targets at UW-Madison
To produce natCr targets that were thick to a 16 MeV proton beam, natCr pellets were hydraulically pressed onto 2 mm thick silver disks using 2 tons of force for 10 seconds (A). These targets were then irradiated at currents up to 60 µA to integrated fluences ranging from 40-80 µAh (B)
Method setbacks:
Large standard deviation of Cr present in solution to be purified – 473 180 mg (n=5)
  Impacts separation factor and overall trace metal content of final fraction
Small diameter of Cr pellet does not capture entire beam spread on UW-Madison GE PETTrace cyclotron (C)
  Production yield is not optimized with smaller diameter targets
Solution: Move to electroplated natCr targets to control mass of target, optimize production and be able to recycle them
C
3
Graves, S. A (2017) Doctoral Thesis for University of Wisconsin- Madison

## Slide 4
natCr electrodeposition from electrolyte based on oxidation state:
Hexavalent Chromium Cr(VI) | Trivalent Chromium Cr(III)
Electrodeposits in thick layer | Possible to recycle
Control over target mass | Non-toxic
Good adhesion to target backing | Limited mass can be electroplated – but targets produced are thick to 12 MeV
Difficult to recycle | Degassing observed during irradiate due to adhesion difficulties
Toxic | Mix of Cr and Cr2O3 after dissolution of target
CrO3 + H2SO4
CrCl3 + ChCl
CrCl3 + HCOOH
+ H2SO4
4

## Slide 5
Targets from Cr(VI) electrolyte
CrO3 + H2SO4 = 100:1
mCr electrolyte [g] | mCr plated [mg] | efficiency [%] | 
1.77 | 162 | 9.2 | 
1.77 | 262 | 14.8 | 
1.77 | 154 | 8.7 | 
5
Working electrode: Silver disk
Counter electrode: Pt wire/Ti mesh covered with Pt
Current density: 0.2-0.3 A/cm2

## Slide 6
Targets from Cr(III) electrolyte
Component | Concentration [mg/mL]
Cr metal powder | 0.75-0.85
HCl | 0.4
HCOOH | 40
H2SO4 | 2
6HCl {H2O} + 2Cr  2CrCl3 {6H2O} + 3H2
current density 0.23 A/cm2
 | N=1 | N=2 | N=3 | N=4 | N=5 | N=6 | N=7
m(added Cr to electrolyte) [mg] |  | 16.4 | 20.5 | 31.4 | 27.1 | 17.1 | 43.9
m(Сr in electrolyte) [mg] | 84.1 | 82.8 | 86.8 | 77.5 | 83.5 | 80.0 | 85.6
m(Сr on substrate) [mg] | 66.4 | 66.3 | 46.1 | 56.4 | 62.9 | 41.7 | 66.8
Efficiency [%] | 78.9 | 80.0 | 53.1 | 72.8 | 75.3 | 52.1 | 78.0
Masses and efficiencies of electroplated recycled targets
6

## Slide 7
natCr targets from Cr(III) electrolyte
natCr electroplated target before (up) and after (down) irradiation
Raman spectroscopy of the Cr targets
7

## Slide 8
Production yield using electroplated natCr targets
natCr3+ Targets irradiated at 12 MeV
natCr6+ Targets irradiated at 16 MeV
Mass [mg] | Yield [mCi/µAh] | Integrated Current [µAh]
79 | 0.04 | 23
72.7 | 0.05 | 30
180 | 0.07 | 30
Mass [mg] | Yield [mCi/µAh] | Integrated Current [µAh]
205.5 | 0.18 | 73
120 | 0.15 | 80
140 | 0.15 | 84.7
*Assuming 10% error for yield
8
D. Thor, J. Siikanen (2022) Matlab Theoretical Yield Tool – Beta Version, Karolinska University

## Slide 9
H2O2
HCl
80.0%
20.0%
drying
100%
CrCl3
Cr2O72-
1 week later
What can be done with the rest of electrolyte?
CrCl3 targets
9

## Slide 10
CrCl3 irradiation
Degrader: 10 µm Nb foil​
Energy: ˜12 MeV​
Integrated current: 6.7 µAh​
61 µCi on target​
471 µCi on Nb foil​
Yield ˜0.01 mCi/µAh​
158.36 mg CrCl3 x 6H2O​
Density: 1.76 g/cc​
10

## Slide 11
natCr recycling from dissolved electroplated target and reduced electrolyte
 | Initial | 1st loop | 2d loop | 3d loop
m (plated Cr), mg | 104.1 | 110.3 | 45.0 | 13.7
Efficiency, % | 71.0 | 75.3 | 30.7 | 9.4
Na2O2
NaOH
torch
centrifugation
11

## Slide 12
Conclusions and future studies
We successfully electroplated enriched 52Cr
  65 mg irradiated at 12 MeV for 30 µAh
  Yield: 0.052 mCi/µAh
Presented results indicate that the production of targets from electroplated natCr gives multiple opportunities to recycle enriched 52Cr to produce pure 52gMn
Investigation of opportunities to decrease Cr2O3 formation
Try to plate thicker targets with better adhesion from Cr(III) electrolyte
12

## Slide 13
Acknowledgement
Prof. Dr. Jonathan Engle
Prof. Dr. Robert Nickles
Prof. Dr. Paul Ellison
Dr. Todd Barnhart
Dr. Eduardo Aluicio-Sarduy
Aeli Olson
Kaelyn Becker
Kendall Barrett
Wilson Lin
Molly DeLuca
Thank you to the DOE Isotope Program, managed by the Office of Science for Isotope R&D and Production for funding support and the WTTC18 travel bursary.

## Slide 14
THANK YOU!