## Slide 1
7/18/2022
New metallic germanium target fabrication and dissolution techniques for the cyclotron production of positron-emitting 71As and 72As
Yi-Hsuan Lo1, Todd E. Barnhart1 Jonathan W. Engle1, Silvia S. Jurisson2,3, Heather M. Hennkens2,3, Paul A. Ellison1
1Department of Medical Physics and 2Department of Radiology, University of Wisconsin School of Medicine and Public Health, Madison, WI 53705, USA
2Department of Chemistry, University of Missouri and 3University of Missouri Research Reactor Center, Columbia, MO 65211, USA
18th Workshop on Targetry and Target Chemistry

## Slide 2
Research topic
77As beta emitter and 71/72As positron emitter
Homologous relationship with 119Sb
119Sb MAe- emitter
N
P
As
Sb
Bi
72Se 8.4 d Ec only | 73Se |  | 72Se 0.89% | 75Se 119.8 d EC only |  | 76Se 9.4 % | 77Se 7.6 % |  | 78Se 23.8 % | 79Se | 
 | 7.2 h | 40 m |  |  |  |  |  |  |  | 4 m | 3×105y
71As 65.3 h β+: 816 keV... | 72As 26 h β+: 1117 keV. |  | 73As 80.3 h Ec only | 74As 17.8 d |  | 75As 100 % | 76As 26.4 h β-: 2962 keV |  | 77As 38.8 h β-: 683 keV | 78As 90.7 m β-: 4209 keV | 
 |  |  |  | β+ | β- |  |  |  |  |  | 
70Ge 20.57% | 71Ge 11.43d Ec only |  | 72Ge 27.45% | 73Ge 7.75% |  | 74Ge 36.5% | 75Ge |  | 76Ge 7.73% | 77Ge | 
 |  |  |  |  |  |  | 48 s | 83 m |  | 53 s | 11 h
[1] P.A. Ellison et al. Bioconjug. Chem. 27 (2016) 179–188. [2] Y. Feng et al., Appl. Radiat. Isot. 143 (2019) 113–122.
[3] Matthew D.Gott et al., Journal of Chromatography A, 1441(2016) 68-74
Notes: As77 could be produced by Ge77 and be used as beta emitters to treat cancer cells.
There are very limited number of places that have an accelerator capable of the 72Se production and so it only has very limited availabilityPut reference As-72 Ellison biocol chem 2015 Put reference Se-72 Y. Feng et al., Appl. Radiat. Isot. 143 (2019) 113–122.
Gott et al. J Chromatogr A for (n,r)
Having a slide after it about .
76Ge(n, γ)77Ge reaction in a reactor, and then β− decays to 77As

## Slide 3
Research topic
Pre irradiation:
After 4 μA*
Difficult to dissolve it and As isolation yield deceased.
GeO2
[1] P.A. Ellison et al. Bioconjug. Chem. 27 (2016) 179–188.
Problem… it is incompatible with deuterons and commercial solid target irradiation systems.
4π-water-cooled target
GeO2 target
Problem… Only tolerant to low beam.
[4] P.A. Ellison et al., AIP Conf. Proc. 1509 (2012) 135-140.
Notes: GeO2 pressed at 225 MPa into H2O-jet-cooled stainless steel or Nb holde
Significantly diminished dissolution and As isolation yields.

## Slide 4
Research topic
Radiopharmaceuticals
Target making
Bombardment
Isolation
Radiolabeling
Reclamation

## Slide 5
Research topic
Radiopharmaceuticals
Bombardment
Radiolabeling
Target making
Isolation
Reclamation

## Slide 6
Research topic
Bombardment
Target making
Isolation (non-radioactive )
70Ge (d,n) 71As
72Ge (p,n) 72As
Bombardment
Dissolution and Separation
Reclamation
Ta coin (⌀=10 mm, 1 mm deep)

## Slide 7
Target making
Bombardment
Target making
Isolation
Reclamation
Ta coin (⌀=10 mm, 1 mm deep)
Ge bb making
Hot pressing
Ge Target

## Slide 8
Method
Target making: Germanium bb making
NatGe bb
≈
Prepare NatGe (~70 mg) powder in carbon crucible.
Heated in furnace for 30 min (1045° C)
Use furnace to heat Ge to form Ge bb.
Ar infilled

## Slide 9
Method
Target making: Ge target production
≈
Prepare NatGe bb (~70mg) on Ta coin.
Heated in furnace at 1000 ° C for 5 min
Hot pressing in furnace
Heated in furnace for 10 min (1000° C)
Ta coin
NatGe
Tamper (Boron nitride)
Ta coin (⌀=10 mm, 1 mm deep)
Ar infilled

## Slide 10
Result
Target making: Germanium bb making and Ge target production
Ge bb making | Initial Ge powder mass (mg) | Ge Loss (mg) | Ge % Loss | 
Natural | ~70 | 0.3 ± 0.27 | 0.5 ± 0.35 | -
Ge-Ta target making | Initial Ge bb mass (mg) | Ge loss on target (mg) | Ge % Loss | Ge thickness (μm)
 | ~70 | 0.7 ± 0.73 | 0.9 ± 1.0 | 325 ± 44
Notes: However, we still can not always make a perfect target like the fully covered Ge target. So we keep trying to improve the procedure to get much better target.

## Slide 11
Result
Target making: Germanium bb making and Ge target production
Ge bb making | Initial Ge powder mass (mg) | Ge Loss (mg) | Ge % Loss | 
Natural | ~70 | 0.3 ± 0.27 | 0.5 ± 0.35 | -
Ge-Ta target making | Initial Ge bb mass (mg) | Ge loss on target (mg) | Ge % Loss | Ge thickness (μm)
 | ~70 | 0.7 ± 0.73 | 0.9 ± 1.0 | 325 ± 44
Theoretical thickness: 166 μm
[5] K. Otozai, et al., Nucl. Phys. A. 107 (1968) 427–435. [6] J.F. Ziegler et al., Nucl. Phys. B. 268 (2010) 1818–1823.

## Slide 12
Bombardment: Irradiation study
Method & Result
Targetry | Reaction | Energy (MeV) | Experiment (mCi/μAh) | Theory (mCi/μAh) [5,7]
Prototype coin-type target | 72Ge(p,n)72As | 12 | 2.5 | 5.7
Prototype coin-type target | 70Ge(d,n)71As | 8 | 0.17 | 0.17
*Enriched target yields extrapolated from experimental proton and deuteron irradiations of a natGe target |  |  |  | 
Before irradiation (deuteron)
After irradiation (deuteron)
Irradiation condition |  | 
Projectile | Proton | Deuteron
Energy | 12 MeV | 8 MeV
Current | 30μA | 18.5 μA
Target | natGe | NatGe
Before irradiation (proton)
After irradiation (proton)
[5] K. Otozai, et al., Nucl. Phys. A. 107 (1968) 427–435. [7] I. Spahn, et al., Appl. Radiat. Isot. 65 (2007) 1057–1064
Notes: Why we choose 12 MeV??
Reference beam spot is larger than coin

## Slide 13
Method
Isolation: Dissolution of Ge
Add 2 mL 0.48M NH4OH in 30% H2O2
Heated at 100 °C for 15 min.
Add 2.5 mL aqua regia
Heated at 100 °C for 30 min.
Add 2 mL 37% HCl
Heated at 100 °C for 15 min.
Dropwise addition of 2 ml of 30% H2O2
NH4OH method
HCl method
Aqua Regia method

## Slide 14
Result
Isolation: Dissolution of Ge
Conclusion
Aqua regia condition dissolved more mass of Ge than others under the same reaction time.
No significant mass lost for Ta coin under aqua regia condition.
Condition | Ge-coated Ta coin |  | 
Dissolution solution | 0.48M NH4OH [M] in 30% H2O2 [7] | 37% HCl with 30% H2O2 [8] | Aqua regia [1]
Solution volume (mL) | 2 | 2 | 2.5
Total reaction time (min) | 15 | 15 | 30
Reaction Temp. (°C) | 100 | 100 | 100
Ge mass dissolved (mg) | 6.9 ± 0.7 (14±2%) n=20 | 20.7 ± 7.4 (25±10%) n=5 | 153± 12 (100%) n-=6
Ta coin mass dissolved (mg) | 1.1 ± 0.2 n=4 | 0.1± 0.1 n=3 | 0.0±0.1 n=3
[8] Y. Feng et al., Appl. Radiat. Isot. 143 (2019) 113–122. [9] J. W. Irvine, Jr., J. Phys. Chem. 46, 910 (1942) 910-914
Notes: Why did you try these methods? Why Ta coins? These reagents? Justify with reasoning/citations.

## Slide 15
Method
Reclamation: Dissolution and Distillation
Ge+4HNO3 GeO2+4NO2+2H2O
GeO2+4HCl GeCl4+2H2O
Dissolution:
GeO2+4HCl GeCl4+2H2O
Distillation and Hydrolysis:
GeCl4+2H2O GeO2+4HCl
2ml HCl
NatGe pieces mass ~150 mg
71/72AsCl5
71/72AsCl5 would remain in heating tube during distillation

## Slide 16
Method
Reclamation: Dissolution and Distillation
Ge+4HNO3 GeO2+4NO2+2H2O
GeO2+4HCl GeCl4+2H2O
Dissolution:
GeO2+4HCl GeCl4+2H2O
Distillation and Hydrolysis:
Reclamation:
GeO2
GeCl4+2H2O GeO2+4HCl
NatGe bb
Heated at 1045°C for 30 min
NatGe powder
Reduction under H2 at 600°C for 1.5 h

## Slide 17
Method
Reclamation: Dissolution and Distillation
HCl capture method
NH4OH neutralization method
NaOH neutralization method
Ge+4HNO3 GeO2+4NO2+2H2O
GeO2+4HCl GeCl4+2H2O
Dissolution:
GeO2+4HCl GeCl4+2H2O
Distillation:
Reclamation:

## Slide 18
Reclamation: Distillation and Reclamation
GeO2
Dry out the precipitate with Ar and
Heated at 150°C to remove residual HCl
Method
HCl capture method
2ml HCl
NatGe pieces mass ~150 mg

## Slide 19
Reclamation: Distillation and Reclamation
GeO2
Dry out the precipitate and
Heated at 350°C to remove salt
Method
NH4OH
Neutralization
NH4OH
H2O
Condense tube
NH4OH neutralization method

## Slide 20
Reclamation: Distillation and Reclamation
GeO2
Method
NaOH pellet (~2 g)
Neutralization
Wash with H2O
and
Dry out the precipitate
1N NaOH
H2O
Condense tube
NaOH neutralization method

## Slide 21
Reclamation
Result
Condition | HCl capture | NH4OH neutralization | NaOH neutralization
Ge piece mass (mg) | 142.2 | 153.6 | 151.7
 | After removing residual HCl or salt |  | 
NatGeO2 mass (mg) | 103.5 | 86.4 | 53.8
 | After reduction by H2 |  | 
Ge mass | 67.5 | 55.3 | 19.6
 | After bb making |  | 
Ge bb mass | 68.7 | 58.6 | 14.8
Reclamation efficiency % | 48.3% | 38.2% | 9.8%
Notes: Some impurity

## Slide 22
Conclusion
Bombardment
Target making
Isolation
Reclamation
Target production: Improve the target production procedure to get fully covered Ge target.
Reclamation: HCl capture method. Optimization for the procedure to increase the efficiency is needed.
Target cooling problem: The Ge is melted during irradiation. We will use thinner Ta coin and try to make the thickness of Ge thinner.
Separation of As from Ge: Aqua regia method displayed higher Ge mass dissolved and shorter dissolving time.

## Slide 23
Acknowledgement
Thanks to Department of Energy Isotope Program, managed by the Office of Science for Isotope R&D and Production grant DE-SC0022032.
Cyclotron Group
Paul Ellison’s Group
University of Missouri
Todd E. Barnhart, PhD
Professor Jonathan W. Engle
Professor Heather M. Hennkens
Professor Silvia S. Jurisson

## Slide 24
Thanks for your attention

## Slide 25
P.A. Ellison et al. Bioconjug. Chem. 27 (2016) 179–188.
Y. Feng et al., Appl. Radiat. Isot. 143 (2019) 113–122.
Matthew D.Gott et al., Journal of Chromatography A, 1441(2016) 68-74
P.A. Ellison et al., AIP Conf. Proc. 1509 (2012) 135-140.
K. Otozai, et al., Nucl. Phys. A. 107 (1968) 427–435.
J.F. Ziegler et al., Nucl. Phys. B. 268 (2010) 1818–1823.
I. Spahn, et al., Appl. Radiat. Isot. 65 (2007) 1057–1064
Y. Feng et al., Appl. Radiat. Isot. 143 (2019) 113–122. [
J. W. Irvine, Jr., J. Phys. Chem. 46, 910 (1942) 910-914
Reference

## Slide 26
Bombardment: Irradiation study
Method & Result
Irradiation condition |  | 
Projectile | Proton | Deuteron
Energy | 12 MeV | 8 MeV
Current | 30μA | 18.5 μA
Target | natGe | NatGe
Targetry | Reaction | Energy (MeV) | Experiment (mCi/μAh) | Theory (mCi/μAh) [1,4]
Prototype coin-type target | 72Ge(p,n)72As | 12 | 2.5 | 5.7
Prototype coin-type target | 70Ge(d,n)71As | 8 | 0.17 | 0.17
*Enriched target yields extrapolated from experimental proton and deuteron irradiations of a natGe target |  |  |  | 
Notes: reference

## Slide 27
Research topic
77As beta emitter
End point energy ≈683 keV
T1/2=38.8 h
Problem… The lack of imaging property which can provide in patient selection, target verification and dosimetry.
71/72As positron emitter
T1/2: 71As=65.3 h and 72As=26 h
End point energy: 71As=816 keV and 72As=2500 keV
Homologous relationship with 119Sb
119Sb MAe- emitter
N
P
As
Sb
Bi
77Ge(n,γ)77As
72Ge(p,n)72As--UWisc PETtrace cyclotron
Notes: Put reference As-72 Ellison biocol chem 2015 Put reference Se-72 Y. Feng et al., Appl. Radiat. Isot. 143 (2019) 113–122.
Gott et al. J Chromatogr A for (n,r)
Having a slide after it about .

## Slide 28
Conclusion
Bombardment
Target making
Isolation
Reclamation
Target production Improve the target production procedure to get fully covered Ge target.
Reclamation HCl capture method. Optimization for the procedure to increase the efficiency is needed.