## Slide 1: SRF DEVELOPMENTS AT TRIUMF Vladimir Zvyagintsev RF/SRF Department, Accelerator Division, TRIUMF July 12, 2017 Accelerator Science Workshop TRIUMF, Vancouver, Canada

## Slide 2
RF PROJECTS AT TRIUMF

## Slide 3: Cyclotron RF Projects
Future upgrade of Cyclotron for 400 µA current will require R&D for the RF Amplifier and Resonator
RF Amplifier HFSS and experimental
Study
1 MW CW RF Load is required also to improve tuning and troubleshooting for operation ~$100k
Study of Resonator for mitigation of parasitic modes and rf leakage effects
IPA Upgrade
For better tunability for optimized stable regime of RF Amplifier

## Slide 4: ISAC-I RF Upgrades for A/Q=7 beams at 1.5MeV/u
Tube RF Amplifier Systems =$31k
DTL 1
Buncher3
DTL 3
Buncher1
DTL 2
Buncher2
DTL 5
DTL 4
Prf 3.8kW 9.5kW 9.5kW 7.7kW 16.1kW 13.8kW 22.2kW 24.3kW
Necessary upgrades and budget estimate
Replace cable Additional water cooling
with rigid TL for resonators
$15k + $8k + $8k = $31k
________________________________________________________________________________________________________
Solid State RF Amplifiers =$102k
Prf 500W 500W 500W 500W 500W 2kW 3kW
Budget estimate to order RF Amplifiers
5 x $10k = $50k + $20k + $32k = $102k
__________________________________________________________________________________________________
Total = $131k
DTL Driver
DTL Driver
DTL Driver
DTL Driver
Rotator
DTL Driver
MEBT Driver

## Slide 5
SRF PROJECTS AT TRIUMF

## Slide 6: INTRODUCTION
The TRIUMF SRF program began in 2000 to support the design and development of the ISAC-II heavy ion linac with the addition of infrastructure to support SRF activities
We now have two SC linacs in operation – the 40MV ISAC-II heavy ion linac and the 30MeV ARIEL 1.3GHz electron linac
TRIUMF also hosts important diagnostics in material science – muSR and betaNMR
We have an active program in student based SRF research to augment are operational capabilities
ISAC-II
SRF Facility
betaNMR
muSR
eLinac

## Slide 7: SRF Accelerators
40MV ISAC-II SRF heavy ion linac @ 106MHz - operational since 2006
30MV ARIEL SRF 10mA electron linac @ 1.3GHz – first beam 2014

## Slide 8: ISAC-II HEAVY ION LINAC
Add degassing oven.
  Heat treat cavities (650C 8 hrs) over a five year period
  Eliminate Q-disease (hydrogen) and improve Q and gradient through Nitrogen infusion

## Slide 9: ARIEL e-Linac –> 50MeV
1.3GHz SRF Electron Linac (10mA)
23 MeV demonstrated from two cavities in 2014
Install 30MeV capability in mid 2017 – 30MeV now in commissioning (ramp up power 2018 )
A third cryomodule needed to bring the linac to the initial specification
  Implications for SRF, RF, cryogenics and supporting technologies
Gun
30MeV
50kW
50kW
2014
50kW
50kW
50kW
50kW
50kW
50kW
20xx
50MeV
10MeV
50kW
50kW
ICM
ACM1
ACM2
2017

## Slide 10
ARIEL Cryomodules – 1.5M$
4K-2K Cryoinsert
Strongback
Heat exchanger
4K phase separator
Support Post
WPM bracket
Power coupler
Houses
two nine-cell 1.3GHz cavity
four 50kW power couplers
HOM coaxial dampers
Features
4K/2K heat exchanger with JT valve on board – allows standard 4K cold box
scissor tuner with warm motor
LN2 thermal shield – 4K thermal intercepts via syphon
Two layers of mu-metal
WPM alignment system

## Slide 11: Cavity and processing Developments
With the closure of PAVAC and AES both Canada and North America are severely diminished in terms of cavity production – implications for large global projects like ILC
EACB would be another opportunity to grow an indigenous supplier of ILC type cavities
TRIUMF latest experience in forming, brazing and spinning for SSR cavities for RISP means that more steps can be done in TRIUMF machine shop as required
SSR1 Parts

## Slide 12: E-Linac RF Drive System
M
CAV
CAV 1
M
M
M
M
CAV 2
Klystron1
300kW
CAV1
CAV2
EINJ
EACA
EACB
Presently there are two 300kW CPI klystrons – sufficient for each of EACA and EACB modules - We need a rf source for EINJ rated at ~150kW to reach final e-Linac specification
Klystron2
300kW
150kW

## Slide 13: ARIEL E-LINAC – plasma cleaning
ERL mode operation would largely eliminate beam loading and so would allow higher gradient operation
Higher gradients for EACB cavities
Develop plasma cleaning for in-situ refurbishing of Eacc if required.
Success demonstrated in SNS tunnel – e-linac module design well suited
S. Kim – TTC MSU
TRIUMF has started collaboration with PKU on 1.3GHz single cell cleaning. Initial recipe 6 hours cleaning with Ar/O2 50/50 at 300mTorr and 8MHz 120W RF.
Plasma cleaning on PKU single cell
Zhongyuan Yao

## Slide 14: Recirculating cavity issues
Klystron Gallery
ICM
ACM1
ACM2
MEBT 10MeV Dump
LEBT
E-Gun
30MeV Dump
ERL Dump
75MeV 100kWDump
HEBT
Shielding Wall
RLA
Single user mode only
ERL
Dual-use possible with two interleaved bunch trains into 1.3GHz buckets
650MHz pulse train - single pass acceleration for RIB production – low brightness
650MHz/n pulse train for ERL – high brightness – new gun required
650MHz rf separator used to separate the beams
Chart: 
ERL
RIB
650MHz

## Slide 15: RF Separation of Interleaved Beams
THz/IR FEL
650 MHz eGun
1.3 GHz SRF Cavities
to RIB production
to ERL ring
decelerated bunches
Simultaneous beam delivery to both RIB production and an ERL/FEL requires RF separation of interleaved bunches
cavity is almost complete – for operation will require
  Rf ancillaries - FPC and HOM coupler, tuner
  Cryomodule, 4K transfer line
  650MHz rf source and LLRF
Electric Field
Magnetic Field
Separation Complex
Transport
to ARIEL
Courtesy Douglas W. Storey

## Slide 16
GLOBAL SRF FRONTIERS

## Slide 17: HIGH Q AND HIGH GRADIENT
ILC
LCLS-II
HFQS
120C bake
A. Grassellino – TTC Saclay
N Doping at T > 800C proven to manipulate mean free path, but constantly throughout several microns, giving high Q .
120C bake known to manipulate mean free path at very near surface on clean bulk, and produce the highest gradients.

## Slide 18: HIGH Q AND HIGH GRADIENT
ILC
LCLS-II
The new N2 infusion treatment (FNAL) raises Q (above ILC baseline) and extends the reachable field beyond Bc1. It was proposed to create few to several nanometers of nitrogen enriched layer on top of clean EP bulk, to attempt to bring together the benefit of the Q and gradient.
X2
A. Grassellino – TTC Saclay

## Slide 19: NITROGEN TREATMENT AT TRIUMF
Variations in the infusion process produce significant variations in the performance – requires optimization
Now commissioning a UHV RF induction oven to process single cell 1.3GHz cavities – goal is to explore various doping and infusion recipes.
Also investigate infusion at lower frequencies with co-axial resonators -> ISAC-II
A. Grassellino – TTC Saclay

## Slide 20: MFQS IN LOW BETA CAVITIES
  Strong Medium Field Q-Slop (MFQS) exists in low frequency and low β resonators.
  Presently facilities are choosing to operate at 2K even at low frequency to avoid MFQS, such as FRIB and RISP.
Some evidence for a weakening of the energy gap at high field
More data is required to explain this effect – can doping/infusion help
K. Saito – SRF2015
FRIB 80.5MHz β=0.085 QWR

## Slide 21: MULTI-FREQUENCY COAXIAL RESONATORS
Two new TEM mode coaxial resonators (QWR and HWR) are being fabricated to systemically study field dependence of RF surface resistance in low beta cavities.
Cavities sized to fit the RF induction oven – allows unique optimization of heat treatments and doping/infusion as a function of RF frequency.
Cavities can be excited at fundamental (200MHz) plus higher harmonics to allow direct comparisons of results.
Allows unique set of measurements to characterize field dependent loss mechanisms in SRF cavities.
QWR
HWR
RF field distribution of TEM modes

## Slide 22: VERTICAL EP DEVELOPMENT
Electro-polish treatment is needed for N-doping – need to remove 5micron layer after doping
TRIUMF SRF is developing vertical EP with Teflon stirrers to augment the doping effort – process being optimized
paddles

## Slide 23: NEW MATERIAL – Nb3Sn
A15 intermetallic alloy of niobium and tin.
Nb3Sn has a higher critical temperature than Niobium (18K vs 9K)
  Allows operation at 4K rather than 2K
  Big cryo. cost savings.
Nb3Sn has a higher metastable magnetic field limit than Niobium (400mT vs 200 mT)
  Could allow operation at higher gradients.
  Presently suffers from quench at moderate fields.
Parameter | Niobium | Nb3Sn
Tc | 9.2 K | 18 K
Bsh | 219 mT | 425 mT
Δ/kbTc | 1.8 | 2.2
λ at T = 0 K | 50 nm | 111 nm
ξ at T = 0 K | 22 nm | 4.2 nm
GL parameter κ | 2.3 | 26
Green: tin
Red: niobium

## Slide 24: Nb3Sn COATED ILC SINGLE CELL
Sn Vapor
Auxiliary Heater for Sn container at 1200 C
Coating chamber in UHV furnace at 1100 C
Nb cavity substrate
Bath T=4.2K
D. Hall – TTC Saclay

## Slide 25: Nb3Sn COATING AT TRIUMF
Nb3Sn coating technique can be studied at TRIUMF with RF induction oven on either samples, single cell cavities or coaxial resonators.
Applying Nb3Sn film on low beta cavities and other complicated geometry cavities can be explored.
Cornell’s results encourage to operate cavities at 4K and moderate gradient.

## Slide 26: MULTILAYER FILMS
SC / insulator / SC multilayer films (SIS) was proposed by A. Gurevich, App. Phys. Lett. 88, 012511 (2006).
Suggests that SIS layers could reach very high fields before vortex penetration.
T. Kubo – TTC Saclay

## Slide 27: Material Science Probes at TRIUMF – muSR and β-NMR*
TRIUMF has two world class material science probes in muSR and betaNMR – utilize the beta decay of a beam of polarized muons or 8Li ions respectively as probes of local magnetism
TRIUMF muSR samples near surface fields (100µm) and betaNMR samples surface fields (0->200nm)
Method
Imbedded probes decay with emitted positrons or electrons correlated with direction of spin. Spin precession dependent on the magnetic field of the imbedded probe
µ+, 8Li
Atomic lighthouse
* More from Tobi and Rob Kiefl

## Slide 28: FIELD OF FIRST FLUX ENTRY WITH muSR
Sample: Fine grain RRR niobium sample 1400°C annelead then 120° bake in vacuum and retested.
Finding: Baking at 120C in vacuum enhances the field of first flux entry from 174 mT to 188 mT.
µ
B
Dirty layer
Bulk Nb
Enhancement by 6%
Implantation depth 100µm
T. Junginger – TTC MSU

## Slide 29: FIELD OF FIRST FLUX ENTRY WITH muSR
Samples: Nb 1400°C annealed, MgB2 (50-300nm) and Nb3Sn (1-3.5µm) on niobium.
Findings: A layer of a higher Tc material on niobium can enhance the field of first entry by about 40% from a field consistent with Hc1 to a field consistent with Hsh.
This enhancement does not depend on material or thickness suggesting that superheating is indeed induced in niobium by the overlayer which is inconsistent with both models.
Intermediate state
Vortex state
Meissner state
Theoretical Bsh
Theoretical Bc1
µ
B
Coating
(50-3500 nm)
Bulk Nb
Implantation depth 100µm
T. Junginger – TTC MSU

## Slide 30: HIGH FIELD SPECTROMETER FOR beta-NMR
beta-NMR is a unique facility to characterize magnetic properties of materials at surfaces and film interfaces.
Perfect for SRF characterization of materials since it can probe the superconductor through the London layer.
muSR at TRIUMF fixed implantation depth (≈100µm) while LE-muSR at PSI limited to 25 mT parallel fields.
TRIUMF will provide a unique facility in the world for diagnosing new treatments (doping), new materials (Nb3Sn) and new structures (SIS layer) with variable implantation depth and parallel magnetic field up to 200mT.
8Li range
B
T. Kubo – TTC Saclay
H

## Slide 31
CONTRIBUTIONS ON OTHER PROJECTS

## Slide 32: SRF/RF Work for Others
RF department is engaging in Work for Others
  Maintains core competence – engages students
  Cavity testing for RISP (QWR/HWR) and PKU (single cell)
Variable couplers for FRIB and RI
LLRF systems for Cornell, RISP and IMP
Variable couplers for FRIB
RISP QWR Cavity Test

## Slide 33: SRF/RF Work for Others
SSR1 spokes + fixture
SSR1 cavity - RISP
RISP project in Korea
    Design and fabrication of two SSRs – 325MHz β=0.3
TRIUMF Machine Shop and SRF team successfully formed Nb parts for SSR1 – developing other local fabricators for brazing and spinning

## Slide 34: VECC COLLABORATION
TRIUMF has had an active collaboration with VECC Kolkata over the last seven years.
The main deliverable from the collaboration was the joint design and production of two injector modules one for TRIUMF and one for VECC (commissioned in 2016).
The latest deliverable is a new heavy ion cryomodule containing 4 QWRs for delivery to VECC – we will be starting this in 2017.

## Slide 35: RFD Cryomodule
DOE (FNAL) is supplying 8(+2) RF Dipole cavities (ODU design) to CERN for HiLumi
CERN requires 4(+1) Crabbing cryomodules
Similar size and technology as the e-Linac Accelerating Cryomodules (ACM)
Propose to design/build the CMs as part of a HiLumi hardware contribution from Canada

## Slide 36: SRF at TRIUMF
SRF department supports
  Internal projects
    ISAC-II heavy ion linac, ARIEL e-Linac,
  Student education
    Fundamental and technical SRF
  External collaborations and Work for others (FRIB, IHEP, IMP, CERN, RISP, FNAL, VECC, Cornell, JLab, Temple)