## Slide 1: Lessons learned from the US program on Nb3Sn magnets for HL LHC, applicable to future IR2 quadrupoles at the EIC
P. Ferracin
on behalf of the US LARP/AUP and CERN MQXF collaboration
EIC Accelerator Partnership Workshop 2021
October 26th, 2021
Virtual

## Slide 2: Acknowledgements
LARP and US HL-LHC Accelerator Upgrade Project (AUP)
  BNL: K. Amm, M. Anerella, A. Ben Yahia, H. Hocker, P. Joshi, J. Muratore, J. Schmalzle, H. Song, P. Wanderer
  FNAL: G. Ambrosio, G. Apollinari, M. Baldini, J. Blowers, R. Bossert, R. Carcagno, G. Chlachidze, J. DiMarco, S. Feher, S. Krave, V. Lombardo, C. Narug, A. Nobrega, V. Marinozzi, C. Orozco, T. Page M. Parker, S. Stoynev, T. Strauss, M. Turenne, D. Turrioni, A. Vouris, M. Yu
  LBNL: D. Cheng, P. Ferracin, L. Garcia Fajardo, E. Lee, M. Marchevsky, M. Naus, H. Pan, I. Pong, S. Prestemon, K. Ray, G. Sabbi, G. Vallone, X. Wang
  NHMFL: L. Cooley, J. Levitan, J. Lu, R. Walsh
CERN: HL-LHC Project
  A. Ballarino, H. Bajas, M. Bajko, B. Bordini, N. Bourcey, S. Izquierdo Bermudez, H. Felice, S. Ferradas Troitino, L. Fiscarelli, J. Fleiter, M. Guinchard, O. Housiaux, F. Lackner, F. Mangiarotti, A. Milanese, P. Moyret, J.C. Perez, H. Prin, R. Principe, E. Ravaioli, T. Sahner, S. Sequeira Tavares, E. Takala, E. Todesco

## Slide 3: Acknowledgements

## Slide 4: Acknowledgements

## Slide 5: Outline
R&D on Nb3Sn quadrupoles (LARP)
HL-LHC and MQXF (LARP/AUP and CERN)
Nb3Sn quadrupole magnets for EIC
Conclusions

## Slide 6: Overview of R&D on Nb3Sn quadrupole magnets for LHC Luminosity Upgrade
US LHC Accelerator Research Program LARP (2003-2018)
US Accelerator Upgrade Project AUP (2018-present)
CERN HL-LHC (2011-present)
MQXF
1 m, 4.2 m, and 7.15 m long
150 mm aperture

## Slide 7: Subscale quadrupole SQ
110 mm aperture
0.3 m length
Racetrack coils
Demonstrated assembly and loading procedure
Conductor characterization
  Measurements of quench propagation velocity
Validation of FE models

## Slide 8: Long Racetrack (LR)
Common-coil (dipole)
3.6 m length
Racetrack coils
First scale up of coil and structure
Coil R&D: handling, reaction & impregnation
Structure R&D: friction effects, assembly

## Slide 9: Long Racetrack (LR)
Extensive study of 3D mechanical effect in long structure with aluminum shells
First segmented al shell
  Reduction of axial strain
  More uniform coil stress

## Slide 10: Technological Quadrupoles TQ
90 mm aperture
1 m length
Double-layer, cos coils
Cos-theta coil design and fabrication process
Two support structures, same coils
  TQS (al-shell based)
  TQC (ss-collar based)
TQS
TQC

## Slide 11: Technological Quadrupoles TQ
Two mechanical structures were developed for the TQ coils and their performance was compared in a series of 15 tests
Both structures surpassed the target gradient of 200 T/m
The shell structure was selected

## Slide 12: The aluminum shell based concept
Pre-load with
  Water-pressurized Bladders
  Loading keys
  Aluminum shell
    Segmented (from LR)

## Slide 13: Long quadrupole LQ
90 mm aperture
3.5 m length
Double-layer, cos coils
LARP milestone
First scale-up of cos coils and quadrupole shell structure

## Slide 14: High field quadrupole HQ
120 mm aperture
1 m length
Double-layer, cos coils
R&D on larger aperture and “accelerator quality” features
  Full alignment of all components

## Slide 15: 3D modeling for mechanical analysis
TQS
SQ
SM
LQS
LRS
HQ

## Slide 16: Outline
R&D on Nb3Sn quadrupoles (LARP)
HL-LHC and MQXF (LARP/AUP and CERN)
Nb3Sn quadrupole magnets for EIC
Conclusions

## Slide 17: From LHC to HL-LHC
LHC operating at 6.5 TeV
In the period 4
  Peak luminosity of 21034 cm-2s-1
  Integrated luminosity of 350 fb-1
High Luminosity LHC (HL-LHC)
  Upgrade the Interaction Region in 2025-2027
  Peak luminosity of 5 to 71034 cm-2s-1  3000 fb-1
  3000 fb-1 integrated luminosity in following ~12 years

## Slide 18: HL-LHC Interaction Region
New inner triplet quadrupole
  From 70 mm aperture Nb-Ti to 150 mm aperture Nb3Sn
    Larger aperture to reduce the beam size
    Nb3Sn allows keeping a compact triplet notwithstanding the larger aperture
LHC
HiLumi LHC

## Slide 19: HL-LHC IR quadrupoles
Q1/Q3 (by US-AUP)
  2 magnets (MQXFA) per cold mass, each 4.2 m long
Q2a/Q2b (by CERN)
  1 magnet (MQXFB) per cold mass, 7.15 m long, with corrector
Different lengths, but identical design

## Slide 20: MQXF design and parameters
2-layes cos coils with 150 mm aperture
18 mm width cable
Nominal (ultimate) conditions (7 (7.5) TeV)
  1.9 K
  G = 132.2 (142.1) T/m
  I = 16.23 (17.49) kA
  B = 11.4 (12.3) T
Operational margin: 23% at Inom
Temperature margin at Inom = 5.0-5.5 K
Shell based structure
  Segmented al shell
SS shell as Lhe containment

## Slide 21: MQXF design and parameters
4 mm cold bore tube
  1.5 mm radial gap to the coil
16 mm thick tungsten absorber

## Slide 22: Short model program MQXFS

## Slide 23: Short model program MQXFS MQXFS1
CERN
FNAL
BNL
LBNL
Coils 103-104
Structure 1
Coil 3-5
Coil 3-5
MQXFS01
Analysis of test results carried out in parallel by LARP and CERN

## Slide 24: Short model program MQXFS (LARP/AUP and CERN)
6 short models tested
  All reached nominal
  5 out of 6 reached ultimate
In the last 4 short models
  Perfect memory after thermal cycle
  Able to operate above ultimate both at
    1.9 K (85%-90% of Iss )
    4.5 K (90%-95% of Iss )
No degradation observed after up to 8 thermal cycles and 1000 powering cycles

## Slide 25: MQXFA (LARP/AUP)

## Slide 26: MQXFA (LARP/AUP)
1st prototype (AP1) training stopped for electrical failure (coil to structure)
  Reassembled, it was then limited by an old coil
2nd prototype (AP2)
  Performance limited by structural failure of aluminum shell

## Slide 27: MQXFAP1-2 lessons learned
After AP1
  Clearly defined and strictly followed electrical design criteria
    Test procedures and test levels
After AP2
  Developed structural design criteria based on Failure Assessment Diagram
    Defined assembly/loading process and stress limits

## Slide 28: MQXFA (LARP/AUP)
5 series MQXFA magnets tested (not yet cold-mass)
  4 successful magnets: reached nominal
  5th limited by one coil: to be disassembled for coil replacement
16 more magnets and 10 cold masses to go

## Slide 29: MQXFB (CERN)

## Slide 30: MQXFB (CERN)
Two prototype cold-masses (BP1 and BP2) tested
  Both limited below nominal
  In both cases, quenches in one coil straight section, performance loss at 4.5 K consistent with 1.9 K behavior, reproducible after thermal cycle

## Slide 31: MQXFB Lessons learned / action items
Production on hold to review/improve
  Coil fabrication process and tooling
    To improve coil uniformity and reduce risk of conductor damage
  Review assembly process
    Reduce coil peak stress and improve pre-load uniformity
  Review of ss shell welding
    Minimize impact of shell welding on coil stress
To be implemented in MQXFA

## Slide 32: MQXF Field Quality
Overall, field quality under control
Possibility of partially correct low order non allowed harmonics with magnetic shims

## Slide 33: Overall MQXF timeline
T0: key parameters selected (aperture, cable geometry…)
To nominal / not to nominal

## Slide 34: From TQS to MQXF from R&D to accelerator quality
MQXFS
TQS

## Slide 35: Outline
R&D on Nb3Sn quadrupoles (LARP)
HL-LHC and MQXF (LARP/AUP and CERN)
Nb3Sn quadrupole magnets for EIC
Conclusions

## Slide 36: Compact Nb3Sn IR quadrupole
Limited available space
  Compact design with active shielding
New magnet design with HQ coils
  No iron yoke
Full 3D mechanical analysis, with novel axial support system
Magnet assembled and ready for test at BNL

## Slide 37: Compact Nb3Sn IR quadrupole
In scale

## Slide 38: Nb3Sn quadrupole magnets for EIC
QFFDS01A
2.9 m length
164 mm ap.
70 mm width
96 T/m grad.
QFFDS01B
3.2 m length
256 mm aperture
92 mm width
71 T/m grad.
Some preliminary considerations
  S01A relatively similar to MQXF
  Length for both demonstrated in LARP/AUP (magnets, not cold mass)
  Coil width may be reduced
  Challenges
    Very large aperture high stress on the conductor
    Compactness?

## Slide 39: Outline
R&D on Nb3Sn quadrupoles (LARP)
HL-LHC and MQXF (LARP/AUP and CERN)
Nb3Sn quadrupole magnets for EIC
Conclusions

## Slide 40: Conclusions
The LARP-AUP-CERN programs successfully demonstrated Nb3Sn quadrupole magnets
  Apertures from 90 to 150 mm
  Lengths from 1 to 4.2 m
Work in progress
  Lengths >4.2 m (7.15 m)
  Full cold masses
Very good field quality achievable
Mechanics and fabrication processes require an extremely tight control
Some possible R&D towards EIC IR
  Very compact support structures
  Very large aperture

## Slide 41: Appendix

## Slide 42: MQFXA
4.2 m length, 150 mm ap., 36 mm width, 130 T/m grad.

## Slide 43: QFFDS01A
2.9 m length, 164 mm ap., 70 mm width, 96 T/m grad.

## Slide 44: QFFDS01B
3.2 m length, 256 mm ap., 92 mm width, 71 T/m grad.