## Slide 1
Carbon coating technology
P. Costa Pinto, V. Baglin, P. Chiggiato, P. Cruikshank, S. Fiotakis, A. Granadeiro Costa, M. Himmerlich, H. Kos, N. Kos, M. Taborelli, J. Tagg
  Introduction to a-C films with low Secondary Electron Emission
    Secondary Electron Yield (SEY, d) of carbon materials
    Effect of Impurities
    Ageing in air
    Ageing
  Coating technology at CERN
    Coating techniques
    Adapt the coating technique to the constrains
    The SPS case
    The HL-LHC case
  Summary

## Slide 2
1 – Introduction to low SEE a-C films
The SEY (d) of carbon materials depend on the molecular bonds between carbon atoms.
N. REY WHETTEN JOURNAL OF APPLIED PHYSICS
VOLUME 34. NUMBER 4 (PART 1) APRIL 1963
dmax ~ 1
Graphite =>low SEY
Diamond => high SEY
dmax ~ high
JACQUES CAZAUX, Mikrochim
. Acta 132, 173±177 (2000)
Carbon thin films
low SEY
high SEY
high SEY

## Slide 3
1 – Introduction to low SEE a-C films
The effect of impurities: hydrogen is bad

## Slide 4
1 – Introduction to low SEE a-C films
The effect of impurities: hydrogen is bad nitrogen is good
1%

## Slide 5
1 – Introduction to low SEE a-C films
Ageing
3 months
In air
(wrapped in Al foil)
Al foil Hollow Cathode sputtering
Magnetron sputtering
IPAC 2011 TUPS027

## Slide 6
1 – Introduction to low SEE a-C films
Ageing
3 months
In air
(wrapped in Al foil)
1st QF coating done by magnetron sputtering

## Slide 7
2 – Coating technology at CERN
Coating techniques
Plasma
Assisted
CVD
Sputtering
PLD
Pulsed Laser Deposition
Cathodic
Arc
Thermal
CVD
Chemical Vapour deposition
Thermal evaporation
Not tested at CERN

## Slide 8
2 – Coating technology at CERN
Coating techniques
Plasma
Assisted
CVD
Sputtering
PLD
Pulsed Laser Deposition
High deposition rate and easy to scale up
SEYmax > 1.4 due to high hydrogen content from precursor gases (CH4, C2H2)
SEYmax~1 if performed at high pressure
(to quench the energy of the C atoms)
Poor adhesion on Cu
SEYmax~1
Adaptable to a wide range of geometries
Low deposition rate (sputtering yield)

## Slide 9
2 – Coating technology at CERN
Coating techniques
Plasma
Assisted
CVD
Sputtering
PLD
Pulsed Laser Deposition
High deposition rate and easy to scale up
SEYmax > 1.4 due to high hydrogen content from precursor gases (CH4, C2H2)
SEYmax~1 if performed at high pressure
(to quench the energy of the C atoms)
Poor adhesion on Cu
SEYmax~1
Adaptable to a wide range of geometries
Low deposition rate (sputtering yield)

## Slide 10
2 – Coating technology at CERN
Adapt the coating technique to the constrains
Geometry of the object to be coated: cylindrical, planar, ellipsoidal, etc.
Accessibility: tube with/without flanges; already inserted in a yoke of a magnet; in the accelerator tunnel;
Adhesion: substrate material, surface treatments, bakeout before coating?
Residual gas during coating: outgassing / pumping (materials; bakeout before coating? thermal treatments)
Schedule & budget
Whenever possible, integrate the coating process from the design phase.

## Slide 11
2 – Coating technology at CERN
The SPS case
Drift chambers
ID 159 mm
Keep quads and dipoles in the ring => coat in-situ
Beam pipes with different geometries:
Quad and dipole chambers are embedded in the yoke. (bakeout not possible)
Quad chambers
Ellipsoid
Dipole chambers
racetrack
Quad chambers
ID 80 mm

## Slide 12
2 – Coating technology at CERN
The SPS case
Drift chambers
ID 159 mm
Beam pipes with different geometries:
Coat ex-situ by DC cylindrical Magnetron sputtering (solenoid)
Graphite rod
(OD 14 mm)
B supplied
by a
solenoid
Bakeout before coating (24@150 oC)
Pressure Ar ~4x10-2 mbar
Power density ~ 200 W / meter of target
Sputtering rate ~ 12 nm / hour

## Slide 13
2 – Coating technology at CERN
The SPS case
Drift chambers
ID 159 mm
Beam pipes with different geometries:
Graphite rod
(OD 14 mm)
B supplied
by a
solenoid
Coat ex-situ by DC cylindrical Magnetron sputtering (solenoid)

## Slide 14
2 – Coating technology at CERN
The SPS case
Drift chambers
ID 159 mm
Beam pipes with different geometries:
Graphite rod
(OD 14 mm)
B supplied
by a
solenoid
Chart: Evolution of SEYmax along the LS2 production
| 21/09/2018 | 04/10/2018 | 15/10/2018 | 05/11/2018 | 07/11/2018 | 15/04/2019 | 06/05/2019 | 08/05/2019 | 25/11/2019 | 17/12/2019 | 13/11/2019 | 17/11/2019 | 16/03/2020 | 16/03/2020 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14
SEY | 1.02 | 1.01 | 1.07 | 1.02 | 1.01 | 1.01 | 1.01 | 1.01 | 0.98 | 0.97 | 0.97 | 0.96 | 0.92 | 0.9
Add NEG pumping for H2
NEG target (flashes)
Coat ex-situ by DC cylindrical Magnetron sputtering (solenoid)

## Slide 15
2 – Coating technology at CERN
The SPS case
QF quads
Quad chambers
Ellipsoid
Coat in-situ by
DC hollow cathode
sputtering
Dipole chambers
racetrack
MBB dipoles

## Slide 16
2 – Coating technology at CERN
The SPS case
QF quads
Quad chambers
Ellipsoid
Dipole chambers
racetrack
Coat in-situ by
DC hollow cathode
sputtering
MBB dipoles

## Slide 17
2 – Coating technology at CERN
The SPS case
QF quads
Quad chambers
Ellipsoid
Dipole chambers
racetrack
MBB dipoles
No bakeout before coating
Pressure Ar ~1.1x10-1 mbar
Power density ~ 120 W / m
Sputtering rate ~ 20 nm / hour
20 hours -> 400 nm films
Coat in-situ by
DC hollow cathode
sputtering

## Slide 18
2 – Coating technology at CERN
The SPS case
QD quads
Coat by DC pulsed cylindrical magnetron sputtering (with LHC technology)
Quad chambers
ID 80 mm

## Slide 19
2 – Coating technology at CERN
The SPS case
The first large scale production in the SPS during the CERN Long Shutdown (212 coating runs):
88 QF quadrupole magnets (294 m) coated in-situ 2 runs / week with 2 systems
110 Short straight Section elements (104 m) coated ex-situ 2 runs / week with 2 systems
29 Drift vacuum chamber (80 m) coated ex-situ 2 runs / week with 2 systems
Chart: Histogram of the SEYmax for the whole LS2 coating campaign
| 0.9 | 0.91 | 0.92 | 0.93 | 0.94 | 0.95 | 0.96 | 0.97 | 0.98 | 0.99 | 1 | 1.01 | 1.02 | 1.03 | 1.04 | 1.05 | 1.06 | 1.07 | 1.08 | 1.0900000000000001 | 1.1000000000000001
number of runs | 1 | 1 | 3 | 0 | 0 | 6 | 17 | 19 | 24 | 29 | 32 | 29 | 11 | 10 | 7 | 4 | 0 | 1 | 0 | 0 | 1

## Slide 20
2 – Coating technology at CERN
The HL-LHC case
In-situ coatings
(inner triplets ALICE and LHCb)
Ex-situ coatings
(New inner triplets ATLAS and CMS)

## Slide 21
2 – Coating technology at CERN
The HL-LHC case
In-situ coatings
(inner triplets ALICE and LHCb)
Only 150 mm to insert the coating device => modular sputtering source
High outgassing of H2O and H2 => Ti gettering

## Slide 22
2 – Coating technology at CERN
The HL-LHC case
In-situ coatings
(inner triplets ALICE and LHCb)
Only 150 mm to insert the coating device => modular sputtering source
High outgassing of H2O and H2 => Ti gettering

## Slide 23
2 – Coating technology at CERN
The HL-LHC case
In-situ coatings
(inner triplets ALICE and LHCb)
Only 150 mm to insert the coating device => modular sputtering source
High outgassing of H2O and H2 => Ti gettering
Pulled by cables
along the beam screen
Cu substrate => critical for adhesion => ion etching + Ti underlayer

## Slide 24
2 – Coating technology at CERN
The HL-LHC case
In-situ coatings
(inner triplets ALICE and LHCb)
Only 150 mm to insert the coating device => modular sputtering source
High outgassing of H2O and H2 => Ti gettering
Pulled by cables
along the beam screen
Cu substrate => critical for adhesion => ion etching + Ti underlayer
Stainless steel (~ 1.5 mm)
OFE Cu (~80 mm)
CuO, Cu2O, Cu(OH)2
Ar+ ~500 eV
Beam screen
Oxide layer

## Slide 25
2 – Coating technology at CERN
The HL-LHC case
In-situ coatings
(inner triplets ALICE and LHCb)
Only 150 mm to insert the coating device => modular sputtering source
High outgassing of H2O and H2 => Ti gettering
Cu substrate => critical for adhesion => ion etching + Ti underlayer
Stainless steel (~ 1.5 mm)
OFE Cu (~80 mm)
Cu2O
Vent to 80% N2 + 20% O2 (“dry air”)
Beam screen
Oxide layer without
copper hydroxide

## Slide 26
2 – Coating technology at CERN
The HL-LHC case
In-situ coatings
(inner triplets ALICE and LHCb)
Only 150 mm to insert the coating device => modular sputtering source
High outgassing of H2O and H2 => Ti gettering
Cu substrate => critical for adhesion => ion etching + Ti underlayer

## Slide 27
2 – Coating technology at CERN
The HL-LHC case
In-situ coatings
(inner triplets ALICE and LHCb)
Only 150 mm to insert the coating device => modular sputtering source
High outgassing of H2O and H2 => Ti gettering
Cu substrate => critical for adhesion => ion etching + Ti underlayer
3 weeks to coat a 14 m long quad => several systems in parallel

## Slide 28
2 – Coating technology at CERN
The HL-LHC case
In-situ coatings
(inner triplets ALICE and LHCb)

## Slide 29
2 – Coating technology at CERN
The HL-LHC case
Ex-situ coatings
(New inner triplets ATLAS and CMS)
=> Adapt the in-situ technology to the new geometry

## Slide 30
2 – Coating technology at CERN
The HL-LHC case
Ex-situ coatings
(New inner triplets ATLAS and CMS)
=> Adapt the in-situ technology to the new geometry

## Slide 31
2 – Coating technology at CERN
The HL-LHC case
Ex-situ coatings
(New inner triplets ATLAS and CMS)
=> Adapt the in-situ technology to the new geometry

## Slide 32
2 – Coating technology at CERN
The HL-LHC case
Ex-situ coatings
(New inner triplets ATLAS and CMS)
=> Adapt the in-situ technology to the new geometry

## Slide 33
2 – Coating technology at CERN
The HL-LHC case
Ex-situ coatings
(New inner triplets ATLAS and CMS)
=> Adapt the in-situ technology to the new geometry

## Slide 34
2 – Coating technology at CERN
The HL-LHC case
Ex-situ coatings
(New inner triplets ATLAS and CMS)
=> Adapt the in-situ technology to the new geometry

## Slide 35
2 – Coating technology at CERN
The HL-LHC case
Ex-situ coatings
(New inner triplets ATLAS and CMS)
=> Adapt the in-situ technology to the new geometry
The a-C film resisted to the deformations induced by quenching at nominal currents.
Tests at 4x nominal current ongoing.

## Slide 36
2 – Coating technology at CERN
The HL-LHC case
Optical inspection devices (before / after coating)
Raspbery Pi camera + motherboard + battery + LED based light system

## Slide 37
3 – Summary
The coating technique to produce carbon films with low SEY must favor sp2 hybridization (sputtering, PLD). SEY increases with H content and decreases with N content.
A growing technological corpus is available to cope with the constrains of the particle accelerator’s community: in-situ / ex-situ; getter co-deposition; N doping; re-set of copper oxide; optical inspection devices…
Large scale production is feasible: more than 200 coating runs during the LS2 coating campaign in the SPS resulted on a average SEY ~1. (in-situ + ex-situ coatings). More to come during LHC run 3 (ex-situ) and LS3 (in-situ).
No pre-defined recipe: the coating technique & process should be adapted to each specific case. Take into account the coating from the design phase is the bet practice.

## Slide 38
Thank you for your attention