## Slide 1: Electromagnetic characterization of coatings for accelerators
26/10/2021
TRIUMF 2021 EIC Accelerator Partnership Workshop
Andrea
Passarelli
Can
Koral
Maria Rosaria
Masullo
Antonello
Andreone*
University of Naples Federico II -Italy
Maria
De Stefano*

## Slide 2
Coatings and resistive wall impedance
Electromagnetic characterization of “coating materials” is fundamental to evaluate accelerator performance limitations and build up a machine impedance model.
Surface impedance of the beam pipe depends on electromagnetic properties of coatings.
Coatings required (as examples) for reducing surface degassing or for secondary electron yield mitigation…but layers of coating materials significantly increase the resistive wall impedance
Low conductivity, thin layer coatings (NEG, a‐C)
Rough surfaces (LESS)

## Slide 3: Two different methods
Electromagnetic characterization of Coating materials
Dielectric resonator
• high sensitivity
Sub-THz waveguide
• small skin-depth
LESS(Laser engineered surface structures)
• conductivity compared with copper
• small samples (10x10mm)
NEG(Non-Evaporable Getter)
• homogeneous coating
a-C (Amorphous carbon)
• coating thickness issues

## Slide 4: Sub-THz waveguide attenuation: the proposed method
Evaluation of the signal attenuation inside a DUT with coating deposited.
Electromagnetic characterization
of coating materials.
Sub-THz transmission methodology

## Slide 5: The DUT
Material | Iron
Waveguide | Circular
Length | 42
Radius | 0.9
Horns | Pyramidal
Length | 39
External side | 6
Total Length | 120
Dimension in mm

## Slide 6: The Device Under Test
Methodology advantages: 1)Homogeneous deposition, 2)System reusability, 3)Large area coating
Copper foil
as
reference
Coated foil
to measure
2
1
3
5
4
6

## Slide 7: Analytical evaluations
In-house retrieval method
Waveguide of length lg (TE1,1 mode) + pyramidal transitions of length lt (TE1,0 TE0,1 modes)
Reliable analytical tool
For calculations
Copper conductivity: σcu = 6∙107 S/m
NEG conductivity: σNEG = 3.5∙105 S/m
Surface impedance
Z and k are functions of material conductivity

## Slide 8: Measurement results on NEG
System specifications:
Spectral Range: > 5 THz
Dynamic Range > 90 dB
Scanning Range ~ 850 ps
Spectral Resolution < 1.5 GHz
Accurate guiding system manufacturing
NEG thickness 3.96 micron
The methodology allows us to directly evaluate the Re(Zs ) that we can use in beam dynamics calculations
From surface impedance Zs to resistive wall impedance Zwall

## Slide 9: Measurement results on a-C
3 μm of Amorphous carbon on copper bulk
Mechanical stress a-C coating on Cu slab

## Slide 10
Dielectric resonant cavity

## Slide 11: Resonant structure methodology
Dielectric resonator: Resonant structure methodology improves the sensitivity
for the electromagnetic characterization of very thin laser surface treated
structures and conductivity close to copper one
CU coated DUT
Sapphire
Hollow
holder
E field distribution
TE011 mode

## Slide 12: Resonant structure methodology-simulations
Chart: ∆h (mm)
| 4 | 3.5 | 3 | 2.5 | 2 | 1.5 | 1 | 0.5 | 0
R=2.6mm | 2.7686 | 3.3688 | 4.1233 | 5.0988 | 6.3938 | 7.9627 | 9.6127 | 10.1647 | 7.8725
R=3.5mm | 2.1398 | 3.1265 | 4.2171 | 5.3535 | 7.7865 | 10.0835 | 14.2018 | 17.5692 | 20.5376
Copper vs. molybdenum coated DUT
The maximum Q-factor percentage difference is obtained
with a minimum distance between the DUT and the sapphire
sapphire
radius
Δh

## Slide 13: Resonant structure methodology- simulations
The sapphire with
larger radius (3.5 mm)
will be used, because
of its higher sensitivity
in EM characterization
of coating materials
(LESS)
Expected LESS

## Slide 14: Conclusion
Electromagnetic characterization of coating materials
Sub-THz waveguide attenuation
  Reliable analytical model for the conductivity retrieval. Good agreement with CST solver.
  Successful measurement campaign: reliable and handy method to evaluate the electromagnetic properties of samples under test.
  Published results on NEG and novels on a-C coatings.
Resonant structure methodology
  Improves the sensitivity, useful for electromagnetic characterization of very thin laser surface treated structures (i.e. LESS)