## Slide 1
Studying LaNiO3 and LaNiO3/LaAlO3 superlattices using 8Li β-detected NMR
Victoria Louise Karner

## Slide 2
The metal-insulator transition in rare-earth nickelates (RNiO3)
2
only metal!

## Slide 3: Goal: Study the change in the metallic state of LaNiO3 between the bulk and ultrathin layers in superlattices
3

## Slide 4
What is β-detected NMR?
4
UHV
Sample
B0
β-

## Slide 5
What is β-detected NMR?
Uses implanted β-decaying radioisotopes
The ions are spin polarized (magnetized) prior to implantation in sample
Detection is possible due to the anisotropy of β-decay
5

## Slide 6
LaNiO3 Samples
6
Single Crystal
J. Mitchell (ANL)
38 nm PLD Film on LSAT
G. Cristiani (MPI-FKF)
8 mm
A.V. Boris, et al. Science 332, 937 (2011)

## Slide 7
Excellent agreement between single crystal and film
7
Biexponential relaxation is surprising!

## Slide 8
Summary of bulk LaNiO3
8
Biexponential relaxation:
  intrinsic to LaNiO3
  two different hyperfine couplings to 8Li
Linear SLR:
  conventional metallic state

## Slide 9
wide band gap insulator
Structure of the LaNiO3/LaAlO3 superlattices
9
LNO lattice constant ≈ 3.75 Å
Notes: The goal of the experiments was to address the question: “How does the correlated metallic state in LaNiO3 become unstable as we approach the 2D limit?”
To this end, we studied a variety of LaNiO3/LaAlO3 superlattices with varying LaNiO3 thicknesses.

## Slide 10
Different Temperature Dependences!
Suggests microscopic electronic phase separation
10
Where is the metal-insulator transition?
Notes: Remember to start by addressing some basic trends in the data. Such as:
Slow:
  Remains linear, i.e., metallic.
  Not too different from the bulk.
Fast:
  No longer linear
  Strongly enhanced compared to the bulk

## Slide 11
Phase separation is unique:
Static on our timescale
Persists to 300 K
Observed in all samples, even bulk
11
Biexponential relaxation suggests phase separation
Notes: Our data therefore suggests that LaNiO3 must have microscopic electronic phase separation.
This phase separation is very unique.
1. It is static on our timescale.
2. It persists up to at least 300 K.
3. And we find it in all measured LaNiO3 samples.
Unfortunately, we cannot comment on its spatial structure since we are using a local probe; however, it is most likely nanoscopic.

## Slide 12
In the bulk:
  linear SLR indicates conventional metallic state
In the SLs:
  slow component is linear even in the n = 2 SL
  fast component is more complex
Biexponential relaxation:
  intrinsic to LaNiO3
  suggests microscopic phase separation
Summary
12

## Slide 13
β-NMR group at UBC/SBQMI:
  A. Chatzichristos
  M.H. Dehn
  D. Fujimoto
  R.F. Kiefl
  W.A. MacFarlane
  R.M.L. McFadden
  J.O. Ticknor
TRIUMF:
  C.P. Levy
  R. Li
  I. McKenzie
  G.D. Morris
  M.R. Pearson
  M. Stachura
MPI-FKF:
  E. Benckiser
  A.V. Boris
  G. Cristiani
  B. Keimer
  G. Logvenov
  F. Wrobel
Argonne National Labs:
  J. Zhang
  J.F. Mitchell
13
Acknowledgements

## Slide 14: Thank you!