## Slide 1: Functionalized Detectors for Superheavy Element Homolog Chemistry Experiments
Amelia S. Kirkland
Texas A&M University
08.22.2024
NN2024

## Slide 2: Superheavy Elements
Transactinide Elements (Z ≥ 104)
Short half-lives, low production cross sections
Single-atom-at-a-time chemistry
A. Yakushev et al., First Study on Nihonium (Nh, Element 113) Chemistry at TASCA, Front. Chem. 9 (2021). doi:10.3389/fchem.2021.753738

## Slide 3: Lighter Homologs
Lighter homologs of elements can serve as models for superheavy element reactivity
Ideal lighter homologs have similar half-life and decay properties, but higher production rates
Previous work in the group focuses on Ir and Rh as homolog of Mt
This work focuses on Po as a homolog of Lv
A. Yakushev et al., First Study on Nihonium (Nh, Element 113) Chemistry at TASCA, Front. Chem. 9 (2021). doi:10.3389/fchem.2021.753738

## Slide 4: Self-Assembled Monolayer
Physisorption
Lying-down Phase Formation
Nucleation of the Standing-up Phase
Completion of the Standing-up Phase
C. Vericat et al., Self-assembled monolayers of thiols and dithiols on gold: new challenges for a well-known system, Chem. Soc. Rev. 39, 1805-1834 (2010). doi:10.1039/B907301A
H. Hamoudi et al., On the self assembly of short chain alkanedithiols, Phys. Chem. Chem. Phys. 10, 6836-6841 (2008). doi:10.1039/B809760G

## Slide 5: Functionalized Detectors
He Flow
Not to Scale
Atom
SAMs
Au
Ti
Si

## Slide 6: Functionalized Detectors
He Flow
Not to Scale
Atom
SAMs
Au
Ti
Si

## Slide 7: Chemically Tunable Detector Surfaces
Previous work in the group studied interactions of Ir, At, and Er on two different SAMs surfaces
Rh adsorption from solution with imidazole-based SAMs was 81.3 ± 3.8%
Ir adsorption from solution with imidazole-based SAMS was 77 ± 12%
V. Zakusilova et al., Characterization and application of alkanethiolate self-assembled monolayers on Au-Coated chips for Ir(IV) and Rh(III) sorption, Applied Surface Science 642, 158356 (2024). doi:10.1016/j.apsusc.2023.158356

## Slide 8: Chemically Tunable Detector Surfaces
V. Zakusilova et al., in preparation (2024).

## Slide 9: Chemically Tunable Detector Surfaces
118Sn(40Ar, xn)158-xEr
165Ho(40Ar, xn)205-xAt
141Pr(40Ar, xn)181-xIr
176Ir α-branching ratios are both low
V. Zakusilova et al., in preparation (2024).

## Slide 10: Functionalized Detectors
Large-area Si PIN photodiode for direct radiation detection, retrieved 2/7/2022, available at https://www.hamamatsu.com/jp/en/product/optical-sensors/photodiodes/si-photodiodes/S14605.html.
C. Vericat et al., Self-assembled monolayers of thiols and dithiols on gold: new challenges for a well-known system, Chem. Soc. Rev. 39, 1805-1834 (2010). doi:10.1039/B907301A
H. Hamoudi et al., On the self assembly of short chain alkanedithiols, Phys. Chem. Chem. Phys. 10, 6836-6841 (2008). doi:10.1039/B809760G

## Slide 11: Characterization of Monolayer
What is the surface roughness?
What is the coverage of the monolayer?
How long does the monolayer last?
How thick is the monolayer?
Spectroscopic Ellipsometry
Nano-projectile Secondary Ion Mass Spectrometry
X-ray Photoelectron Spectroscopy
Atomic Force Microscopy
V. Zakusilova et al., Characterization and application of alkanethiolate self-assembled monolayers on Au-Coated chips for Ir(IV) and Rh(III) sorption, Applied Surface Science 642, 158356 (2024). doi:10.1016/j.apsusc.2023.158356

## Slide 12: Characterization of Monolayer
What is the surface roughness?
What is the coverage of the monolayer?
How long does the monolayer last?
How thick is the monolayer?
Nano-projectile Secondary Ion Mass Spectrometry
The coverage was measured to be 83 ± 15 %
X-ray Photoelectron Spectroscopy
Studies ongoing
Spectroscopic Ellipsometry
Measured thickness is 1.56 ± 0.017 nm
Spectroscopic Ellipsometry
Nano-projectile Secondary Ion Mass Spectrometry
X-ray Photoelectron Spectroscopy
Atomic Force Microscopy
Atomic Force Microscopy
Bare Au has a surface roughness of 1.17 nm
NDT on Au has a surface roughness of 0.983 nm
V. Zakusilova et al., Characterization and application of alkanethiolate self-assembled monolayers on Au-Coated chips for Ir(IV) and Rh(III) sorption, Applied Surface Science 642, 158356 (2024). doi:10.1016/j.apsusc.2023.158356

## Slide 13: Recoil Transfer Chamber (RTC)
M. C. Alfonso et al., New recoil transfer chamber for thermalization of heavy ions produced in fusion-evaporation reactions, Nucl. Instrum. Methods Phys. Res., Sect. A 798, 52-61 (2015). doi:10.1016/j.nima.2015.07.004
Detector array design at the end of the RTC

## Slide 14: 216Po Extraction with RTC
Preliminary Data

## Slide 15: Al Ghiorso’s Gas-filled Ion Equipment (AGGIE) and the sRTC
AGGIE is a DvQhDy type separator
AGGIE is operated at 0.5 torr He to equilibrate charge states
sRTC used to thermalize evaporation residues once they have been separated from the beam
Detector array will be present in the sRTC

## Slide 16: Nuclear Reaction Based Po Production
Preliminary Data

## Slide 17: Thank you for your attention!
Many thanks to:
Anna M. Bukowski, Robert Eichler, Jenna R. Garcia, Isaac W. Haynes, Jordan A. Mildon, Patrick Steinegger, Evgeny E. Tereshatov, Georg Tiebel, Vira Zakusilova, and Charles M. Folden III
SNF Award No. 204701020001
Award No. DE-FG02-93ER40773

## Slide 18: Supporting Information

## Slide 19: Energy Loss of Alpha Particles in SAMS and Au
Isotope | Eα (keV) | Eloss 50 nm Au (keV) | Eloss 1 nm SAMs (keV)
196Po | 6521.9 | 20.2 | 0.068
216Po | 6778.3 | 19.7 | 0.065

## Slide 20: Superheavy Elements

## Slide 21: Fusion-evaporation Reaction
Projectile
Target
Di-nuclear System
Compound Nucleus
Evaporation Residue
D. A. Mayorov, Doctor of Philosophy, Synthesis of Shell-Stabilized Nuclides in Fusion-Evaporation Reactions Induced by 48Ca, 50Tl, or 54Cr Projectiles, Thesis, Texas A&M University (2015).
Proposed Nuclear Reactions
40Ar + 162Dy  196Po + 6n

## Slide 22: Chemistry Experiments of Superheavy Elements
C. E. Düllmann et al., Chemical investigation of hassium (element 108), Nature 418, p. 859-862 (2002). doi:10.1038/nature00980
Growing need to further functionalize detector surfaces

## Slide 23: sRTC

## Slide 24: Decay Properties and Production Methods of Livermorium and Polonium
Methods of Livermorium Production
Heavy-ion induced fusion-evaporation reactions
Methods of Polonium Production
Naturally through the decay chains of 238U and 232Th
Neutron irradiation of Bi in a reactor
Fusion-evaporation reactions
Element | Isotope | Half-Life | Decay Modes (Intensity)
Livermorium | 289Lv | – | –
 | 290Lv | 15 ms | α (100%)
 | 291Lv | 6.3 ms | α (100%)
 | 292Lv | 18 ms | α (100%)
 | 293Lv | 53 ms | α (100%)
Polonium | 196Po | 5.8 s | α (98%) ε (2.00%)
 | 216Po | 0.145 s | α (100%)
Data from NuDat 3.0

## Slide 25: Decay Properties and Production Methods of Polonium
Methods of Polonium Production
Naturally through the decay chain of 228Th
Fusion-evaporation reactions
  162Dy(40Ar, xn)202-xPo
  160Dy(40Ar, xn)200-xPo
  162Dy(36Ar, xn)198-xPo
Production Mode | Isotope | Half-Life | Decay Modes
228Th decay | 216Po | 0.145 s | α (100%)
Fusion-Evaporation | 198Po | 1.760 min | α (57%) ε (43%)
Fusion-Evaporation | 197Po | 84 s | ε (56%) α (44%)
Fusion-Evaporation | 196Po | 5.8 s | α (98%) ε (2.00%)
Fusion-Evaporation | 195Po | 4.64 s | α (94%) ε (4.00%)
Fusion-Evaporation | 194Po | 0.392 s | α (100%)
Data from NuDat 3.0

## Slide 26: Fusion Evaporation Reaction
Projectile
Target
Di-nuclear System
Quasi-fission
Compound Nucleus
Fusion-Fission
Evaporation Residue
σcap
PCN
Wxn
D. A. Mayorov, Doctor of Philosophy, Synthesis of Shell-Stabilized Nuclides in Fusion-Evaporation Reactions Induced by 48Ca, 50Tl, or 54Cr Projectiles, Thesis, Texas A&M Univeristy (2015).

## Slide 27: HIVAP Excitation Functions
165Ho(35Cl, 4n)196Po
162Dy(40Ar, 6n)196Po
Two reactions that have not been published in the literature

## Slide 28: Thiol Functional Group
Choice of monolayer: 1,9-nonanedithiol
Acid-base interactions
~ 1 nm in thickness
Challenging assembly process
H. Hamoudi, Z. Guo, M. Prato, C. Dablemont, W. Q. Zheng, B. Bourguignon, M. Canepa, and V. A. Esaulov, On the self assembly of short chain alkanedithiols, Phys. Chem. Chem. Phys. 10, p. 6836-6841 (2008). doi:10.1039/B809760G

## Slide 29: Polonium Adsorption on Metallic Surfaces Under Different Gas Atmospheres
E. A. Maugeri, J. Neuhausen, R. Eichler, R. Dressler, K. Rijpstra, S. Cottenier, D. Piguet, A. Vogele, and D. Schumann, Adsorption of volatile polonium and bismuth species on metals in various gas atmospheres: Part I - Adsorption of volatile polonium and bismuth on gold, Radiochim. Acta 104, p. 757-767 (2016). doi:10.1515/ract-2016-2573

## Slide 30: Polonium Adsorption Literature- Cyanex
Cyanex-301
Cyanex-302
Cyanex-272
M. Johansson, R. Malmbeck, B. Wierczinski, and G. Skarnemark, Extraction of polonium from aqueous alpha-hydroxyisobutyric acid solutions using dioctyl sulphide, Cyanex 272, Cyanex 301 or Cyanex 302 in toluene, J. Radioanal. Nucl. Chem. 250, p. 437-443 (2001). doi:10.1023/A:1017932602308

## Slide 31: 228Th Decay and Big RTC

## Slide 32: “Big” Recoil Transfer Chamber (RTC) Schematic
M. C. Alfonso, E. E. Tereshatov, M. J. DeVanzo, J. A. Sefcik, M. E. Bennett, D. A. Mayorov, T. A. Werke, and C. M. Folden III, New recoil transfer chamber for thermalization of heavy ions produced in fusion-evaporation reactions, Nucl Instrum Meth A 798, p. 52-61 (2015). doi:10.1016/j.nima.2015.07.004

## Slide 33: 228Th Decay Scheme
228Th
t1/2: 1.9 Y
224Ra
t1/2: 3.6 d
220Rn
t1/2: 55 s
216Po
t1/2: 0.14 s
212Pb
t1/2: 10.6 h
212Bi
t1/2: 60.6 min
212Po
t1/2: 294 ns
208Pb
Stable
208Tl
t1/2: 3.1 min
Neutron Number
Proton Number
α
α
α
α
α
α
β-
β-
β-
Data from NuDat 3.0

## Slide 34: Alpha Energies in 228Th Spectrum
Isotope | Alpha Energy (keV) | Intensity (%)
228Th | 5423.15 | 73.4
 | 5340.36 | 26.0
224Ra | 5685.37 | 94.92
 | 5448.6 | 5.06
220Rn | 6288.08 | 99.886
216Po | 6778.3 | 99.9981
212Bi | 6050.78 | 25.13
 | 6089.88 | 9.75
212Po | 8784.86 | 100
Data from NuDat 3.0
All alpha energies with a intensity <1% were omitted

## Slide 35: AC Detector 228Th Spectrum
Preliminary Data
216Po
212Po
220Rn
212Bi
224Ra
228Th
216Po

## Slide 36: Comparison of Full RTC Settings and No RTC Settings
Electrode Status | Gas Pressure Status | 228Th Count Rate (s-1) | 224Ra Count Rate (s-1) | 220Rn Count Rate (s-1) | 216Po Count Rate (s-1) | 212Bi Count Rate (s-1) | 212Po Count Rate (s-1)
On | On | 0.11 ± 0.01 | 0.86 ± 0.04 | 2.65 ± 0.07 | 91.80 ± 0.39 | 1.31 ± 0.05 | 0.54 ± 0.03
Off | Off | 0.27 ± 0.003 | 1.74 ± 0.01 | 1.23 ± 0.01 | 1.32 ± 0.01 | 3.60 ± 0.01 | 4.46 ± 0.01
Preliminary Data

## Slide 37: Self-Assembled Monolayers

## Slide 38: Self-Assembled Monolayer
4 Major Components
Surface Metal
Head Group
Alkyl Chain
Terminal Group
C. Vericat, M. E. Vela, G. Benitez, P. Carro, and R. C. Salvarezza, Self-assembled monolayers of thiols and dithiols on gold: new challenges for a well-known system, Chem. Soc. Rev. 39, p. 1805-1834 (2010). doi:10.1039/B907301A

## Slide 39: X-ray Photoelectron Spectroscopy

## Slide 40: Atomic Force Microscopy
Typical configuration of an AFM. (1): Cantilever, (2): Support for cantilever, (3): Piezoelectric element (to oscillate cantilever at its eigen frequency), (4): Tip (Fixed to open end of a cantilever, acts as the probe), (5): Detector of deflection and motion of the cantilever, (6): Sample to be measured by AFM, (7): xyz drive, (moves sample (6) and stage (8) in x, y, and z directions with respect to a tip apex (4)), and (8): Stage.
https://en.wikipedia.org/wiki/Atomic_force_microscopy

## Slide 41: Nano-projectile Secondary Ion Mass Spectrometry

## Slide 42: NP-SIMS
To measure the coverage of SAMs, the Surface Analysis and Mapping of Projectile Impacts (SAMPI) software can be used
A characteristic par of Au-S cluster ions are chosen (Au2S- and Au3S-) are selected to perform calculations.
A total spectrum with all detected ions per impact can be measured
Au3S- is chosen to form a coincidence spectrum, to see all ions that are co-emitted with it.
The total yield of Au2S- and the yield of it in the coincidence spectrum can be calculated using SAMPI, and the surface coverage can be calculated from these yields

## Slide 43: Spectroscopic Ellipsometry
“Ellipsometry measures a change in polarization as light reflects or transmits from a material structure. The polarization change is represented as an amplitude ratio, Ψ, and the phase difference, Δ. The measured response depends on optical properties and thickness of individual materials.”
https://www.jawoollam.com/resources/ellipsometry-tutorial/what-is-ellipsometry