## Slide 1: Engineering of small grain size and porous Th-based targets for ISOL@MYRRHA
Lisa Gubbels – 22/10/2025

## Slide 2: Why are we interested in a Th-based target ?
Introduction
Recommended cross sections with estimated uncertainties for the 232Th(p,x)225Ac reaction
Medical isotopes of interest for ISOL@MYRRHA:
225Ac for TAT
Kratochwil, JNM 2016, 57 (12) 1941-1944
ISC: Public

## Slide 3: Design of a ThO2 and a ThCx target material
Properties | ThO2 | ThCx
Handling Safety | 🤲 Safe to handle | 💣 Pyrophoric (requires careful handling)1
Chemical Reactivity | 😇 Chemically stable | 🧪 May react with ²²⁵Ac
Thermal Conductivity | ⛰️ Low (~2–5 W/m·K at 2000 °C) | 🌋 High (~15–30 W/m·K depending on carbon content)2, 3, 4
Impact on Target Design | 🫖 Poor heat dissipation can lead to hot spots and sintering | 🧽 Better heat management, helps preserve porosity2, 3, 4
Temperature Uniformity | 🧊 Less uniform, risk of localized overheating | 🌡️ More uniform, supports stable operation2, 3, 4
Sintering Behavior | 🪨Rapid densification above 1700 °C | 🧽 Sintering hindered by excess carbon2, 3, 4
Porosity Retention at High T | 😔 Loses porosity due to sintering | 🏆 Retains porosity at >2000 °C2, 3, 4
Introduction
1 Corradetti, S., et al. (2021)Sc. Re. 11(1): 9058.
2 Hagebø, E., et al. (1992). Nuc. Ins. and Me.70(1-4): 165–174.
3 Ravn, H., et al. (1975). Nuc. Ins. and Me. 123(1): 131–144.
4 Ravn, H. L., et al. (1987). Nuc. Ins. and Me.26(1): 183–189.
5Johnson, PhD Thesis: KU Leuven; 2024.
ThO₂ remains highly attractive because of its higher release efficiency both from a bulk target and from a coating of actinium on the surface of a material5
ISC: Public

## Slide 4: Target material development is a balancing act
Stable > 2000°C for 1 – 4 weeks
Open porosity of >50 %²
Mechanical stability of the pellet to high power
Tailored pore size: No closed pores
Optimized target material for isotope release which is mechanically stable for handling
Introduction
Small grain size
< 10 µm²
Hypothetical requirements put forwards from literature research
²Guillot, J., et al. (2019). Nuc Inst and Me, 440: 1–10.
For refractory isotope release:
Main goal
General ISOL target
ISC: Public

## Slide 5
Tailoring ThO2 target material through morphology changes
ThO2 material with different morphologies
ThO2
93-98 % TD after 10h for all of the powder morphologies
1
2
3
4
1 µm
1 µm
1 µm
1 µm
1
2
3
4
L.Gubbels (2025), J. Nucl. Mater. submitted
1 and 2 are platelets of different dimensions, 3 cubic particle and 4 nanoparticles
Material | 1 | 2 | 3 | 4
Bulk density (%TD) | 76.0±1.0 | 87.0±2.0 | 89.0±1.4 | 93.0±1.0
% Closed porosity | 3.0±1.1 | 4.0±2.0 | 3.0±1.5 | 4.0±1.0
% Open porosity | 21.0±1.1 | 9.0±2.0 | 7.0±1.5 | 3.0±1.0
Results from 76-93 % TD after 1h at 1750°C in reductive atmosphere for all of the powder morphologies:
After 10 h at 1750°C in -420 kJ/mol reductive atmosphere:
ISC: Public

## Slide 6: Mixing ThO2 with pore formers
10 µm
2 µm
2 µm
2
1
(3) A.Cordero, L.Gubbels, F.Jutier, et al., Tuning of ThO2 target materials towards highly porous structure to produce medical radioisotopes, Master Thesis, 2024
Garnica, Macias et al. 2020
Pawar, Kang et al. 2016
Ammonium bicarbonate (AB)1
Nylon (NY)³
Graphitic carbon nitride (GCN)2
2 µm
400 µm
2 µm
ThO2 starting powders of different morphologies precipitated from heterogeneous oxalate precipitation (RT and 70°C)
Pore formers used:
ThO2
Volume ratio of the mixture |  |  | 
ThO2 | AB | NY | GCN
25% |  | 75% | 
50% |  |  | 50%
33% | 33% |  | 33%
25% | 25% | 50% | 
50% | 20% | 10% | 20%
Tested on surrogate material³
Surrogate material study presented in poster ID 71
ISC: Public

## Slide 7: Results after heat treatment 1750°C for 1h
Oxalate precipitation based ThO2 pellets with O2 after 1h at 1750°C
ThO2
Pore formers ratio |  |  | 
ThO2 | AB | NY | GCN
25% |  | 100% | 
50% |  |  | 50%
33% | 33% |  | 33%
25% | 25% | 50% | 
50% | 20% | 10% | 20%
2 µm
2 µm
2 µm
Pore former used in ThO2 | Open porosity (%)
NY | 17
GCN | 39
GCN + AB | 35
NY +AB | 15
NY+GCN+AB | 20
2 µm
2 µm
2 µm
2
2
2
2
2
2
No pore former
2
ISC: Public

## Slide 8
High temperature stability
Test conditions: 1850°C for 24h and 2000°C for 24h in vacuum
Transport of material to CERN for testing at higher temperature
Heat treatment at CERN
ThO2
ISC: Public

## Slide 9: Results after higher temperature heat treatment
ThO2 target material remains porous after treatment 2000°C 24h in vacuum!
ThO2
2 µm
2 µm
ThO2
GCN
GCN + AB
ThO2
GCN
GCN + AB
29 % open porosity
25 % open porosity
25 % open porosity
2 % open porosity
3 % open porosity
1850°C
2000°C
1
1
1
1
1
1
2 µm
2 µm
2 µm
2 µm
33 % open porosity
ISC: Public

## Slide 10: Irradiation of ThO2 at CERN
Objective : 50 g of ThO2 from the pore former study
ThO2 powder 1 made of small platelet
Dry mixed for 30 min at 50 RPM
Pellets of 20 mm of diameter and 1.5 mm thick
Mechanically stable (sintered 1750°C for 1h)
Irradiation test in early November at CERN
Extraction of radioisotopes in the MEDICIS facility
Unmixed powder of ThO2 + graphitic carbon nitride the pore former
ThO2
ThO2 target material that will be irradiated on the 3rd of November
ISC: Public

## Slide 11
Mixed
Heating to 1700°C in inert atmosphere
at JRC Karlsruhe
In Karlsruhe
ThO2 precursors
2 µm
2 µm
Graphite
Expanded graphite
Carbon black
Carbon sources
(reference ISOL carbon source)
(Novel material)
(novel for ThO2)
100 µm
100 µm
100 µm
ThCx
Development of porous ThC2
Surrogate materials ZrCx, NbCx and TiCx presented in poster ID 71
1
4
18 pellets of ThO2 made of platelets and nanoparticles and mixed with carbon sources
Pressed
Synthetized
ISC: Public
Notes: Also the work of Lisa

## Slide 12: Development of porous ThC2
Based on the mass loss the reaction was completed
The characterization of the material is done by SEM, XRD, BET and TGA in air
11 mm
11 mm
11 mm
ThCx pellets after CTR
Pellet | #1 | #2 | #3
Mass loss | 52,6 | 59 | 55,6
Theoretical mass loss | 48,3 | 59,3 | 55,9
ThCx
100
200
300
400
600
Carbothermal reduction of ThO2 with CO exhaust monitored
CO measured by IR detectors
ISC: Public

## Slide 13: ThC2 material characterization ongoing
ThCx
2 µm
First results of graphite mixed with 1 (platelets)
ThC2 C2/c seems to correspond with the all the pellets synthetized by carbothermal reduction of ThO2
ISC: Public

## Slide 14: Conclusion and outlook
Development of porous ThO2
  0 % of open porosity from ThO2 morphology tests after 10h at 1750°C
  42 % of open porosity reached after pore former addition and heat treatment of 1h at 1750°C in reductive atmosphere
  33% of open porosity after 24h at 2000°C in vacuum
  Isotope release at CERN with a 1.4GeV proton beam in November 2025
Development of porous ThCx
  Carbothermal reduction at JRC Karlsruhe was successful
  Characterization is ongoing
Conclusion
ISC: Public

## Slide 15
I would like to thank my colleagues from KULeuven, FMA and PTR group, and all of CERN and JRC people that helped me!
Funded by MYRRHA and SCK CEN academy
Thank you for your attention!
ISC: Public

## Slide 16
Copyright © SCK CEN
PLEASE NOTE!
This presentation contains data, information and formats for dedicated use only and may not be communicated, copied, reproduced, distributed or cited without the explicit written permission of SCK CEN. If this explicit written permission has been obtained, please reference the author, followed by ‘by courtesy of SCK CEN’.
Any infringement to this rule is illegal and entitles to claim damages from the infringer, without prejudice to any other right in case of granting a patent or registration in the field of intellectual property.
SCK CEN
Belgian Nuclear Research Centre
Foundation of Public Utility
Registered Office: Avenue Herrmann-Debrouxlaan 40 – BE-1160 BRUSSELS
Operational Office: Boeretang 200 – BE-2400 MOL
confidential
32
ISC: Public