## Slide 1
Longhi, G. (2025). Synthesis and characterisation of highly porous transition metal carbides, Master thesis, KULeuven.
Cordero, A. G. (2024). Tuning of ThO2 target materials towards highly porous structure to produce medical radioisotopes, Master Thesis, Universidad Politécnica de Madrid.
Rodriguez, C. (2025). Carbon source assessment for ISOL ThCx target materials, Master thesis, Universidad politcnedad Madrid.
Development of porous non-actinide target materials for the facility ISOL@MYRRHA
L. Gubbels1,2, B. Acevedo1, J.P. Ramos1, A.G. Cordero1,3, C. Rodríguez1,3, G. Longhi2,4, N. Rey-Raap5, F. Jutier1, S. Huang2, A. Arenillas5, P. Creemers1, D. Hermans1, M. Verwerft1, J. Vleugels2, L. Popescu1
1Belgian Nuclear Research Centre (SCK CEN), Mol, Belgium
2KU Leuven, Department of Materials Engineering (MTM), Leuven, Belgium
3Universidad Politécnica de Madrid (UPM), Madrid, Spain
4 Università degli Studi di Trento (UNITN), Trento, Italy
5 Instituto de Ciencia y Tecnología del Carbono, INCAR-CSIC. Francisco Pintado Fe, 26. 33011, Oviedo, Spain
Efficient isotope release in ISOL targets operating at extreme temperatures (≥2000 °C) requires materials with high porosity (>50 %) and thermal stability to ensure sustained radioactive isotope beam production. This study focuses on non-actinide carbide and oxide target material, specifically TiC, ZrC, ZrO₂, and NbC, synthesized via carbothermal reduction and advanced powder processing techniques. This was done as surrogate material work for ThO2 and ThCx. By incorporating various carbon sources -Expanded graphite (EG), multi-walled carbon nanotubes (MWCNT), carbon aerogels (C-aerogels) and polyamide - and pore former graphitic carbon nitride (GCN), we aim to control microstructural properties such as grain size, porosity, and phase stability to hinder sintering and maintain high diffusion and effusion rates. Optimizing these parameters is critical for enhancing refractory isotope release and extending target lifetime in high-power proton beam environments like ISOL@MYRRHA.
Introduction
Objectives
Small grain size < 10µm
Stable at > 2000 °C
Open porosity of 50 %
Pore size of 50 µm
Results
Conclusion and Outlook
www.sckcen.be
1
3
All six materials achieved grain sizes below 10 µm, meeting structural requirements. Porosity levels varied depending on composition and processing. TiCₓ, with added MWCNT and graphite, showed the highest open porosity, making it a strong candidate for ISOL targets. In contrast, NbC, despite the use of polyamide, had insufficient porosity for efficient isotope release. These results highlight the importance of pore formers and mixing methods in tailoring material performance for high-temperature isotope production.
ZrO2 mixed with pore formers (Cordero 2024)
Carbothermal reduction of TiO2 (Rodriguez, 2025) and ZrO2 (Longhi, 2025) with excess carbon
Oxide (s) + Carbon (s) → Carbide (s) + Volatile species (g) + Excess carbons
NbCx mixed with carbon sources (Longhi 2025)
Sintering hindering mechanisms
Using pore formers on oxides
Using excess carbon on carbides
Mix
Press
Heat
Carbide harder to sinter
Materials processing
ZrCx/NbCx/TiCx
ZrO2
Oxide
Carbon source
 | ZrO2 | ZrCx |  |  | NbC | TiC |  |  |  | 
Pore former/ Carbon sources | GCN | Graphite | Polyamide |  | Polyamide | Graphite | MWCNT |  | EG | C-aerogels
Ratio | 57* | 5** | 5** |  | 30* | 5** | 5** |  | 5** | 4**
Mixed conditions | dry, turbula | wet,turbula | wet,turbula |  | wet,turbula | wet,turbula | wet,sonicator |  | wet,turbula | wet,sonicator
Sintering | 1 h, 1750 °C | std |  | std | std | std |  | std | std | std
Bulk density (%) | 46 | 37 | 25 |  | 53 | 30 | 10 |  | 10 | 10
Open porosity (%) | 54 | 39 | 61 |  | 13 | 64 | 88 |  | 77 | 89
* Ratio in % volume,** Ratio in mol, std refers to standard conditions 2000 °C for 15 h in vacuum, ZrO2 was heat treated in reductive conditions
The SEM picture heat-treatment are presented in the table.
All materials kept grain size <10 µm after heat treatment. Porosity stability up to 2000 °C was observed for carbides, which is crucial for ISOL targets.
ZrO₂ + GCN: 54% open porosity, large pores (~50 µm) → good diffusion.
TiCₓ + MWCNT + graphite: very high porosity (88% total, 64% open) → excellent release, lower strength.
ZrCₓ: 61% open porosity → promising balance.
NbC: Porosity too low for efficient isotope release in ISOL targets
References
This research was funded by the MYRRHA project and the SCK CEN Academy.
Acknowledgments