## Slide 1: ISOL RIB Production EMIS XX Student Lecture Programme Whistler, Canada
João Pedro Ramos
Sunday, 19 Oct 2025
(Facilities overview will be given tomorrow at 10h30)

## Slide 2: ISOL Isotope Separation
Energetic particles
+/- 15V
1000 A
+/- 15 V
2400 A
Ion Source
Particle
Transfer line
4. Ionization
3. Effusion
2. Diffusion
1. Production
– Cross section [mb]
– Proton flux [cm-2]
– Nr of exposed atoms [dim]
– Efficiency [%]
5. Mass Separation
6. Transport
Extraction optics
Mass separator
Target unit
OnLine
Extraction electrode
up to 2300 °C
20 cm
Target heating by current and/or beam
<60 kV
0 V
(on target)
(on converter)

## Slide 3: Efficiency is key!
1 proton on target
~1 isotope created
(order of magnitude)
~0.5 mol
~1023 atoms
Target (U/Th)
~6 pmol/s
~1012 atom/s
1 µA p+
All production
(6x1012)
~0.2 fmol/s
~108 atom/s
RIB of interest
~0.2 amol/s
~105 atom/s
(to extract!!)
pico – 10-12
femto – 10-15
atto – 10-18
Full stadium has now:
1016 – 10 quadrillion grains of sand
Sand:
8 – 15 billion grains per m3
Typical football stadium. Inner volume ~ 1 million m3
Let’s fill it with sand!
Now we need hope that 1 specific grain of sand gets out of the stadium by heating it up to 2000°C!
(corresponds to an isotope with an in-target production of ~107 /s=16 amol/s)

## Slide 4: ISOL Facilities Worldwide
ISOLDE
CERN
1.4 – 1.7 GeV p Geneva (CH)
ALTO-LEB
IPN Orsay
50 MeV e→ Orsay (FR)
ISAC, ARIEL
TRIUMF
490 MeV p, 30 MeV e→ Vancouver (CA)
TRIGA Reactor
UNI Mainz
n (1.1×1011 n/(cm2 s)
Mainz (DE)
IGISOL
UNI-JYFL
30 MeV p, 14 MeV d,
HI < 130 MeV/u Jyväskylä (FI)
LERIB
iThemba LABS
70 MeV p Cape Town (ZA)
SPES
INFN-LNL
40 MeV p
Legnaro (IT)
ISOL RAON
IBS
70 MeV p
Daejeon (KR)
CARIBU
Argonne National Lab
252Cf sf Lemont (US)
Spiral, SPIRAL-II
GANIL
HI <95 MeV/u ,40 MeV d, 33 MeV p, 14.5 MeV/u HI
Caen (FR)
IRIS
PNPI
1 GeV p
St. Petersburg (RU)
ISOL@MYRRHA
SCK CEN
100 MeV p
Mol (BE)
TATTOOS
PSI
590 MeV p Villigen (CH)
ANURIB
VECC
50 MeV e→ New Town in Kolkata (IN)
MEDICIS
CERN
1.4 GeV p and
external sources
Geneva (CH)
RISIKO
UNI Mainz
External sources
Mainz (DE)
BRIF
CIAE
100 MeV p Beijing (CN)
Operational
Future
Offline RIB (operational)
Legend:
p+ High energy
p+ Low energy
e→
Gas catcher
Heavy ion
IRIN-PIK reactor
PNPI
n (3×1013 n/(cm2 s)
St. Petersburg (RU)
BISOL-CARIF reactor
CIAE
n (8 × 1014 n/(cm2 s)
Beijing (CN)
Reactor

## Slide 5: Why radioactive ion beams?
Production:
high radiation environment
Detection:
low radiation background
Transport methods:
carry (“SRAFAP”)
drive (G.T. Seaborg and W.D. Loveland, The Elements beyond Uranium, John Wiley & Sons, 1990)
transport shuttle with pressurized air
transport in gas-jet
pump through vacuum system
send as ion beam
primary
beam
target
1’000’000 m/s
10 m/s
1’000 m/s
50 m/s
100 m/s
Speed (approx.)
[SR22,UK06]
Slide courtesy of S. Rothe and S. Stegemann

## Slide 6: ISOL-history: off-line mass separation
Ionization to typ. q = 1+
Acceleration to e.g. 60 keV
Mass selection by magnetic deflection (Lorentz force)
( Br = p/q  A )
Position x
Position y
[SR22,UK06]
Slide courtesy of S. Rothe and S. Stegemann

## Slide 7: ISOL-history: first ISOL experiment at Niels Bohr Institute
[UK06, TDG17, SR22]
ISOL beams of 89-93Kr
O. Kofoed-Hansen and K. O. Nielsen, Phys. Rev. 82 (1951)
Slide courtesy of S. Rothe and S. Stegemann

## Slide 8: Production: Primary beam
Protons, electrons and (heavy) ions are typical primary beams
(p,f): 3x
(p,nx): 15x
Ratio of cross sections at 100 MeV vs 1GeV
35 MeV e- – 2.8 mA
100 kW
95 MeV/u or 40 MeV d+ – mA
200 kW
1.4GeV p+ – 2 μA
2.8 kW (1.2 GW)
(6 kW)
L. Popescu, et al., DOI: 10.1016/j.nimb.2019.05.023
W
Fast neutrons
Isobarically pure n-rich fission products
High Z material (Ta)
Bremsstrahlung photons
Induce fission in U
ISOL@
40 MeV p+ – 200 μA
8 kW
Computational codes are typical tools used to estimate in-target productions (e.g. FLUKA)

## Slide 9
Let’s zoom into
Proton beam
Radioactive Ion Beam
*courtesy of A. Atherton and D. Atanasov
*courtesy of P. Creemers
*courtesy of S. Hurier, D. Houngbo, K. Rijpstra
ISOL@

## Slide 10: The Target Ion Source – variety of target materials
A. Gottberg, DOI: 10.1016/j.nimb.2016.01.020
Top view – proton fluences
Target and Ion Source Assembly
In a box: currently used
ISOL Target Materials tested so far
Underlined/bold: materials development
J.P. Ramos, NIM B 463 (2020)
J.P. Ramos, PhD thesis

## Slide 11: Target Unit – Heart of
Ions
Radioisotopes
Primary beam
*picture and animation courtesy of M. Delonca
Vacuum
Air
1.4 GeV proton
fragmentation
fission
spallation
238U
142Cs
11Li
201Fr
X
Y
Beam power
2.8 kW in average
1.2 GW (pulse length 2.3 μs)
  ~10% deposited
What is the sound of proton impact on target?

## Slide 12
Targets

## Slide 13: ISOL Targets
High Power
Target PTF, D. Houngbo
TiC nano, J.P. Ramos, PhD Thesis
SPES target, M. Manzolaro, PhD Thesis
Stacked Ø 2 cm coated graphite foils to conduct heat away.
Need to be cooled
Complex and “dirty” fabrication procedure (pollute targets with many contaminants, long conditioning)
ISAC Targets
ISOL@MYRRHA / SPES
High Power Targets
ISOLDE - Low Power <300 W
  Very high deposited power densities
  Needs to be cooled – radiative cooling
  In development – yet to be proven technology
  Compact assembly of disks
  High energy beams (1.4 GeV) – very low energy loss/deposited
  Target needs to be heated with an oven

## Slide 14: Liquid targets
Targets can also be liquid metals or salts (ISOLDE)
High density but slow diffusion times (cm instead of µm)
High vapor pressure needs usage of chimneys to condense targe material
Pulsed beams creates shockwaves
E. Noah et. al DOI: 10.1016/j.nimb.2008.05.051
F. Boix Pamies et. al DOI: 10.1016/j.nimb.2019.06.043
LIEBE target tested offline to create a LBE (Lead Bismuth Eutectic) loop and a shower of droplets

## Slide 15: Temperature homogeneity importance
M. Ballan et. al doi: 10.1016/j.nimb.2016.01.038
S. Rothe et. al doi: 10.1016/j.nimb.2016.01.038
Dy yield increased from around 1% to ~24%!
Low Power – Ohmic heating optimization!
High Power – Ohmic + beam heating optimization!

## Slide 16: Converter targets
Water cooled fins
100 kW, 35 MeV electrons (range ~ 5 mm)
L. Egoriti, A. Gottberg, HPTW 2018
J.P. Ramos, doi: 10.1016/j.nimb.2019.04.060
A. Gottberg, HPTW 2018
Target assembly at 2000 ºC
Tungsten converter
100 µA protons
100 µA protons
Tantalum container and legs
Annular UCx target material
Axial screws & spring washers
Converter Assembly
Water cooled copper
100 µA protons
Heating current IN
Heating current OUT
Graphite sleeve

## Slide 17: Gas catcher and fragmentation
Fragments are stopped in 200-500 mbar of He, but remain charged. They are transported by the He to the extraction optics for acceleration.
P. Chauveau, S. Hurier, et al.
IGISOL U238 or Th232 target – 30 MeV p+ beam
Y. Blumenfeld, et al. DOI: 10.1088/0031-8949/2013/T152/014023

## Slide 18: Target material influence on RIB intensity?
Melting/Sublimation
Sintering
Grain size increase
Reduction of porosity
Targets are traditionally operated at very high temperatures (close to the materials melting point)
Chart: Target Temperature
| 24.699999999999989 | 102 | 202 | 301.99999999999994 | 401.99999999999994 | 451.99999999999994 | 501.99999999999994 | 552 | 602 | 652 | 702 | 752 | 802 | 852 | 902 | 952
 | 0.42573 | 114.082 | 10631.9017 | 204812.0561 | 1642873.545 | 3751666.0785 | 7701734.9507 | 14491200.7639 | 25366333.3837 | 41795805.1335 | 65429100.1916 | 98045046.8083 | 141496257.8747 | 197654319.9033 | 268359307.4753 | 355375928.474
31Ar (15.1 ms)
32Ar (98 ms)
35Ar (1.78 s)
Arrhenius dependence of effusion and diffusion with temperature
However during operation
Target material degradation
or even low from the beginning
Very often
Expected beam intensity

## Slide 19: What is sintering?
Temperature - time
Sintering temperature (densify):
Defined in function of the material melting point (Tm)
0.5 to 0.8Tm
0.2 to 0.4Tm
Main reason why nanomaterials were discarded in the past for ISOL target application
Micrometric materials
Nanomaterials
The smaller the particle size (larger surface area) the higher the sintering driving force
!
!
Sintering can be affected by irradiation (defect creation)

## Slide 20: Target material influence on beam intensity?
Time
In most cases limit by far the yields.
Operation T
Grain size/Porosity
Assess microstructure stability
r /10
Diffusion limited release:
x10
Chart: t1/2 (s)
| 0.01 | 0.02 | 0.03 | 0.04 | 0.05 | 0.06 | 7.0000000000000007E-2 | 0.08 | 0.09 | 0.1 | 0.2 | 0.3 | 0.4 | 0.5 | 0.6 | 0.7 | 0.8 | 0.9 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100 | 200 | 300 | 400 | 500 | 600 | 700 | 800 | 900 | 1000 | 2000 | 3000 | 4000 | 5000
 | 0.00054957 | 0.0018729 | 0.0036522 | 0.0057048 | 0.00792 | 0.010229 | 0.012586 | 0.014963 | 0.017341 | 0.019706 | 0.041777 | 0.06095 | 0.078054 | 0.093714 | 0.10831 | 0.12207 | 0.13516 | 0.14767 | 0.15969 | 0.26076 | 0.33869 | 0.4014 | 0.45312 | 0.49656 | 0.53358 | 0.56552 | 0.59335 | 0.61782 | 0.76137 | 0.82651 | 0.86371 | 0.88777 | 0.90462 | 0.91706 | 0.92663 | 0.93423 | 0.94039 | 0.96924 | 0.97927 | 0.98437 | 0.98745 | 0.98952 | 0.991 | 0.99212 | 0.99299 | 0.99369 | 0.99683 | 0.99789 | 0.99841 | 0.99873
1 μm
1
2
3
4
t1/2 = 1 s
1s – 50%
2s – 25%
3s – 12.5%
4s – 6.25%
10x smaller!
Porous nanomaterials campaign started ~15 years ago (ISOLDE is 55 years old)
  Shorter diffusion lengths
  Higher porosity
Chart: Target Temperature
| 24.699999999999989 | 102 | 202 | 301.99999999999994 | 401.99999999999994 | 451.99999999999994 | 501.99999999999994 | 552 | 602 | 652 | 702 | 752 | 802 | 852 | 902 | 952
 | 0.42573 | 114.082 | 10631.9017 | 204812.0561 | 1642873.545 | 3751666.0785 | 7701734.9507 | 14491200.7639 | 25366333.3837 | 41795805.1335 | 65429100.1916 | 98045046.8083 | 141496257.8747 | 197654319.9033 | 268359307.4753 | 355375928.474
Diffusion/Effusion
Can we stabilize porous nanostructures at high temperatures?
Unique in the literature
Needs R&D
100 nm
Same T!
Nano materials sinter faster
Reduce operation temperature to stabilize
Diffusivity
(rate of diffusion)
Diffusion lengths

## Slide 21: How to develop a new target material?
Identifying suitable target nucleus and target chemical compound
Stabilizing microstructure at high temperature and high-power irradiation
Engineering desired microstructure
Studying diffusion and release properties
Post-irradiation material analysis
Online tests
Protons
Refractory materials!
Post irradiation pictures: S. Fernandes, J. Nucl. Mat. 416 (1-2), 99-110 (2011)
FLUKA
ABRABLA
2-5 years per material
Slide adapted from A. Gottberg

## Slide 22: Material characterization techniques
Scanning Electron Microscopy
Nitrogen adsorption
Mercury intrusion porosimetry
Laser diffraction particle size distribution
Thermal treatments
Dilatometry
Residual gas analysis
Differential thermal analysis
Thermogravimetric analysis
Pore size distribution (micro, meso, macro)
Particle size (distribution)
Mass losses (temperature)
Elemental analysis
Linear shrinkage
Morphology
Grain size
Phase composition and changes
Crystallite size
Lattice parameters
Specific surface area
Isotope release properties
Energy Dispersive X-ray Spectroscopy
X-ray powder diffraction
X-ray photoelectron spectroscopy
Carrier gas hot extraction analysis
Combustion analysis with IR spectrometry
Tapestation (ISOLDE facility)
Gamma spectroscopy
Dedicated physics experiments
Thermal techniques
Microstructure
Phase and elemental composition
Radioactivity/online

## Slide 23: Let’s keep zooming in! Into the microstructure…
0.67 mm
100 μm
20 μm
2.0 μm
660 nm
200 nm
“There is plenty of room at the bottom”! R. Feynman
31 x
200 x
1 000 x
10 000 x
30 000 x
100 000 x
…At ISOL@MYRRHA we span almost 10 orders of magnitude!

## Slide 24: TRIUMF (non-)irradiated UCx analysis
About small 6 samples of uranium carbide sent to SCK CEN
  Both irradiated and non-irradiated
  Very radioactive samples (reduced size), also UCx is pyrophoric
MNA, NMS (Microstructural and Non-destructive analysis)
FMA, NMS (Fuel Material)
At SCK CEN… preparation of lamella
At TRIUMF… Sample preparation and extraction in hot cell (not in picture)
M. Cervantes et al. – To be published

## Slide 25: TRIUMF (non-)irradiated UCx analysis
Drastic changes are seen after irradiation.
MNA, NMS (Microstructural and Non-destructive analysis)
FMA, NMS (Fuel Material)
Non-irradiated
Irradiated
M. Cervantes et al. – To be published
Preliminary
Preliminary

## Slide 26: Example of the B beams
Area 7140 m2 (68 x 105 m) – FIFA recommendation
14.85 g of MWCNT
4352.1 m2
> 60% Football field
Specific Surface Area
293.1 m2/g
Injection of CF4 or SF6
Melting point 2070 °C
Reacts with other elements to form refractory compounds
Formation of BFx
870 12BF2+ / µC measured in IDS later
per mC of proton beam
Chart: 
 | 64000 | 515 | 2
 | 8220000 | 2868000 | 31260
 | 1370000000 | 478000000 | 5210000
6.4 E+04
Measurement
Prediction
5.1 E+02
2 E+00
/ mC
Half-life losses during release
Extracted yield
Not extractable due to fixed efficiencies*
*not depending on half-life: ionization eff., molecular formation eff., etc.
0.15%
1.7%
0.0026%
Boiling point ~4000 °C
Yield =
N0
erelease (T1/2)
eion eother
eform
J. Ballof, EMIS2018, PhD thesis & http://doi.org/10.1140/epja/i2019-12719-1

## Slide 27: Example of the B beams
J. Ballof, EMIS2018 & http://doi.org/10.1140/epja/i2019-12719-1
1. Diffusion in the solid
Yield =
N0
erelease (T1/2)
eion eother
eform
Offline mobility studies: Christoph Seiffert
Release Efficiency: Fraction of isotopes not decayed before release
Slow process
Was investigated in offline experiments
Long heat treatment times necessary ~ 30 min
Simple model: Fick‘s 2nd law
2. Effusion through open space
Fast process
Best investigated online
Online release curve fitted with release model
measured on 8B and corrected for decay
Model for release of a stable isotope:
with , , mth positive root of Bessel function of order 0, normalization constant
Characteristic diffusion time tD = 862 s
Effusion time constant teff = 339 ms

## Slide 28
Transfer Lines

## Slide 29: Transfer lines - standard
Only very volatile species allowed:
Noble gases, CO, NO, O2
Hot/standard transfer line
2000°C
(same temperature as ion source)
All elements allowed
Cold transfer line
~25°C

## Slide 30: Transfer lines - special
Delays/traps higher adsorption enthalpy elements (i.e. alkali):
Reduces beam of interest slightly
But Rb reduced by 10-5, Cs by 10-3 and Li, K by 10-2.
“Warm”/temperature regulated transfer line
200-400°C
Relatively low volatility elements allowed (Zn, Cd, Hg)
Mainly used in liquid metal targets: condense target material evaporating) but also filters less volatile elements
Quartz, temperature regulated transfer line
“Cold” type 380-790°C “Warm” type 680-1150°C

## Slide 31
Ion Sources

## Slide 32: Ionization methods
[UK06-mod]
U. Koster, DOI: 10.1016/S0375-9474(01)01625-6
Also ECR ion sources, negative ion sources (but for another time…)

## Slide 33: Surface ionization
R. Kirchner. NIM 198 (1981) 10.1016/0029-554X(81)90916-2
R. Kirchner. NIM A 292 (1990). 10.1016/0168-9002(90)90377-I
R. Kirchner. NIM B 204 (2003). 10.1016/S0168-583X(02)01900-6
[UK06-mod, TDG17-mod]
Adapted from S. Stegemann, ISOL-France workshop V, Bordeaux Lecture, 2023 and S. Rothe, CERN Academic Training 2023
Ionization efficiency vs (eff.) ionization potential
Ionizer material
* Ta, W, Re, Ir, Pt
* temperatures up to 2800 K
* e.g. tungsten with f~4.5 eV at 2400 °C
* Work function depends on crystal orientation,
temperature and cleanliness

## Slide 34: Surface ionizable elements
[UK06]
S. Stegemann, ISOL-France workshop V, Bordeaux Lecture, 2023

## Slide 35: Laser ionization
Mass separation
Resonance ionization
Energy
Ground state
Excited states
Probed transition
Ionization potential
Auto-ionizing state
Atom
Ion
10 eV
[UK06-mod, TDG17-mod, RH22-mod]
Adapted from S. Stegemann, ISOL-France workshop V, Bordeaux Lecture, 2023
Ionization
lasers
Target / sample
Collection / Experiment
HV platform
Ion
B. Marsh, DOI: 10.5170/CERN-2013-007.203

## Slide 36: Laser ionized elements (RILIS – CERN)
[RE23]
RILIS Elements, DOI: https://rilis-web.web.cern.ch/node/103

## Slide 37: Electron impact ionization
Properties
+ universal ionization (“dirty” ion source )
+ good efficiency for noble gasses and volatile species
+ moderate emittance (<20 p mm mrad at 15 kV, 95%)
Limited lifetime
- Has to be used with transfer lines to filter out contaminants
Example: Forced Electron Beam Arc Discharge ion source
[UK06-mod, TDG17, FW03, SR22]
Adapted from S. Stegemann, ISOL-France workshop V, Bordeaux Lecture, 2023

## Slide 38
[TDG17]
S. Stegemann, ISOL-France workshop V, Bordeaux Lecture, 2023
Electron impact ionization

## Slide 39: Ionization methods: overview
[YM17-mod, SR22]
Hot cavity
Universality
Selectivity
Simplicity
Reliability
Efficiency
Surface ionization
Laser ionization
FEBIAD – Plasma ion source
ISOLDE
Slide courtesy of S. Stegemann, S. Rothe, Y. Martinez

## Slide 40: Overview of element ionization techniques (ISOLDE)

## Slide 41
Extraction, transport and mass separation
Extraction optics
Mass separator
Target unit

## Slide 42: Extraction and beam transport
>+60 kV
0 V - Ground
Potential field in kV
Particle trajectories and potential in kV
Picture courtesy of S. Ramos
F. Maldonado, MSc thesis (TRIUMF)

## Slide 43: Mass separation
Radioactive
isotopes
Magnetic field
bends ions
Too light
Too heavy
Selected mass
Adapted from M. Mougeot
+ molecules with lighter isotopes (e.g. 136Ce+16O is A=152)
+stable contaminants from targe/ion source (molecules or atomic)

## Slide 44: Mass separation
Adapted from D. Atanasov
Higher resolution
(MR-ToF)
А = 151
А = 152
А = 153
Typical resolution

## Slide 45: Key takeaways - efficiency is key!
1 proton on target
~1 isotope created
(order of magnitude)
~0.5 mol
~1023 atoms
Target (U/Th)
~6 pmol/s
~1012 atom/s
1 µA p+
All production
(6x1012)
~0.2 fmol/s
~108 atom/s
RIB of interest
~0.2 amol/s
~105 atom/s
(to extract!!)
pico – 10-12
femto – 10-15
atto – 10-18
Full stadium has now:
1016 – 10 quadrillion grains of sand
Sand:
8 – 15 billion grains per m3
Typical football stadium. Inner volume ~ 1 million m3
Let’s fill it with sand!
Now we need hope that 1 specific grain of sand gets out of the stadium by heating it up to 2000°C!
(corresponds to an isotope with an in-target production of ~107 /s=16 amol/s)

## Slide 46: Key takeaways
RIB production through ISOL is very diverse technique
Isotope production can happen through different driver beams which can include conversion steps (electron to gamma, proton to neutron)
Target materials microstructural behavior under high temperature and high irradiation and stabilization methods are essential for reliable cumulated yields to users.
In-situ chemical selection can be done, already in the target-ion source assembly, through special transfer lines, before reaching the mass separation
Ion sources in ISOL are highly efficient and a few methods exist
Molecular beams are becoming more popular for extraction of refractory beams, but also for contamination cleanup (shifting in A/q)
ISOL technique, with enough services available for the Target and Ion source Assembly, allows thousand of combinations with different targets, transfer lines and ion sources.
Working on efficient and innovative target and ion source systems (target materials, ion sources, etc.) is a much more cost-effective path than just increasing power on target, for high in-target production

## Slide 47
Copyright © SCK CEN
All property rights and copyright are reserved.
This presentation contains data, information and formats for dedicated use only and may not be communicated, copied, reproduced, distributed or cited without the explicit written permission of SCK CEN.
If this explicit written permission has been obtained, please reference the author, followed by ‘by courtesy of SCK CEN’.
Any infringement to this rule is illegal and entitles to claim damages from the infringer, without prejudice to any other right in case of granting a patent or registration in the field of intellectual property.
SCK CEN
Belgian Nuclear Research Centre
Studiecentrum voor Kernenergie
Centre d'Etude de l'Energie Nucléaire
Foundation of Public Utility
Stichting van Openbaar Nut
Fondation d'Utilité Publique
Registered Office:
Avenue Herrmann-Debrouxlaan 40 - 1160 BRUSSELS - Belgium
Research Centres:
Boeretang 200 - 2400 MOL - Belgium