## Slide 1: Revealing the superconducting gap structure of kagome metals via μSR and complementary techniques
Jennifer Graham and Zurab Guguchia
Paul Scherrer Institute

## Slide 2: Acknowledgements
Zurab Guguchia
Sohel Islam
Debarchan Das
Vahid Sazgari
Chip Mielke
Rustem Khasanov
Hubertus Luetkens
Andrin Doll
Ritu Gupta
Tommaso Morresi
M. Zahid Hasan
Stephen Wilson
Andrea Salinas
Z. Wang
Y. Li
Y. Yao
Hai Deng
Jiaxin Yin
Yigui Zhong
Kozo Okazaki
Hechang Lei

## Slide 3: Overview
C. Mielke III et al. Nature 602, 245-250 (2020) • R. Gupta et al. Comms. Phys. 5, 232 (2022)
Z. Guguchia et. al., Nat. Commun. 14, 153 (2023) • J. N. Graham et al. arXiv:2411.18744 (2024)
Superconductivity in undoped compounds
Enhancing superconductivity
BCS or something more exotic?
TC

## Slide 4: AV3Sb5 (A = K, Rb, Cs)
a
b
c
a
b
 | Tc (K) | TCO (K)
K | 0.93 | 80
Rb | 0.75 | 110
Cs | 2.5 | 90
A
B. R. Ortiz et al. Phys. Rev. Mater 3, 094407 (2019), K. Jiang et al. Natl. Sci. Rev. 10, 2, nwac199 (2023),
Y. Zhong et al. Nature 617, 488 (2023), Y. Liu et al. Phys. Rev. Mater. 6, 124803 (2022).
V Sb
P6/mmm space group
TC (K)
RVS
KVS
CVS
0.75
0.93
2.5
Notes: Add TRSB orbital currents to kagome

## Slide 5: Pairing symmetries with μSR
s-wave
p-wave
ℓ = 1
d-wave
ℓ = 2
ℓ = 0
Chiral d-wave
Lz =
Nodeless (s)
Nodeless (s)
Nodal (d)
How to distinguish more exotic symmetries from s?
s and d – no TRSB || p and chiral d – TRSB
J.E. Sonier et al, PRL 72, 744 (1994)
Nodeless (s, p, chiral d)
Nodal (d)

## Slide 6: Superfluid response
(μs)
Weak TF μSR measurements of KV3Sb5 (Dolly)
C. Mielke III et al. Nature 602, 245-250 (2020)
TC (K)
RVS
KVS
CVS
0.75
0.93
2.5

## Slide 7: 2 band superconductor
C. Mielke III et al. Nature 602, 245-250 (2020), V. Kogan, et. al., PRB 80, 014507 (2009)
Superfluid density of KV3Sb5
No saturation → nodal
Two step behaviour = 2 weakly coupled gaps
TC (K)
RVS
KVS
CVS
0.75
0.93
2.5
d

## Slide 8: Does nodal behaviour persist under pressure?

## Slide 9: Gap structure
TC (K)
RVS
KVS
CVS
0.75
0.93
2.5
μSR measurements under pressure for RbV3Sb5 (GPD)
Gap changes from two nodal to single nodeless
Z. Guguchia et. al., Nat. Commun. 14, 153 (2023)

## Slide 10: Phase diagrams
RbV3Sb5
KV3Sb5
TC (K)
RVS
KVS
CVS
0.75
0.93
2.5
Phase diagrams constructed from μSR and AC susceptibility
Change in gap structure under pressure
KV3Sb5
RbV3Sb5
Saturation of superconductivity coincides with full suppression of charge order
Z. Guguchia et. al., Nat. Commun. 14, 153 (2023)
Charge order influences superfluid density and superconducting gap structure

## Slide 11: How does chemical doping affect superconductivity?

## Slide 12: Chemical doping
Y. Zhong, J. Liu, X. Wu, Z. Guguchia et. al. and K. Okazaki, Nature 617, 488-492 (2023).
J. N. Graham et. al., arXiv:2411.18744 (2024).
TC (K)
CVS
Nb-CVS
Ta-CVS
2.5
4.4
5.2
Doping changes gap structure from nodal to nodeless

## Slide 13: ARPES
Y. Zhong, J. Liu, X. Wu, Z. Guguchia et. al. and K. Okazaki, Nature 617, 488-492 (2023),
J. N. Graham et. al., arXiv:2411.18744 (2024).
TC (K)
CVS
Nb-CVS
Ta-CVS
2.5
4.4
5.2
 | muSR (meV) | ARPES (meV)
Nb-CVS | 0.59(5) | 0.54(6)
Ta-CVS | 0.80(5) | 0.77(6)

## Slide 14: STM
Nb-CVS
Ta-CVS
TC (K)
CVS
Nb-CVS
Ta-CVS
2.5
4.4
5.2
J. N. Graham et. al., arXiv:2411.18744 (2024),
H. Deng, G. Liu, Z. Guguchia et. al., Nature Materials 23, 1639–1644 (2024)
STM shows nodeless gap structures for doped compounds consistent with μSR and ARPES
Undoped compounds are nodal

## Slide 15: What if we combine pressure and doping?

## Slide 16: Pressure Dependence
AC χ data and b. μSR measurements at different pressures
TC (K)
CVS
Nb-CVS
Ta-CVS
2.5
4.4
5.2
J. N. Graham et. al., arXiv:2411.18744 (2024)

## Slide 17: Pressure Dependence
AC χ data and b. μSR measurements at different pressures
TC (K)
CVS
Nb-CVS
Ta-CVS
2.5
4.4
5.2
J. N. Graham et. al., arXiv:2411.18744 (2024)

## Slide 18: Pressure Dependence
AC χ data and b. μSR measurements at different pressures
TC (K)
CVS
Nb-CVS
Ta-CVS
2.5
4.4
5.2
J. N. Graham et. al., arXiv:2411.18744 (2024)

## Slide 19: Pressure phase diagram
TC (K)
CVS
Nb-CVS
Ta-CVS
2.5
4.4
5.2
Pressure phase diagram from AC susceptibility measurements
J. N. Graham et. al., arXiv:2411.18744 (2024)
Chemical doping enhances superconductivity
Pressure enhances superconductivity
Critical pressure smaller than undoped CVS (1.75 GPa)
Always nodeless

## Slide 20: BCS or more exotic?
Theory (chiral-d) : M.L. Kiesel and R. Thomale, Phys. Rev. Lett. 110, 126405 (2013), X. Wu et. al., Phys. Rev. Lett. 127, 177001 (2021), S.C. Holbaek et. al., Phys. Rev. B 144508 (2023), Y. Dai et. al., Phys. Rev. B 110, 144516 (2024).
Nodal → nodeless superconductivity
Suppression of charge order
→ TRSB across TC
Universal feature of AV3Sb5 superconductors
J. N. Graham et. al., arXiv:2411.18744 (2024)

## Slide 21: Conclusions
C. Mielke III et al. Nature 602, 245-250 (2020) • R. Gupta et al. Comms. Phys. 5, 232 (2022)
Z. Guguchia et. al., Nat. Commun. 14, 153 (2023) • J. N. Graham et al. arXiv:2411.18744 (2024)
Multigap nature, small superfluid density and nodal structure in (K/Rb)V3Sb5
Pressure and doping induce crossover from nodal to nodeless gap when charge order weakened
TRSB across Tc indicated unconventional (chiral d) superconductivity
TC

## Slide 22: CsV3Sb5
R. Gupta et al. Comms. Phys. 5, 232 (2022)
Two strongly coupled nodeless gaps
Pressure has complex evolution
Tc maximised after full suppression of charge order
TC (K)
RVS
KVS
CVS
0.75
0.93
2.5

## Slide 23: Superconducting Gap: Pressure
 | 0 GPa | 0.4 GPa | 0.8 GPa | 1.2 GPa
Tc (K) | 3.000(6) | 3.25(1) | 6.67(7) | 6.94(2)
λ-2(T = 0) (μm-2) | 6.9(3) | 5.7(3) | 10.0(4) | 12.5(1)
λ(T > 0) (nm) | 381 | 419 | 315 | 283
Δ1 (meV) ω1 (%) | 0.54(9) 100 | 0.47(7) 100 | 0.65(5) 73(4) | 1.56(4) 100
Δ2 (meV) ω2 (%) | - | - | 3.5(9) 27(4) | -
λ = London penetration depth, Δ = Gap size, ω = Phase fraction