## Slide 1: Non‑destructive depth‑selective quantification for carbon in steel using negative muon lifetime analysis
Kazuhiko Ninomiya
ninomiya-kazu@hiroshima-u.ac.jp

## Slide 2: Collaborators
The 16th International Conference on Muon Spin Rotation, Relaxation and Resonance (μSR2025)
Hiroshima University
Kosei Yakushi
International Christian University
Michael Kenya Kubo
Kyoto University
Makoto Inagaki
KEK
Go Yoshida, Soshi Takeshita, Naritoshi Kawamura, Patrick Strasser, Yasuhiro Miyake, Koichiro Shimomura
National Museum of Japanese History
Tsutomu Saito
Dr. Inagaki
Dr. Yoshida

## Slide 3: Contents
The 16th International Conference on Muon Spin Rotation, Relaxation and Resonance (μSR2025)
Introduction
Muonic atom formation and muon decay
Muon lifetime measurement
Experimental
Results and Discussion
Lifetime spectrum analysis
Calibration
Depth profile analysis
Application to Japanese sword analysis
Summary
Published : K. Ninomiya et al., Scientific Reports, 14, 1797 (2024)

## Slide 4: Muonic atom formation and muon decay
The 16th International Conference on Muon Spin Rotation, Relaxation and Resonance (μSR2025)
nucleus
electron
muon
muonic X-ray
nuclear absorption
decay into electron
or
A muonic atom forms when a muon is captured into a muon atomic orbit.
Muonic X-rays are emitted in the de-excitation process of a muonic atom.
After a muon reaches to the muonic 1s state, the muon decays into an electron or is absorbed in a nucleus.

## Slide 5: Muon lifetime measurement
The 16th International Conference on Muon Spin Rotation, Relaxation and Resonance (μSR2025)
A. Knecht et al., Eur. Phys. J. Plus 135, 777 (2020)
T. Yamazaki et al., Phys. Scr. 11, 133 (1975)
Nuclear absorption
(λabsorption)
Decay
(λdecay：constant)
τ：muon life time
λabsorption varies by element
(larger with increasing atomic number)
µ-
Z
Z
e-
n
γ-ray
νµ
νµ
Identify elements by lifetime measurement
νe

## Slide 6: Muon lifetime measurement
The 16th International Conference on Muon Spin Rotation, Relaxation and Resonance (μSR2025)
The atom captured muon can be identified by lifetime
Intensity for each element corresponds to the number of captured muons
 | Z | Lifetime/ns [2]
Cr | 24 | 255.3±2.0
O | 8 | 1795.4±2.0
C | 6 | 2026.3±1.5
[2] T. Suzuki et al., Phys. Rev. C, 35 (1987) 2212.
Schematic view of lifetime measurement
µ-
e-
Plastic scintillation counter
Sample
Lifetime spectrum
Muon induced timing
Electron detection timing
Quantitative elemental analysis is possible
lifetime spectrum for Cr2O3[2]

## Slide 7: Muon lifetime measurement
The 16th International Conference on Muon Spin Rotation, Relaxation and Resonance (μSR2025)
Why the muon lifetime analysis method ?
Analyze the inside of materials non-destructively.
Stopping depth can be controlled by the incident energy of the muon.
High energy decay electron (~50 MeV) escapes from the bulk material
Highly sensitive to light elements
Muons captured by heavy elements disappear quickly
Muons captured by light elements can be observed in a long time window
=> analysis of trace elements, especially for light elements, is possible
Decay electrons can be detected by a μSR spectrometer
Additional detection system is not necessary
We selected steel (Fe + small amount C) as the first target

## Slide 8: Experimental
The 16th International Conference on Muon Spin Rotation, Relaxation and Resonance (μSR2025)
Muon irradiation experiment was conducted at the muon facility in J-PARC.
µSR spectrometer at D1 area in J-PARC (KALLIOPE)[3] was used for lifetime measurement
[3] K M Kojima et al 2014 J. Phys.: Conf. Ser. 551 012063
2000 ch plastic scintillation counter system
µ-
sample
Plastic scintillation counters
Schematic view of experimental setup
e-

## Slide 9: Experimental
The 16th International Conference on Muon Spin Rotation, Relaxation and Resonance (μSR2025)
Sample | Incident muon momentum (MeV/c) | Range in Fe (mm)
Fe-STD C: 30ppm | 43 | 0.95
Fe-STD C: 0.42% | 43 | 0.95
Fe-STD C: 4.46% | 43 | 0.95
 | 51 | 1.63
Layered sample | 32 | 0.35
 | 40 | 0.73
 | 46 | 1.21
Structure of layered sample
C:1.03%
C:0.20%
C:0.51%
Muon beam
*0.5 mm thickness in each
Experiment 1 (Standard Fe samples (Fe-STD)) : Calibration curve (quantitative analysis)
Experiment 2 (Layered sample) : Demonstration of non-destructive depth-profiling

## Slide 10: Lifetime analysis
The 16th International Conference on Muon Spin Rotation, Relaxation and Resonance (μSR2025)
N(t)： electron counts at time “t”
Ai： captured muon in component “i”
τi： life time of components “i”
The spectra were fitted by 4 components; Iron, Carbon, Air and BGD.
The component of Air was estimated from the results of pure Fe.
 | Fe | C | air | BGD
lifetime /ns[2] | 206 | 2026 | N: 1907 O: 1795 Ar: 537 | 20000
[2] T. Suzuki et al., Phys. Rev. C, 35 (1987) 2212.

## Slide 11: Calibration data
The 16th International Conference on Muon Spin Rotation, Relaxation and Resonance (μSR2025)
Linear relation between intensity and content of C/Fe
Estimated detection limit was 140 ppm by 2-hour measurement
Sample: Fe-STD C:0.42 %

## Slide 12: Depth profile analysis
The 16th International Conference on Muon Spin Rotation, Relaxation and Resonance (μSR2025)
Lifetime spectra were clearly changed by changing muon incident momentum (muon stopping depth)
0.5 mm thickness in each
C:1.03 %
C:0.20 %
C:0.51 %
Muon beam
40 MeV/c
32 MeV/c

## Slide 13: Depth profile analysis
The 16th International Conference on Muon Spin Rotation, Relaxation and Resonance (μSR2025)
Lifetime spectra were clearly changed by changing muon incident momentum (muon stopping depth)
0.5 mm thickness in each
C:1.03 %
C:0.20 %
C:0.51 %
Muon beam
Incident muon momentum /MeV/c | Carbon contents by muon analysis /% | Certified value /%
32 | 1.084±42 | 1.03
40 | 0.192±11 | 0.20
46 | 0.494±20 | 0.51
Depth profile analysis is successfully demonstrated

## Slide 14: Japanese sword analysis
The 16th International Conference on Muon Spin Rotation, Relaxation and Resonance (μSR2025)
Experimental condition
Sn mask with
5 x 30 mm hole
Incident muon momentum of 38, 43, 49, 57 and 63 MeV/c
(muon range : 0.6 ~ 3.2 mm)
Thickness ~6 mm
Sample: Kyusyu Higo Dodanuki Hyobu: 九州肥後同田貫兵部 (late 16th century)
Muon irradiation position
Irradiation time : 3 ~ 6 hours
Typical structure of Japanese sword
Surface part (hard iron)
皮金（Kawa Gane）
Core part (soft iron)
芯金（Shin Gane）
Muon beam

## Slide 15: Japanese sword analysis
The 16th International Conference on Muon Spin Rotation, Relaxation and Resonance (μSR2025)
Depth profile of carbon contents in the Japanese sword was non-destructively investigated
The carbon contents in surface is relatively higher than these in core part, this profile was consistent with the known property of Japanese swords
Surface part
(hard iron)
Core part
(soft iron)

## Slide 16: Summary
The 16th International Conference on Muon Spin Rotation, Relaxation and Resonance (μSR2025)
We have developed a novel non-destructive light element analysis method for bulk materials by muon lifetime analysis.
A linear relation was found between intensity and the content of C/Fe. Quantitative analysis is possible using the calibration data.
The detection limit was 140 ppm for a 2-hour measurement.
In the analysis of a layered sample with 3 iron standard samples having different carbon contents, each layer was selectively analyzed by adjusting the incident muon momentum.
Carbon contents of a Japanese sword can be investigated non-destructively.