## Slide 1: Observation of Na and Li Ion Diffusion in Battery Materials NaCrO2 and LiCrO2 by mSR
Izumi UMEGAKI (KEK)
2025. 7.21.
16th International Conference on Muon Spin Rotation, Relaxation and Resonance (μSR2025)

## Slide 2: Collaborators
Yuya Sakurai（NIMS）
Kazuki Ohishi（CROSS）
Hiroto Ota (Doshisya Univ.)
Jun Sugiyama（CROSS）
ISIS Neutron and muon
Rutherford Appleton labs.
Peter Baker （ISIS, U.K.）
Martin Månsson (KTH, Sweden)
16th International Conference on Muon Spin Rotation, Relaxation and Resonance (μSR2025)

## Slide 3
The Green Technologies of Excellence (GteX) Program
The GteX program aims to contribute to the realization of GX (Green transformation)
from the perspective of creating innovative technology seeds and nurturing human resources
by supporting R&D and human resource development at universities
and national institutes, etc.,
making the most of the high potential and accumulation
of basic research capabilities in academia in Japan.
There are storage battery, hydrogen and biomanufacturing areas:
Development of Sodium-Ion Batteries Free from Resource Constraints
Study of Na-ion batteries with muon beam PI: Izumi Umegaki
KEK Long-term S2-type proposal (2024MS01)
https://www.jst.go.jp/gtex/en/overview/index.html
16th International Conference on Muon Spin Rotation, Relaxation and Resonance (μSR2025)

## Slide 4
2009
2025
15th mSR conf.
Italy
2019
First publication (2009)
by Dr. J. Sugiyama
First publication on
operando experiment (2022)
by Dr. K. Ohishi
Grant approved
(2023)
14th mSR conf.
Sapporo
join (2012)
Ti cell
for mSR
Operando mSR cell
History
16th International Conference on Muon Spin Rotation, Relaxation and Resonance (μSR2025)
13th mSR conf.
Switzerland
16th mSR conf.
Canada
2017
2021
2013
2014
2022

## Slide 5
Our group and activity
16th International Conference on Muon Spin Rotation, Relaxation and Resonance (μSR2025)
Prof. Komaba
PI of GteX program
Pressure exp. at PSI
Collaboration with theorists
Collaboration with ISIS
Prof. Sugino
At J-PARC

## Slide 6
Li+
x
radius d=10 mm
average distance <x>2
(a)
(b)
DLi indicates an intrinsic physical property
related to battery performance
Diffusion coefficient DLi >10-11cm2/s
Time for Li+ to achieve the center of the material < 10 mins.
Time(mins.)
Active cathode material
Electrolyte
Rechargeable battery for EV
requires fast-charging.
⇒Diffusion coefficient
How fast Li ion moves in the material
Diffusion coefficient
16th International Conference on Muon Spin Rotation, Relaxation and Resonance (μSR2025)

## Slide 7
J. Sugiyama, JPSJ 82, SA023 (2013).
Electrochemical Method
・independent of reaction area
・independent of condition of battery
・intrinsic property of material
NMR
・relatively small effect
from magnetic elements
Neutron（QENS）
・slower but suitable time window
for diffusion in a battery material
Advantage of mSR to observe ion diffusion
Compared with…
16th International Conference on Muon Spin Rotation, Relaxation and Resonance (μSR2025)

## Slide 8
Cathode materials LiCrO2 and NaCrO2
S. Komaba et al., Electrochemistry Communications, 12, 3, (2010) 355-358.
LiCrO2 and NaCrO2 share the same crystal structure. NaCrO2 has a large charge capacity, while LiCrO2 is inactive.
16th International Conference on Muon Spin Rotation, Relaxation and Resonance (μSR2025)

## Slide 9: Na ion diffusion by mSR
Na ion diffusion in cathode materials were measured by mSR and
its result are consistent with the ones obtained by Na-NMR.
16th International Conference on Muon Spin Rotation, Relaxation and Resonance (μSR2025)

## Slide 10
NaCrO2 powder Ti holder φ26 mm,1 mmt Ti window Gold O-ring
LiCrO2 powder Ti holder φ26 mm, 1 mmt Ti window Gold O-ring
Samples
16th International Conference on Muon Spin Rotation, Relaxation and Resonance (μSR2025)

## Slide 11
m3
m2
m1
→m1（0, 0, 0.2425）
→m2（0.03585, 0.07170, 0.41276）
→m3（0, 0, 0.27716）
基準
-6.71829725 eV
Stable
-0.73230285 eV
NaCrO2
m1（0, 0, 0.115）
m2（0.120, 0.240, 0.4050）
m3（0, 0, 0.300）
Na
Cr
O
16th International Conference on Muon Spin Rotation, Relaxation and Resonance (μSR2025)
Muon stopping site
Colomb potential
energy

## Slide 12
Muon stopping site
m3
m2
m1
m1（0, 0, 0.2425）
m2（0.03585, 0.07170, 0.41276）
m3（0, 0, 0.27716）
基準
-6.71829725 eV
Stable
-0.73230285 eV
NaCrO2
1.278 Oe
1.775 Oe
2.025 Oe
Na
Cr
O
16th International Conference on Muon Spin Rotation, Relaxation and Resonance (μSR2025)
Colomb potential
energy
Field distribution widthΔ

## Slide 13
LiCrO2
m3
m2
m1
基準
→m1（0, 0, 0.20325）
→m2（0.15980, 0.08285, 0.13072）
→m3（0, 0, 0.38299）
-9. 2395 eV
Stable
-0.3291 eV
m1（0, 0, 0.180）
m2（0.24667, 0.12333, 0.12333）
m3（0, 0, 0.3950）
Li
Cr
O
Muon stopping site
16th International Conference on Muon Spin Rotation, Relaxation and Resonance (μSR2025)
Colomb potential
energy

## Slide 14
LiCrO2
m3
m2
m1
基準
Colomb potential
energy
m1（0, 0, 0.20325）
m2（0.15980, 0.08285, 0.13072）
m3（0, 0, 0.38299）
-9. 2395 eV
Stable
-0.3291 eV
Li
Cr
O
3.460 Oe
3.457-3.489 Oe
Field distribution widthΔ
2.358 Oe
Muon stopping site
16th International Conference on Muon Spin Rotation, Relaxation and Resonance (μSR2025)

## Slide 15
16th International Conference on Muon Spin Rotation, Relaxation and Resonance (μSR2025)
Self-trapping and potential energy
Putting m moves the closest Li ions away.
The potential energy at the muon site is lower by ~ 2 eV
than that around m, which indicates that m is stable.
Before
After

## Slide 16
16th International Conference on Muon Spin Rotation, Relaxation and Resonance (μSR2025)
0
5
10
15
TIME (ms)
0
5
10
15
TIME (ms)
mSR measurements on NaCrO2
Temperature dependence of spectra
A0P(t)=AKTGDKT(D,n,H,t) exp(-lKTt)+ AFexp(-lFt) +ABG
With increasing temperatures,
mSR spectra become dynamic
ZF mSR spectrum is decoupled with LF=10G
 magnetic field that m feels 〜 10 G

## Slide 17
16th International Conference on Muon Spin Rotation, Relaxation and Resonance (μSR2025)
mSR measurements on NaCrO2
With increasing temperature,
Field fluctuation rate n increases
above 250 K
Activation energy E= 0.130 eV
A0P(t)=AKTGDKT(D,n,H,t) exp(-lKTt)+ AFexp(-lFt) +ABG

## Slide 18
A0P(t)=AKT1GDKT(D1,n,H,t) + AKT2GDKT(D2,n,H,t) +ABG
mSR measurements on LiCrO2
Temperature dependence of spectra
16th International Conference on Muon Spin Rotation, Relaxation and Resonance (μSR2025)
0
5
10
15
0
5
10
15
TIME (ms)
TIME (ms)
With increasing temperatures,
mSR spectra become dynamic
ZF mSR spectrum is decoupled with LF=10G
 magnetic field that m feels 〜 10 G

## Slide 19
With increasing temperature,
Field fluctuation rate n increases a little
Activation energy E= 0.091 eV
n behavior at low temperatures is considered to be related to magnetic properties
Not only dipole but quadrupole interaction between m-Li may explain
16th International Conference on Muon Spin Rotation, Relaxation and Resonance (μSR2025)
mSR measurements on LiCrO2
A0P(t)=AKT1GDKT(D1,n,H,t) + AKT2GDKT(D2,n,H,t) +ABG

## Slide 20
16th International Conference on Muon Spin Rotation, Relaxation and Resonance (μSR2025)
Comparison with LiCrO2 and NaCrO2
0
100
200
500
TEMPERATURE (K)
300
400
0
100
200
TEMPERATURE (K)
300
400
 | LiCrO2 | NaCrO2
Distance between CrO2 | 0.256 nm | 0.315 nm
Charge capacity | < 20 mAh/g | 120 mAh/g
n at 350 K | 0.2 ms-1 | 1 ms-1
DJ at 350 K (10-9) cm2/s | 0.025 | 0.2
Activation Energy | 0.091 eV | 0.13 eV
DNa > DLi. above 250 K
The diffusive nature observed in LiCrO2 was strongly suppressed compared to that of NaCrO2.
This difference is consistent with the difference in electrochemical properties between LiCrO2 and NaCrO2.

## Slide 21
16th International Conference on Muon Spin Rotation, Relaxation and Resonance (μSR2025)
Comparison between
experiment D and simulated D
In these battery materials, Dexp/Dmin is lower than 80%.
As a result, muons is stable thanks to self-trapping effect.
The stability of muon can be represented by Dexp/Dmin.
Muon diffusion
is reported

## Slide 22
Conclusion
Cathode materials LiCrO2 and NaCrO2 share the same crystal structure. However, LiCrO2 is inactive, while NaCrO2 has a large charge capacity.
We performed mSR measurements with powder samples of LiCrO2 and NaCrO2 at EMU, ISIS. As a result, both show dynamic behavior above 250 K. We observed that Li diffusion in LiCrO2 is strongly suppressed. Even at x=1, Li hardly diffuses in LiCrO2. The composition dependence of Li diffusion / Na diffusion is planed at J-PARC with an operando cell soon.
The difference between DJ is most likely related to the distance between CrO6 plane and ionic radius. We also performed mSR measurements under pressure at GPD, PSI.
This research was supported by GteX(Green Technologies of Excellence) JPMJGX23S4.
16th International Conference on Muon Spin Rotation, Relaxation and Resonance (μSR2025)

## Slide 23
Thank you for your attention.
16th International Conference on Muon Spin Rotation, Relaxation and Resonance (μSR2025)