## Slide 1: Towards Fluctuating Magnetism in Zn-doped Averievite
Gediminas Simutis
Laboratory for Neutron and Muon Instrumentation
PSI Center for Neutron and Muon Sciences
24 July 2025
Towards Fluctuating Magnetism in Zn-doped Averievite
Gediminas Simutis
Laboratory for Neutron and Muon Instrumentation
PSI Center for Neutron and Muon Sciences
airpano.com/360video/video-kamchatka-volcano-plosky-tolbachik

## Slide 2
Lara Suarez-Garcia Madeleine Georgopoulou Fabrice Bert Philippe Mendels

## Slide 3
T/J
1/S, 1/z, 1/D, frustration
Bethe (1931)
Néel (1932)
Landau (1933)
Anderson (1952)
Mermin and Wagner (1966)
Chakravarty et al., (1989)
Chubukov et al., (1994)
Balents (2010)
Savary and Balents (2016)
Broholm et al., (2020)
Unconventional magnetic states

## Slide 4
Energetics and connectivity

## Slide 5
Energetics and connectivity

## Slide 6
Energetics and connectivity

## Slide 7
Triangular lattice has Neel state with reduced (40%) ordered moment
Kagome is expected to have no ordered moment
Many subsequent theoretical reports about absence of order in the Kagome lattice
Numerics

## Slide 8
S = ½ on a Kagome – The only isotropic NN model for QSL
What type of QSL?
Theory:
No exact solution
Many states near in Energy
VMC gapless
Many other methods - gapped
Depends on how the problem is truncated
Tensor Network Wavefunctions truncate the Ansatz wavefunctions and suggest gapless state
- How stable is it ? (DM, impurities, inter-layer, anisotropy) Truncation is hard:
Gapless spin liquids in disguise
Ferrari, Parola, Becca
PRB 103, 195140 (2021)
Experiments:
Few (any?) perfect lattices
Always DM present
Disorder…
Layer intermixing?
Herbertsmithite example
(..other materials emerge..)
?
What are the properties ?

## Slide 9
airpano.com/360video/video-kamchatka-volcano-plosky-tolbachik
Where are the materials?
> 100 new minerals from Tolbachik (Kamchatka) Eruptions: 1975, 2012 Averievite: Cu5V2O10(CsCl) (Dokl. Earth Sci. 359, 804 (1998))
Volcanoes as mineral forges

## Slide 10
airpano.com/360video/video-kamchatka-volcano-plosky-tolbachik
Where are the materials?
> 100 new minerals from Tolbachik (Kamchatka) Eruptions: 1975, 2012 Averievite: Cu5V2O10(CsCl) (Dokl. Earth Sci. 359, 804 (1998))
Synthetic versions: Towards Cu4Zn1V2O10(CsCl)
Botana et al., PRB 98 (2018)
Towards Cu3Zn2V2O10(CsCl) Georgopoulou et al., arXiv:2306.14739 using solid state reaction
Volcanoes as mineral forges

## Slide 11
Series of structural transitions for the parent compound
Low - > T distorted pyrochlore slab
Kagome plane sandwiched by two Cu2+ - V5+ honeycomb layers
Cu2+ - V5+ honeycomb layer
Cu2+ distorted kagome layer
Cs spacer
Cu2+ - V5+ honeycomb layer
Cu2+ distorted kagome layer
A.S. Botana et al., Phys. Rev. B 98 (2018)
M. Georgopoulou et al, ArXiv 2306.14739
Zn
Previous studies – parent compound
Magnetic order
TN = 24 K
qCW = 185 K

## Slide 12: Averievite: Cu5-xZnxV2O10(CsCl)
2-dimensionality
Kagome layers
Cu
Zn
V
Notes: - Kagome layer with copper, magnetic atom with spin ½ + 2 honeycomb layers in between, also with copper
- If we dope with Zn (non magnetic), it replaces Cu in interlayer, so we decouple Kagome layers + avoid problems with defects
- There were already studies up to x=1

## Slide 13: Averievite: Cu5-xZnxV2O10(CsCl)
T. Biesner et al., Phys. Rev. B 105 (2022)
A.S. Botana et al., Phys. Rev. B 98 (2018)
Notes: - Kagome layer with copper, magnetic atom with spin ½ + 2 honeycomb layers in between, also with copper
- If we dope with Zn (non magnetic), it replaces Cu in interlayer, so we decouple Kagome layers + avoid problems with defects
- There were already studies up to x=1

## Slide 14: Averievite: Cu5-xZnxV2O10(CsCl)
T. Biesner et al., Phys. Rev. B 105 (2022)
M. Georgopoulou et al, ArXiv 2306.14739
A.S. Botana et al., Phys. Rev. B 98 (2018)
When does the system become dynamic?
What are the ground states for different substitutions?
How do the ground states evolve?
-> muon experiments on Zn0, Zn1, Zn2
Notes: - Kagome layer with copper, magnetic atom with spin ½ + 2 honeycomb layers in between, also with copper
- If we dope with Zn (non magnetic), it replaces Cu in interlayer, so we decouple Kagome layers + avoid problems with defects
- There were already studies up to x=1

## Slide 15: Muon measurements – Zn0 case
Comparing with the neutron results
Magnetic order setting in at ~24 K Excitations can be modelled as spin waves (all powder measurements)

## Slide 16: Muon measurements – Further removal of copper from interlayers

## Slide 17: Muon measurements – Zn2
Gaussian + exponential relaxation components
If it were static, decoupling expected at ~100 G
Not the case! A dynamical state at T =0.28 K << J
ZF
LF

## Slide 18: Muon measurements – Zn2
Gaussian fraction
Gaussian relaxation
Exponential relaxation

## Slide 19: Muon measurements – Zn1

## Slide 20: Muon measurements – Zn1
Gaussian fraction
Gaussian relaxation
Exponential relaxation

## Slide 21: Muon measurements – Zn1 – a quasi-static state
Gaussian fraction
Gaussian relaxation
Exponential relaxation

## Slide 22: Comparing with neutron results
Zn1
Zn2
Zn0
Spin waves
Diffuse magnetic scattering
Magnetic fluctuations for
Q<0.3 Å-1 best seen for δE<0
B. Fak (1959-2024)

## Slide 23: Averievite – Cu5−xZnxV2O10(CsCl) - a new Kagome on the block!
Cu
V
Zn/Cu
From x=0 to 2, progressive decoupling between the kagome planes to reach a dynamic state
Two spacer layers available – better controlled decoupling
x= 2 averievite is a new experimental platform for the study of QSL
x = 1 averievite still has a transition to a mixed disordered frozen / fluctuating state (Tg=3.5 K) with likely a variety of environments (spin glass/fluctuating clusters?)
What next?:
Single crystal studies to understand the correlations Better understanding the muon response
Can Zn2 be externally tuned ?
Bonus:
Different to hydroxide compounds, potential for doping (theoretical proposals of Zn2+ -> Ga3+ and V5+ -> Ti4+)
8.4 A

## Slide 24: High-Pressure Workshop at PSI
https://indico.psi.ch/event/17608/
High pressure science using - muons - neutrons - X-rays - and other techniques
and technical developments

## Slide 25: Averievite – Cu5−xZnxV2O10(CsCl) - a new Kagome on the block!
Cu
V
Zn/Cu
From x=0 to 2, progressive decoupling between the kagome planes to reach a dynamic state
Two spacer layers available – better controlled decoupling
x= 2 averievite is a new experimental platform for the study of QSL
x = 1 averievite still has a transition to a mixed disordered frozen / fluctuating state (Tg=3.5 K) with likely a variety of environments (spin glass/fluctuating clusters?)
What next?:
Single crystal studies to understand the correlations Better understanding the muon response
Can Zn2 be externally tuned ?
Bonus:
Different to hydroxide compounds, potential for doping (theoretical proposals of Zn2+ -> Ga3+ and V5+ -> Ti4+)
8.4 A

## Slide 26: Towards Fluctuating Magnetism in Zn-doped Averievite
Gediminas Simutis
Laboratory for Neutron and Muon Instrumentation
PSI Center for Neutron and Muon Sciences
24 July 2025

## Slide 27
T. Biesner et al., Phys. Rev. B 105 (2022)
A.S. Botana et al., Phys. Rev. B 98 (2018) M. Georgopoulou et al, ArXiv 2306.14739

## Slide 28
(Zn1.86Cu0.14)(Cu2.85Zn0.15)(VO4) 2CsCl
Zn2 averievite
In the kagome plane, Cu has square planar coordination In the honeycomb planes, Cu is surrounded instead by five O with the short Cu-O apical bonds lying along the c axis
CF - in herbertsmithite element specific anomalous x-ray diffraction indicated
a 15% Cu occupancy of the interlayer site
and no site disorder on the kagome lattice

## Slide 29
(Zn1.86Cu0.14)(Cu2.85Zn0.15)(VO4) 2CsCl
Zn2 averievite
Herbertsmithite
(Zn0.85Cu0.15)(Cu3)(OH)6Cl 2
5.1 Å