## Slide 1: Contrasting in-plane and c-axis uniaxial stress effects on superconductivity and stripe order in La2-xBaxCuO4 (x = 0.125, 0.115)
Shams Sohel Islam
μSR 2025, 23 July 2025

## Slide 2
PSI Center for Neutron and Muon Sciences
Technische Universität Dresden
MPI, Stuttgart
Clifford Hicks
Sophia University
Brookhaven National Laboratory
John M. Tranquada
Genda Gu
Acknowledgements
Hubertus Luetkens
Jennifer Nadine Graham
Orion Gerguri
Petr Král
Jonas A. Krieger
Thomas J Hicken
Hrishikesh Gopakumar
Marek Bartkowiak
Markus Müller
Zurab Guguchia
Vahid Sazgari
Debarchan Das
Gediminas Simutis
Toni Shiroka
Rustem Khassanov
Mathias Elender
Alex Amato
Marc Janoschek
Ikuya Maetsu
Tadashi Adachi
Hans-Henning Klauss
Rajib Sarkar
Shreenanda Ghosh
Felix Brückner
Tsung-Dao Lee Institute
Vadim Grinenko
University of Zürich
Johan Chang
Julia Küspert
Tohoku University
Yoji Koike
DESY
Martin Von Zimmermann
Oleh Ivashko

## Slide 3
La2-xBaxCuO4 (LBCO) – rich phase diagram of Intertwined orders
Motivation – Uniaxial Strain study
Strain apparatus - μSR and ac susecptibility
Results
Conclusion
In-plane uniaxial stress effect on superconductivity, spin-stripe order and structural transitions in LBCO (x = 0.125)
Contrasting c-axis and in-plane uniaxial stress effects on superconductivity and stripe order in LBCO (x = 0.115)
Outline of the talk
S. S. Islam et. al., Commun. Phys. 8, 291 (2025)

## Slide 4
Complex phase diagram of HTSC La2-xBaxCuO4 (LBCO)
a
b
c
a
b
[1] Li et. al., Phys. Rev. Lett. 99, 067001 (2007).
[2] J. Tranquada et. al., Phys. Rev. B 78, 174529 (2008).
Onset of 2D SC correlations at
Tc,2D (Tso),>>Tc,3D
Loss of inter-layer Josephson coupling between 2D SC layers
Origin?
[3] M. Hücker et. al., Phys. Rev. B 83, 104506 (2011).

## Slide 5
[1] E. Fradkin, S.A. Kivelson, J.M. Tranquada, Rev. Mod. Phys. 87, 457 (2015).
[2] E. Berg et. al., Phys. Rev. Lett. 99, 127003 (2007).
Theory of Intertwined Orders in High-T Superconductors
Prediction of 2D PDW SC order: SC pairing occurs along quasi-1D charge stripes.
The phase of the pair wave function alternates by π between neighboring charge stripes[1-2].
In adjacent CuO2 layers, anti-phase PDW states on orthogonal charge stripes frustrate the interlayer Josephson coupling[1-2]
Compatible with the suppressed uniform 3D SC, and 2D SC correlations.
The predicted phase modulation in the PDW state[4]
Schematic cartoon illustrating stripes in real-space[3]
[3] J.-S. Lee et. al., arXiv:2310.19907 (2023).
[4] D. F. Agterberg et. al., Ann. Rev. Cond. Matt. Phys. 11, 231 (2020).
Adapted from [3]
Adapted from [1]
Question
What governs the interplay between such intertwined orders?
How to Study them?

## Slide 6
Study of intertwined orders and perturbative techniques
Hydrostatic Pressure
Uni-axial stress
Anisotropic perturbation
Enabling the precise tuning of lattice parameters along specific crystallographic directions
External perturbation (Pressure)
Isotropic perturbation
Does not allow exploring anisotropic / direction dependent behaviors
controlled, continuous, reversible
M. Hücker et. al., Phys. Rev. Lett. 104, 057004 (2010).
Z. Guguchia et. al., Phys. Rev. Lett. 125, 097005 (2020).
Z. Guguchia et. al., Proc. Natl. Acd. Sci. U.S.A. 121, e2303423120 (2024).
L. Thomarat, et. al., Commun. Phys. 7, 271 (2024).
Motivation
What happens for x = 0.125 under in-plane stress ?
Can we establish a general (T-x) phase-diagram under stress ?
TCDW

## Slide 7
[1] C.W. Hicks et. al., JPS Conf. Proc. 21, 011040 (2018), [2] S. Ghosh et. al., Rev. Sci. Instrum. 91, 103902 (2020), [3] V. Grinenko et. al., Nature Physics 17, 748 (2021).
In-situ piezoelectric-driven uniaxial stress device for μSR
Core mechanism: The relative length of the actuators determines the fraction of the preload that is transferred to the sample.
(PSI-TU Dresden-MPI Stuttgart collaboration)
Bµ
Strain Gauges
AC Coil
Sample

## Slide 8
Piezoelectric-driven uniaxial stress device for μSR

## Slide 9
In-plane uniaxial stress effect on superconductivity, spin-stripe order in La1.875Ba0.125CuO4

## Slide 10
45o
45o
La1.875 Ba0.125 CuO4: Magnetic susceptibility under in-plane compression

## Slide 11
La1.875 Ba0.125 CuO4: Magnetic volume fraction under in-plane compression
Weak-TF μSR
Static spin-stripe order persist up to the highest applied uniaxial stress, but with reduced volume fraction.

## Slide 12
La1.875 Ba0.125 CuO4: Phase diagram under in-plane compression
Z. Guguchia et. al., Phys. Rev. Lett. 125, 097005 (2020).
Z. Guguchia et. al., Proc. Natl. Acd. Sci. U.S.A. 121, e2303423120 (2024).

## Slide 13: Resulting phase diagram of LBCO under uniaxial Compression
Copper
Oxygen
𝝈in-plane
0.25

## Slide 14
Contrasting c-axis and in-plane uniaxial stress effects on superconductivity and stripe order in La1.885Ba0.115CuO4
S. S. Islam et. al., Commun. Phys. 8, 291 (2025)

## Slide 15: Magnetic susceptibility under c-axis compression
c-axis compression:

## Slide 16: Weak-TF μSR under c-axis compression

## Slide 17
ZF-μSR under c-axis compression

## Slide 18: Contrasting effects of in-plane and c-axis compression on stripe order

## Slide 19: Robustness of stripe order under c-axis compression

## Slide 20
d-wave
d-wave
d-wave
d-wave
c-axis stress
d-wave
d-wave
In-plane stress
Inter-layer frustration of
Josephson coupling
lifts
promote
Physical Interpretation - contrasting in-plane and c-axis stress Effects
S. S. Islam et. al., Commun. Phys. 8, 291 (2025).
Z. Guguchia et. al., Proc. Natl. Acd. Sci. U.S.A. 121, e2303423120 (2024).
Z. Guguchia et. al., Phys. Rev. Lett. 125, 097005 (2020).

## Slide 21
Large-volume-fraction spin-stripe order is anti-correlated with 3D SC coherence.
An extremely low in-plane uniaxial stress of 0.1 GPa induces a dramatic rise in the onset of 3D superconductivity. These states are very finely balanced.
The onset temperatures of 3D superconductivity and spin-stripe order are very similar above critical pressure.
c-axis strain causes the reduction of Tc, has a negligible effect on the magnetic fraction and Tso.
Highly anisotropic strain response for both superconductivity and spin-stripe order.
This could suggest underlying pairing mechanism for 2D (PDW) and uniform 3D SC orders are essentially same.
Impose an important constraint on theoretical models!
Conclusion
Critical role of crystallographic anisotropy in governing competing electronic phases in LBCO.
S. S. Islam et. al., Commun. Phys. 8, 291 (2025)

## Slide 22
PSI Center for Neutron and Muon Sciences
Technische Universität Dresden
MPI, Stuttgart
Clifford Hicks
Sophia University
Brookhaven National Laboratory
John M. Tranquada
Genda Gu
Acknowledgements
Hubertus Luetkens
Jennifer Nadine Graham
Orion Gerguri
Petr Král
Jonas A. Krieger
Thomas J Hicken
Hrishikesh Gopakumar
Marek Bartkowiak
Markus Müller
Zurab Guguchia
Vahid Sazgari
Toni Shiroka
Rustem Khassanov
Debarchan Das
Mathias Elender
Alex Amato
Gediminas Simutis
Marc Janoschek
Ikuya Maetsu
Tadashi Adachi
Hans-henning Klauss
Rajib Sarkar
Shreenanda Ghosh
Felix Brückner
Tsung-Dao Lee Institute
Vadim Grinenko
University of Zürich
Johan Chang
Julia Küspert
Tohoku University
Yoji Koike
DESY
Martin Von Zimmermann
Oleh Ivashko
Thank you for your attention!

## Slide 23
LBCO: Transport measurements under in-plane stress

## Slide 24: In-plane uniaxial stress effect on the crystal structure of La2-xBaxCuO4 (x = 0.115)
Elastic X-ray scattering scans of the (020)o/(200)o Bragg peaks at several temperatures through the transition from the LTO phase to the LTT phase with coexistence of the two phases at intermediate temperatures.
Z. Guguchia et. al., Proc. Natl. Acd. Sci. U.S.A. 121, e2303423120 (2024).
LBCO Strain Research at LMU-PSI: An Overview

## Slide 25
Estimated Lattice Parameter Changes Under c-axis Compression
G. B. Salvetat et al., Elastic properties of La2​CuO4​, J. Phys.: Condens. Matter 5, 7543 (1993).

## Slide 26
Position of piezos during different modes

## Slide 27
[1] Li et. al., Phys. Rev. Lett. 99, 067001 (2007).
[2] Tranquada et. al., Phys. Rev. B 78, 174529 (2008).
Existence of 2D SC correlations, Tc,3D ≪ Tc,2D (Tso)
Evidence for unusual 2D superconducting correlations
Sharp drop in ρab at Tso
but no corresponding change in ρc.
 screening currents within the CuO2 planes  sensitive to Tc,2D  diamagnetic response onset at Tso.
La1.875Ba0.125CuO4
Loss of inter-layer Josephson coupling between 2D SC layers
Origin?
Taken from Ref. [2]
consistent with the onset of 2D SC correlations at Tso.
 screening currents between the CuO2planes  not sensitive to Tc,2D  no diamagnetic response onset Tso.

## Slide 28: In-plane uniaxial stress effect on Superconductivity and stripe order (x = 0.115)
Z. Guguchia et. al., Phys. Rev. Lett. 125, 097005 (2020).
LBCO Strain Research at LMU-PSI: An Overview

## Slide 29: In-plane uniaxial stress effect on La2-xBaxCuO4 (x = 0.115, 0.135)
45o
Z. Guguchia et. al., Proc. Natl. Acd. Sci. U.S.A. 121, e2303423120 (2024).
Static spin-stripe order persist up to the highest applied uniaxial stress, but with reduced volume fraction.
LBCO Strain Research at LMU-PSI: An Overview