## Slide 1
Field-orientation-dependent magnetic phases in GdRu2Si2 probed with muon-spin spectroscopy
Ben Huddart
µSR2025
B. M. Huddart et al., Phys. Rev. B 111, 054440 (2025)

## Slide 2
Durham University
Alberto Hernández-Melián
Tom Lancaster
University of Oxford
Stephen Blundell
University of Warwick
George Wood
Daniel Mayoh
Geetha Balakrishnan
Acknowledgements
Paul Scherrer Institut
Thomas Hicken
Zurab Guguchia
Chennan Wang
Jožef Stefan Institute
Matjaž Gomilšek

## Slide 3
Talk outline
GdRu2Si2 as a host of magnetic skyrmions
Establishing the nature of the muon stopping site in GdRu2Si2
Detection of magnetic phases using transverse-field µSR
Observing a transition between two distinct magnetic phases using zero-field µSR

## Slide 4
T. Lancaster, Contemp. Phys. 60, 246 (2019).
T. Kurumaji et al., Science 365, 914 (2019).
Skyrmion
SkL
Magnetic skyrmions
Topological objects, found in some chiral or polar magnetic materials.
Generally stabilized by Dzyaloshinskii-Moriya Interaction (DMI)  non-centrosymmetric systems
Proposed applications: Digital memory, spintronics, reservoir computing

## Slide 5
Gd2PdSi3
Skyrmion lattices in centrosymmetric systems
Gd3Ru4Al12
GdRu2Si2
T. Kurumaji et al., Science 365, 914 (2019)
M. Hirschberger et al., Nat. Commun. 10, 5831 (2019)

## Slide 6
Square SkL in GdRu2Si2
B – T phase diagram mapped out using magnetisation, longitudinal resistivity and hall resistivity
Find square skyrmion lattice using resonant elastic x-ray scattering
N. Khanh et al., Nat. Nanotechnol. 15, 444 (2020)

## Slide 7
Phase diagrams in GdRu2Si2
Different phase diagrams result for H ∥ [001] and H ∥ [100]
Magnetic structures identified from polarisation analysis of resonant x-ray scattering
N. D. Khanh et al., Adv. Sci. 9, 2105452 (2022)

## Slide 8
Muon stopping sites
Muon stopping sites calculated using the MuFinder program.
Find two crystallographically distinct sites, one ≈ 0.3 eV higher in energy.
Experiment suggests only one crystallographically distinct site.
B. M. Huddart et al., Comput. Phys. Commun., 108488 (2022)
https://gitlab.com/BenHuddart/mufinder

## Slide 9
Energy barriers and zero-point energy
ZPE2
ZPE1
Estimate zero-point energy of the muon at each site
using phonon calculations and the harmonic approximation.

## Slide 10
Energy barriers and zero-point energy
Energy barriers obtained using nudged elastic band method.

## Slide 11
Energy barriers and zero-point energy
Energy barriers obtained using nudged elastic band method.

## Slide 12
Energy barriers and zero-point energy
Energy barriers obtained using nudged elastic band method.

## Slide 13
Experimental verification of muon site
Muon Knight shift

## Slide 14
Experimental verification of muon site
Muon Knight shift

## Slide 15
Experimental verification of muon site
Muon Knight shift

## Slide 16
Muon Knight shift – hyperfine contribution
Muon Knight shift is less positive (more negative) than one would expect from dipolar contribution alone
Data also suggest a significant negative contact hyperfine interaction between muon and spin polarised conduction electrons
 Evidence for RKKY interactions.

## Slide 17
Field along [001]
Field along [100]
Transverse-field µSR

## Slide 18
Can access field polarized state at high fields at this temperature.
Multiplicity of peaks for each field orientation is consistent with the muon stopping site.
Locations of the peaks requires a significant hyperfine field.
TF µSR at 40 K

## Slide 19
TF µSR at 5 K

## Slide 20
ZF µSR
Clear evidence for a transition between two distinct magnetically ordered phases.
G. D. A. Wood et al., Phys. Rev. B 107, L180402 (2023)

## Slide 21
ZF µSR - modelling
{Bi}
MuESR
+
SCA
P Bonfà et al., JPS Conf. Proc. 21, 11052 (2018)
G. Allodi and R. De Renzi, Phys. Scr. 89, 115201 (2014)

## Slide 22
ZF µSR - modelling
PND proposed three possible structures for higher-T phase, µSR spectra most consistent with sinusoidal structure with moments along [011].
µSR parameters
material parameters
µGd
f

## Slide 23
Summary
The muon stopping state in GdRu2Si2 has been calculated using DFT and confirmed experimentally using angular dependent measurements if the muon Knight shift, which also suggest the existence of RKKY-driven muon hyperfine coupling.
The magnetic phases in this system are distinguished via their distinct muon response, which are compared with simulations based on candidate magnetic structures.
Zero-field µSR provides clear evidence for a transition between two distinct magnetically-ordered phases at 39 K.