## Slide 1: Observation of charge carrier manipulation with nm depth-resolution at semiconductor-oxide interfaces
Thomas Prokscha
mSR2025, St. John’s, Canada, 24 July 2025

## Slide 2
Page 2
Why is this interesting? Controlled manipulation of charge carrier concentration in nanometer-thin layers is the basis of current semiconductor technology. Usually, macroscopic transport measurements and modeling are used to determine charge carrier profiles across interfaces – however, depth resolution is limited to tens of nm or even > 100 nm.
In the attempt to build more energy-efficient devices the understanding of the characteristics of semiconductor interfaces with nanometer depth resolution is of prime importance.
The formation and spin-depolarization of muonium is sensitive to the presence of free charge carriers and defects.
Muonium as a tool to characterize semiconductor interfaces
Notes: 2

## Slide 3
Page 3
Why is this interesting?
Low-energy m+SR (1-30 keV, mean depths 5-200nm) as a local probe technique with nm depth resolution can provide hitherto unaccessible direct information about carrier/defect profiles and dynamics at semiconductor surfaces and interfaces (e.g., metal-oxide-semiconductor MOS structures, pn-junctions).
Here: use the SiO2/Si and SiO2/4H-SiC interfaces in a MOS structure as prototype systems to test the feasibility of detecting the variation of charge carrier concentrations at the interface by applying a gate bias to the MOS.
Application to technologically and scientifically relevant devices: solar cell structures (Coimbra team, Xiaojie Ni et al.), oxide-semiconductor interfaces in advanced power devices, quantum well structures etc.
Muonium as a tool to characterize semiconductor interfaces
Notes: 3

## Slide 4
Muonium Mu0 in Si: MuT0, MuBC0
nm: Larmor precession frequency of m+, 20.4 MHz at B = 0.15 T
θ: angle between Mu symmetry axis (<111> in Si) and applied magnetic field, 54.7o if B || <100>
High field limit:
@0.15 T, MuT0: n12 = 756.4 MHz, n34 = 1249.6 MHz (unobservable in LEM)
@0.15 T, MuBC0: n12 = 22.3 MHz, n34 = 57.0 MHz
MuT0
MuBC0
MuT0: isotropic, A = 2006 MHz, charge states MuT0, MuT-
MuBC0: anisotropic, A|| = 16.8 MHz, A = 92.6 MHz, charge states MuBC0, MuBC+
Notes: 4

## Slide 5
Muonium Mu0 in Si: MuT0, MuBC0
nm: Larmor precession frequency of m+, 20.4 MHz at B = 0.15 T
θ: angle between Mu symmetry axis (<111> in Si) and applied magnetic field, 54.7o if B || <100>
High field limit:
MuT0: isotropic, A = 2006 MHz, charge states MuT0, MuT-
MuBC0: anisotropic, A|| = 16.8 MHz, A = 92.6 MHz, charge states MuBC0, MuBC+
@0.15 T, MuT0: n12 = 756.4 MHz, n34 = 1249.6 MHz (unobservable in LEM)
@0.15 T, MuBC0: n12 = 22.3 MHz, n34 = 57.0 MHz
MuBC0
Notes: 5

## Slide 6
Page 6
m+SR in Si: MuBC as a sensitive probe for free charge carriers
In the presence of free electrons with concentration n,
spin-exchange with the bound electron in MuBC0 causes
fast depolarization of the muon spin:
B.D. Patterson, Rev. Mod. Phys. 60, 69 (1988).
If n > 1013 cm-3, l > 2 ms-1, n12 + n34 disappear
Here: Si n-doping 2x1017 cm-3
30 K: «carrier freeze-out», donors not ionized
50 K: n ~ 1016 cm-3, Mu lines disappeared
Notes: 6

## Slide 7
Observation of charge carrier manipulation in a Si-MOS
M. M. Martins et al., https://arxiv.org/abs/2405.18211
Bias voltage scan at 15.4 keV of Mu fraction FMu
Setup for “electric field low-energy mSR (EF-LEM)”
Notes: 7

## Slide 8
Observation of charge carrier manipulation in a Si-MOS
M. M. Martins et al., https://arxiv.org/abs/2405.18211
Fit of FMu data assuming a sharp transition from
FMu = 0, n >> 1013 cm-3
FMu = 0.2, n < 1013 cm-3
electron depletion region clearly visible
A.F.A.Simões,H.V.Alberto,et al., n, Rev. Sci. Instrum. 91, 023906 (2020)
M. Mendes Martins et al, J. Phys.: Conf. Ser. 2462, 012025 (2023)
Notes: 8

## Slide 9
Comparison with C-V measurements and TCAD simulations
M. M. Martins et al., https://arxiv.org/abs/2405.18211
Observations:
Good agreement in determination of WD
However, electron accumulation in the first 35 nm cannot be reproduced by C-V/TCAD measurements/simulation
Role of fixed positive charge in SiO2 not properly reproduced by C-V/ TCAD
C-V measurement at 300 K
Depletion width WD determined from C-V and EF-LEM
TCAD (Technology Computer-Aided Design) simulation based on C-V measurements
Notes: 9

## Slide 10
R. L. Lichti, et al., Phys. Rev. B 70, 165204 (2004)
M. E. Bathen, et al., J. Appl. Phys. 127, 085701 (2020)
4H-SiC
in AB to Si(k),
at ABC,
(missing fraction in LEM)
Muonium complexes in 4H-SiC, annealing effects
Diamagnetic fraction FD
In SiC: FD ↑ due to Mu- formation
n ≳ 1×1016 cm-3
Annealing in NO at 1300℃ introduces N which acts as donor.
ND=1017 cm−3
Name | ND (cm−3) | Annealing process
N15-1300x | 2.6 × 1015 | no annealing
N15-1300NO | 2.6 × 1015 | 1300 ◦C in NO
N17-1300NO | 1.0 × 1017 | 1300 ◦C in NO
Notes: In Si, we will focus on the BC state. MuBC0 ionizes a
In 4H-SiC: Mu0 in AB to Si(k)
Which is also likely to be acceptor.

## Slide 11: Results N15-1300x, T = 260 K
Courtesy: Maria Martins

## Slide 12: Accumulation: N15-1300NO vs N15-1300x, T = 260 K
↑ FD due to the presence of electrically active N near SiO2/SiC interface.
Good agreement between saturation voltage of FD and C-V.
Courtesy: Maria Martins

## Slide 13: Results N15-1300NO, T = 260 K
Courtesy: Maria Martins
10-20 nm near the interface are affected by the electron concentration increase in accumulation condition.
Applied bias does not affect FD formation further from the interface.

## Slide 14: Results N17-1300NO, T = 260 K
Courtesy: Maria Martins
A.F.A.Simões,H.V.Alberto,et al., n, Rev. Sci. Instrum. 91, 023906 (2020)
M. Mendes Martins et al, J. Phys.: Conf. Ser. 2462, 012025 (2023)

## Slide 15: Summary
Electric-Field low-energy-mSR (EF-LEM) is a novel extension to LE-mSR to study semiconductor interfaces with nanometer depth resolution under applied electric bias
In Si- and 4H-SiC-MOS structures, the final state of muonium is affected by the applied gate bias, providing information about charge carrier accumulation/depletion profiles with unprecedented depth resolution
The observed band-bending conditions – with increased precision around the oxide-semiconductor interface – agree with C-V measurements
In SiO2/Si, an unexpected electron accumulation was observed in a 30-nm-wide region at the oxide interface, which cannot be reproduced by TCAD simulations
In 4H-SiC, the observed “induced electron accumulation” as a function of depth confirms the unintentional N doping caused by post-oxidation-annealing in NO

## Slide 16: LE-mSR publications related to defects, charge carrier profiles and band bending in semiconductors
M. Martins et al., https://arxiv.org/abs/2405.18211
P. Kumar et al., Materials Science in Semiconductor Processing 174, 108241 (2024)
M. Martins et al., Advanced Materials Interfaces 10, 2300209 (2023)
P. Kumar et al., Physical Review Applied 19, 054025 (2023)
P. Kumar et al., Materials Science Forum 1062, 315 (2022)
H. Alberto et al., Advanced Materials Interfaces 9, 2200374 (2022)
J. Woerle et al., Materials Science Forum 1004, 581 (2020)
J. Woerle et al., Physical Review Applied 14, 054053 (2020)
T. Prokscha et al., Physical Review Applied 14, 014098 (2020)
M. Curado et al., Applied Materials Today 21, 100867 (2020)
J. Woerle et al., Physical Review B 100, 115202 (2019)
H. Alberto et al., Physical Review Materials 2, 025402 (2018)
T. Prokscha, Journal of Physics: Conference Series 551, 012049 (2014)
T. Prokscha et al., Physical Review B 90, 235303 (2014)
T. Prokscha et al, Scientific Reports 3, 2569 (2013)

## Slide 17: Acknowledgement
Maria Mendes Martins (PSI/ETH Zürich)
Zaher Salman (PSI)
Marianne Bathen (U Oslo/ETH Zürich)
Piyush Kumar (ETH Zürich)
Ulrike Grossner (ETH Zürich)
Funding:
SNSF grant number 192218
ETH Zürich Postdoctoral Fellowship
Thank you for your attention!

## Slide 18: Muon signal in SiO2 and 4H-SiC at 0.7 mT
M. Mendes Martins, et al., Adv. Mater. Interfaces, 10, 2300209 (2023)
Courtesy: Maria Martins