## Slide 1
Time-Reversal Symmetry Breaking Superconductivity in HfRhGe:
A Noncentrosymmetric Weyl Semimetal
Adrian Hillier
ISIS Neutron and Muon source, STFC, UK

## Slide 2: Unconventional superconductors
Photo: commons.wikimedia.org
Photo: Kenneth G. Libbrecht, snowflakes.com
‘Unconventional’ superconductors:
HTSC, Sr2RuO4, PrOs4Sb12, (UTh)Be13 , ...
May exhibit non-phonon mediated superconductivity
Photo: Eddie Hui-Bon-Hoa, www.shiromi.com
Notes: 2
Part 1 Crystal symmetry image one shows water where no sysmmetries are broken: image2 shows ice where point symmetry is broken
Part 2 Gauge symmetry if this was not broken then you wouldn’t get Meissner effect
Part 3 Rotational and Time reversal – this give a definition of unconventional superconductors (but not necessary non-BCS ) as Time and Rotational are not broken

## Slide 3: Noncentrosymmetric superconductors
Antisymmetric spin-orbit coupling
The lack of inversion centre introduces an antisymmetric spin-orbit coupling (ASOC)
This ASOC lifts the spin degeneracy of Fermi surface
New J. Phys. 11 055054 (2009)
E. Bauer et. al, Springer-Verlag, Heidelberg, (2012)
Antiparallel spin pair
ASOC
(E )
kx
ky
kz
kx
ky
kz

## Slide 4: Noncentrosymmetric superconductors
Singlet pair
Triplet pair
Non-degenerate Fermi surface
Conventional s-wave
Li2Pd3B
Triplet, and nodes
Li2Pt3B
ASOC
Admixed singlet-triplet pairing
In the presence of ASOC, the electrons constituting the Cooper pair can be formed from different Fermi surfaces
An admixed singlet-triplet pairing is possible with mixing ratio determined by strength of ASOC
Nodes in the superconducting gap
Upper critical field exceeding Pauli limit
Broken time reversal symmetry but only a few!
Presence of strong SOC alone is not the reason behind this phenomenon
As some of these materials display properties of fully gapped conventional BCS-type
AIP Conf. Proc. 850, 633–634 (2006)

## Slide 5: Weyl Semimetal superconductors
Weyl semimetals are a special class of topological quantum materials
Non-centrosymmetric Weyl superconducting semimetals lead to non-trivial Berry curvature
Momentum-independent pairing
topological superconductivity
Interplay of:
Crystal Symmetry
Electronic Structure
Spin orbit coupling
Those that break time reversal symmetry
Intrinsic superconducting diode effect
Possible Quantum electronics
Yan Annu. Rev. Condens. Matter Phys. 8:337

## Slide 6: HfRhGe: Crystal Properties
Hexagonal P62m
  Noncentrosymmetric,
  Point group, D3h
Confirmed from Xray Diffraction Rietveld refinement
Adv. Mater. 2025, 37, 2415721
_

## Slide 7: HfRhGe: Superconducting Properties
Tc ≈ 1.7 K
Verified by magnetization, resistivity and specific heat
Full diamagnetic screening
Specific Heat Analysis
Fully gapped BCS-type behavior
ΔC/γnTc = 1.46, Δ₀/kBTc = 1.70(5)
Adv. Mater. 2025, 37, 2415721

## Slide 8: Electronic Structure & Topology
Strong antisymmetric SOC (ΔE ~ 100 meV)
Multiband nature (Hf-5d, Rh-4d, Ge-4p)
Fermi surfaces of HfRhGe show no nodes
Multiple Weyl Points
Adv. Mater. 2025, 37, 2415721

## Slide 9: TF Muon Results
A representative asymmetry spectra collected above and below Tc at different applied fields
Since the upper critical field of HfRhGe is low
Transverse field measurements were performed at different applied field 100 Oe, 200 Oe, 300 Oe and 400 Oe
Temperature and field dependence was obtained
Adv. Mater. 2025, 37, 2415721

## Slide 10: TF Muon Results
Adv. Mater. 2025, 37, 2415721
The contribution from FLL was extracted and the σ(H) were found from isothermal cuts and fitted with the following equation
Temperature-dependent inverse square penetration depth shows a fully gapped isotropic s-wave state
Gap value: Δ₀ = 0.26(1) meV → Δ₀/kBTc = 1.77
Remarkable agreement with Heat Capacity 1.70(5)

## Slide 11: ZF Muon Spin relaxation
ZF– μSR spectra show a distinct difference between spectra collected below and above Tc
LF – μSR, decoupling in a weak field
Data were fitted with a Gaussian Kubo-Toyabe function with electronic relaxation rate and a background asymmetry ABG
Adv. Mater. 2025, 37, 2415721

## Slide 12: ZF Muon Spin relaxation
Onset of spontaneous fields below Tc
Temperature-independent nuclear depolarization rate (Δ)
Electronic relaxation rate (Λ) increases with reducing temperature, indicating time reversal symmetry breaking
Internal field Bint ≈ 0.15 G
Adv. Mater. 2025, 37, 2415721

## Slide 13: Principle Component Analysis
Model independent Analysis
Clear transition observed
Adv. Mater. 2025, 37, 2415721

## Slide 14: Symmetry Analysis
HfRhGe – D3h point group
Irreducible Representation
Four 1-D
Two 2-D
Taking Ginzburg-Landau free energy
Only two symmetries allowed
Adv. Mater. 2025, 37, 2415721

## Slide 15: Superconducting order parameter
Assuming Strong SOC
E’
Singlet Triplet
E’’
Singlet Triplet
Note: d(1) and d(2) are non-unitary c.f. LaNiC2 and LaNiGa2
Non-Centrosymmetric with strong Spin Orbit Coupling allows mixed singlet and triplet
Adv. Mater. 2025, 37, 2415721

## Slide 16: Superconducting order parameter
Assuming Strong SOC
E’
Singlet Triplet
Gives Point Nodes: θ = 0 and π
E’’
Singlet Triplet
Gives Point Nodes: θ = 0, π/2, π
Umm… but experimental evidence strongly suggests fully gap s-wave
Adv. Mater. 2025, 37, 2415721

## Slide 17: Reconciling Theory and experimental
Electronic band structure calculations suggest multi-band nature
A loop supercurrent order mechanism is proposed
Needs several symmetry related sites
Can explain Time reversal symmetry breaking
Gives real space pairing –Singlet!
Adv. Mater. 2025, 37, 2415721

## Slide 18: Conclusions
HfRhGe is a rare example of a noncentrosymmetric Weyl semimetal that exhibits:
Bulk superconductivity with a fully gapped, weak-coupling s-wave gap
Spontaneous time-reversal symmetry breaking (TRSB) below Tc, confirmed via ZF-μSR
Symmetry analysis rules out conventional TRSB states (singlet/triplet/mixed), which are nodal, contradicting the observed isotropic gap
Combining Theory and Experiments supports a loop supercurrent state, a multiband, TRSB superconducting state with internal Josephson currents but no gap nodes
The coexistence of
Topological Weyl nodes
TRSB superconductivity
Positions HfRhGe as a compelling platform for topological superconductivity and intrinsic superconducting diode effect (SDE)
Future work: High-quality single crystals, directional transport measurements, and phase-sensitive probes will be crucial to uncover nonreciprocal effects and fully map the topological SC state
Adv. Mater. 2025, 37, 2415721

## Slide 19: Acknowledgments
Funding: SERB (India), UGC, (Government of India), IIT Kanpur Andromeda server and STFC for beamtime
Sajilesh. K. P., Roshan Kumar Kushwaha, Dibyendu Samanta, Pavan Kumar Meena, Shashank Srivastava, Deepak Singh, Ravi Prakash Singh
IISER Bhopal, India
Tymoteusz Tula,
Université de Sherbrooke, Canada
Amit Kanigel,
Technion-Israel Institute of Technology
Sudeep Kumar Ghosh
Indian Institute of Technology

## Slide 21: Electronic Structure & Topology
• Topological Features:
Multiple Weyl points (positive (red dots)/negative (blue dots) chirality) in BZ
Surface Fermi arcs on (001), (100), and (110) planes
Surface energy spectra at the constant energy = – 0.216 eV projected onto the (001) and (110) surface Brillouin zones. Here, k11 denotes the direction along the ky = −kx line
Adv. Mater. 2025, 37, 2415721

## Slide 22
Maximally localized Wannier functions (MLWFs) were computed for a precise representation of electronic structure, using WANNIER90 package.
Using these MLWFs, the Fermi surfaces were calculated for six bands crossing the fermi energy, and side views of these fermi surface sheets with SOC are shown in the Fig1.
Further the surface state projections onto (001), (100), (110), were calculated using WANNIER TOOLS package.
Fig1.
Fig2.
Fig3.
The surface spectrum of HfRhGe, projected onto (100) along high symmetry points, is shown in Fig 2a., while constant energy (0.022eV) Fermi arcs projected on (001) and (100) surfaces are shown in Fig2b and Fig2c respectively.
Figure 3a. illustrates the energy dispersion on (110) surface Brillouin zone while constant energy fermi arcs at -0.07 eV and 0.14 eV are shown in Figure 3b and Figure 3c respectively.