## Slide 1: Anomalous magnetism in NiI2: how structure affects dynamics
Theo Breeze
SR2025, St John’s, Canada
T.L. Breeze et al. Phys. Rev. B 111, 104420 (2025)

## Slide 2: Acknowledgements
  Durham:
  Prof. Tom Lancaster
  Prof. Stewart Clark
  Nathan Bentley
  Southampton:
  Dr Alberto Hernández-Melián
  Oxford:
  Dr Benjamin Huddart
  ISIS:
  Dr George Wood
  Dr John Wilkinson
  Dr Francis Pratt
  PSI:
  Dr Thomas Hicken
  Warwick:
  Dr Daniel Mayoh
  Prof. Geetha Balakrishnan

## Slide 3: Material overview
  NiI2 is a magnetic Van der Waals material
  Proposed to host a novel form of skyrmion phase in the 2D limit
  We were interested in probing bulk magnetic behaviour around the 2 magnetic transitions
D. Amoroso, P. Barone, and S. Picozzi, Nat. Commun. 11, 5784 (2020).

## Slide 4: Bulk magnetism
  Two magnetic phase transitions at TN1=73 K, TN2=62 K
  Structural transition at TN2, from rhombohedral above to monoclinic below

## Slide 5: PSI data

## Slide 6: Muon site analysis

## Slide 7: Simulated Spectra
  Simulated ground state spectrum with good fit to single frequency of 117 MHz (0.867 T)
  Fitted , compare with in experiment

## Slide 8: ISIS data
  Behaviour of below TN2 consistent with a model for fluctuations from spin-wave excitation due to a single gapless magnon band
  D is effective dimensionality, s is exponent in spin-wave dispersion relation
  is consistent

## Slide 9: ISIS data
  Temperature-indepence above TN2 is inconsistent with this model, suggesting qualitatively different dynamics in this region

## Slide 10: Group theory analysis
  Structural shift at TN2, changing symmetry
  At Ni ion centre, structure has point group D3d above TN2, giving degenerate bands:
  Below TN2, structure has one of three low-symmetry point groups, lifting all orbital degeneracies