## Slide 1
- RIKEN Center for advanced photonics (RAP)
Neutron Beam Technology Team
T.Kobayashi Y. Otake Y. Ikeda
T. Fukuchi M. Mizuta Y. Wakabayashi S. Ohgo
Tokyo Science University
S. Ikeda N. Hayashizaki
Development of RANS-III for outdoor measurement

## Slide 2: RIKEN Accelerator-driven Neutron Systems (RANS)

## Slide 3: RIKEN Accelerator-driven compact Neutron Source RANS and RANS-II
15m, 25t
5m, 8t
RANS
RANS-II
RANS
2013～
RANS-II
2019～
7MeV-H+
Be Target
2.5MeV-H+
Li Target
Details are given by Yoshie Otake at session 6 invited talk

## Slide 4
4.2m
21m
RANS-II
RANS
RANS started operation (2013)
Dedicated building completed (2016.5)
Construction of RANS-II separation wall（2019.3.5）
RANS-II started operation（2019.7.22）
RANS-II operation space
4
RANS
operation room
15m

## Slide 5: RANS
7MeV LINAC
2.5MeV LINAC
Li target
with shielding(3.5t)
Be target
with shielding
(20t)
Neutron beam hole
Neutron beam hole
RANS-II
Replaceable beam collimator
1m
2m
5

## Slide 6
Be or Li target
H+ beam
Multi-layer shielding
Neutrons are stopped by Polyethylene (PE) and Boron Polyethylene (BPE)
Gamma rays are stopped by lead (Pb).
Reducing the lead in the outermost shell reduces the total weight
2m (RANS)
1m(RANS-II)
Neutron beam
Target and multilayered shield
Moderators
Polyethylene (for thermal neutrons)
He-cooled mesitylene (for cold neutrons)
Accelerator
（RANS, RANS-II common）
PE
BPE
Pb
Pb

## Slide 7
 | RANS | RANS-II
Operation started | 2013～ | 2019～
Accelerated particle | Proton | Proton
Acceleration energy | 7 MeV | 2.5MeV
Max. current (time averaged) | 100 μA | 100 μA
Ion source | Duo-plasmatron | ECR plasma
Accelerator (LINAC type) | RFQ + DTL (AccSys Technology Inc.) | RFQ (TIME Co., ltd.)
Reaction | 9Be(p,n)9B | 7Li(p,n)7Be
Weight (Accelerator) | 5 t | 2.5 t
Weight (Shield) | 20 t | 3.5 t
Length (Accelerator+Shield) | 10 m | 5 m
Neutron energy | ～ 5 MeV | ～ 0.7 MeV
Neutron yield | ～ 1012 /sec | ～ 1011 /sec
RANS, RANS-II specification

## Slide 8: RANS, RANS-II experiments

## Slide 9
Neutron beamline
DTL
RFQ
IS
Visualization of water in corroded region
(Transmission Radiography) RANS
Properties in plastic deformation of metals
(Neutron diffraction) RANS
Detector and dosimeter development
RANS, RANS-II
Soundness analysis of reinforced concrete
(Transmission and backscatter imaging)
RANS, RANS-II
Salinity analysis in concrete (PGA)
RANS, RANS-μ（RI source）
IS
RFQ
Amplifier
Amplifier
Target
Target
Parameter study for the development of a portable onboard neutron source
RANS-II → Examination of conditions for the production of RANS-III
RANS
RANS-II
Hydrogen implantation for metals
RANS-II
Cold neutron source development
RANS
Prompt gamma and activation gamma imaging
RANS-II
Properties of soft materials
（SANS） RANS
RANS, RANS-II Latest Themes

## Slide 10: Safety Assessment of Aging Infrastructure and RANS-III Development

## Slide 11
Increased need for non-destructive testing of social infrastructure (aging and construction defects)
Water and salt penetration into concrete, voids and corrosion of reinforcing steel → Neutrons are effective for detection

## Slide 12
PASJ2019 第16回年会（京都市）口頭発表会場
PASJ2017 第14回年会（札幌市）懇親会場
PASJ2016 第13回年会（千葉市）懇親会場から
Asphalt
2nd
concrete
Neutron beam
3rd
concrete
PE or Acryl
Concrete
10 or 20mm
50 or 40mm
Asphalt
2nd
concrete
Void
Concrete
Neutron beam
10 or 20mm
50 or 40mm
50mm
60mm
3rd
concrete
60mm
60mm
60mm
50mm
RANS, RANS-II common issues (diagnosis of infrastructure deterioration)
Backscatter measurement of samples simulating actual deteriorated bridge road surface (bedding)
2D-analysis with backscattered neutron
Concrete+Asphalt
Sample
Details are given by Tomonori Fukuchi at Poster session 1

## Slide 13
Another key technology for infrastructure degradation diagnosis (under development at RANS and RANS-II)
concrete
Reinforcing bar
Measurement of salinity in concrete by gamma from chlorine
Neutron beam
γdetector
γdetector
Gamma rays generated by neutron irradiation inside concrete
Prompt gamma analysis (PGA)
Details are given by Yasuo Wakabayashi at session 10

## Slide 14
 | Energy [MeV] | Reaction | RF [MHz]
RANS | 7 | 9Be(p,n)9B | 425
RANS-II | 2.5 | 7Li(p,n)7Be | 200
RANS-III | 2.5 | 7Li(p,n)7Be | 500
RANS Wide range of uses from technology to science.
RANS-II Prototype for transportable use. For laboratory use.
RANS-III Transportable
Role of 3 RANS

## Slide 15
検出器
New tools for social implementation
RANS-III and RANS-m
252Cf source with bucket track
Specialized in salt damage analysis by prompt gamma analysis.
In operation by RANSVIEW inc. （2023）
https://ransview.co.jp/
RANS-III, a smaller version of RANS-II, is mounted on a trailer. The main purpose is to inspect roadbeds.
Details are given by Yasuo Wakabayashi at session 10

## Slide 16
RANS-III development
2370 mm
300 mm
330 mm
(RFQ)
RANS-III(500MHz)/RANS-II(200MHz)
Diameter 1/2
Weight 1/4
2019-2024 in lab.
RFQ
Bend mag.
Apr. 2024
ECR-IS
20cm
Truck loading

## Slide 17
Accelerator
Neutrons
Study for realization on-board （2023-24）
Considering the axle position and floor structure material, neutron generation position is moved to the rear of the trailer
Lightened target shielding with vertical drive mechanism
Separate compartments for cooling system and amplifier and heat removal performance
Amplifiers
Amplifiers
Chillers
Chillers
Proton beam
Accelerator
Shield &
Detector
Accelerator
I.S.
Amplifiers
Chillers
RANS-III development

## Slide 18
Lithium target
Shield(lead)
Shield(BPE)
Collimator（BPE）
Proton
Neutron
1110
RANS-III lightweight target shield
Accelerator
Neutron
Detector space

## Slide 19
RANS-III on-board installation
May 2024
Jun. 2024
Jul. 2024

## Slide 20
Construction of RANS-III test building
Neutron scattering measurements, Radiation levels and Shielding capabilities will be investigated.
Completed in Jan 2025

## Slide 21
RANS summary
RIKEN Accelerator-driven compact Neutron Sources RANS
15m
5m
4m
70cm
RANS: Fundamental Physics
Method Development
RANS-II: Portable study
Fast neutron
Backscattering
RANS-II is marketed by TIME Inc.
First delivery was made to Mirrotron Inc.
RANS-III: Demonstration of portability
RANS-μ:
Specializing in salt measurement
2023 Commencement of commercialization