## Slide 1: Tracking the progress of nonuniform deterioration in a lithium-ion battery using Bragg-edge imaging ~an application of the AISTANS compact neutron source~
Koichi Kino, Takeshi Fujiwara, Tatsunori Shibuya, Brian O’Rourke
National Institute of Advanced Industrial Science and Technology (AIST)
K.Kino: koichi.kino@aist.go.jp

## Slide 2
Motivation
  Previous research
  Technique “Bragg-edge imaging”
  Why experiment at CANS ?
Experiments at AISTANS
  Facility, Sample, Setup, and Measurements
Results
  Transmission spectra
  Recently obtained images
Conclusion
Contents

## Slide 3
１.Motivation Previous research (K.Kino et al.)
市販LIBセルを非破壊“ブラッグエッジイメージング”にて得た知見：
蓄電能力劣化LIBでは、負極材グラファイトへのLiイオンの挿入にcmオーダーの空間的非一様性
かつLiイオンの挿入度合いの異なる2つの結晶相(Li1.0C6、Li0.5C6) 間で非一様性の大きな違い
K.Kino et al.,
Appl. Phys. Express
15 (2022) 027005
Negative electrode (graphite) at charged state
Li1.0C6
Li0.5C6
＠J-PARC
Measurement time:
8 to 10 hours
per single sample state
LIB sample
photograph
X-ray CT
Neutron analyzing area
Fresh
Fatigue
Fresh
Fatigue
LiC6
LiC12
3.5-mm thick
Negative
electrode
tab
Positive
electrode
tab
Relation
to the tab
Streaky
structure
Number of Li-ion per pixel
Nonuniform degradation in cm-order size
Different uniformity between LiC6 and LiC12

## Slide 4
１.Motivation Bragg reflection and Lithium-ion battery
Application for Lithium-ion battery (LIB)
Analysis of electrodes nondestructively
example:
Graphite
Negative
electrode
Positive
electrode
Positive
electrode
Negative
electrode
example:
Lithium cobaltate
Carbon
Carbon
Li-ion
Li-ion
Li-ion
Oxygen
Oxygen
Cobalt
Cobalt
Electron
Electron
Current
Current
Charge
Discharge
Bragg reflection
Crystalline information
Bragg
condition
Interference
Crystalline structure etc.
Atom
neutron
Neutron detector

## Slide 5
１.Motivation Bragg-edge imaging with Lithium-ion battery
Bragg-edge imaging can provide images of charge/discharge.

## Slide 6
１.Motivation Questions left and Purpose
Where and how the deterioration begin ?
How does it proceed ?
Track the process of deterioration by Bragg-edge imaging at AISTANS

## Slide 7
１.Motivation Why experiment at CANS ?
Why at CANS (AISTANS)
Hard to do measurements periodically at large facilities (Huge number of proposals)
CANS
Flexibility of machine time
Easy to do measurements
Key for successful data at CANS
Neutron beam performance
Sharp pulse
  → Bragg-edge spectra
Sufficient flux
  → Measurement time
Neutron detector
High detection efficiency

## Slide 8
２.Experiments AISTANS
~30 m
Electron beam
First beam line
Second
Beam line
① Electron linear
accelerator
Neutron beam
~14 m
② Neutron
source
③ Neutron beam line
④ Neutron detector
AIST, Tsukuba, Japan
The whole components (①〜④) were optimized
High performance and Practical measurement time
Neutron beam
Electron beam
Neutron beam
Optimized for TOF-based Bragg-edge imaging

## Slide 9
２.Experiments Sample
50 mm
55 mm
50 mm
55 mm
Neutron
analysis
area
Photograph
X-ray CT
Sample
A commercial LIB cell for smart phone (Android)
Capacity: 2900 mA
Electrode tabs
Instrument for cyclic
charging-discharging
Constant temperature bath
LIB sample inside
In the same room of AISTANS

## Slide 10
２.Experiments Sample conditions at measurement
First measurement
8 hours for charged(4.2V) and discharged(2.7V) states
[Charge]
CCCV (constant current and voltage)
CC: rate 0.7C until 4.2 V
CV: keep 4.2 V until 100 mA
Temperature: 45℃
[Discharge]
CC (constant current)
CC: rate 1.0C until 2.7 V
Temperature: 45℃
Second measurement
8 hours for charged(4.2V) and discharged(2.7V) states
Third measurement
8 hours for charged(4.2V) state
92 cycles
＋108 cycles
Toal 92 cycles
Toal 200 cycles

## Slide 11
２.Experiments Experimental setup
100 mm
100 mm
2D neutron detector
(x,y,TOF)
Scintillator + multi-anode PMT
High detection efficiency and count rate
Neutron beam
Sample
2D neutron
detector
Around sample
L(Source-detector) = 8.1 m
Sample is 10 cm upstream from the detector.

## Slide 12
３.Results Transmission image
50 mm
55 mm
50 mm
55 mm
Neutron
analysis
area
Photograph
X-ray CT
Neutron
analysis
area
Transmission image obtained
in a broad neutron wavelength region
Shadow of the sample
55 mm
50 mm

## Slide 13
３.Results Counts and transmission spectra
92 cycles data
All pixels (50x55 mm)
Graphite
LiC12
LiC6
Li
Bragg-edges of negative electrodes were observed.
Sample
w/o sample
Graphite
Discharged
Charged
LiC12
LiC6
Discharged
Charged

## Slide 14
Charged
LiC12
LiC6
３.Results Bragg-edge analysis for negative electrode
Including reflections: Graphite 002, LiC6 001, and LiC12 002
Crystalline orientation in simulation: Isotropic
92 cycles data
1pixel (5x5 mm)
Spectra were fitted by the Bragg-edge curves.
Discharged
Graphite
Crystalline
density
Depth

## Slide 15
３.Results Images of negative-electrode crystal density
Graphite
LiC12
LiC6
50 mm
55 mm
Analysis area
Discharged
Charged
92 cycles
Discharged
Charged
200 cycles
Not yet meas-ured
Not yet meas-ured
Not yet meas-ured
No clear inhomogeneity even after 200 cycles.
Discharged
Charged
50 mm
55 mm
0 cycle

## Slide 16
３.Results Beginning of deterioration ?
LiC6 distributions
0 cycle
92 cycles
200 cycles
Uniform distribution even after 200 cycles
But LiC6 density distribution shifted to a smaller value

## Slide 17
４ Conclusion
Thank you for your kind attention !
Succeeded in Bragg-edge imaging of a LIB cell at AISTANS
We obtained the image which might suggest the beginning of deterioration.
We will continue periodical measurements and will try to reveal the origin and progression of the deterioration.