## Slide 1
Superconducting Tunnel Junction Radiation Detectors
Stephan Friedrich, LLNL
Outline
• Textbook case: “Standard” STJs
• Real life: “Non-standard” events cause artifacts
• What’s next?

## Slide 2
The Workhorse: Ta-Based STJs
For some of you, this is all you need to know.
• Small (~1 meV) gap D  High resolution (~1-2 eV)
• Short (~100 µs) life-time  Fast (>1 kcps per pixel)
Ta Al AlOx Al Ta
Ta Absorber
Si Substrate
Ta
Al
Al
• High efficiency  Thick, large gap absorber
• Fast tunneling  Thin, small gap trap
STJ Cross Section
STJ Operating Principle
Photon or 7Be
EF+DTa
EF–DTa
EF
Al2O3

## Slide 3
The Workhorse: Ta-Based STJs
For some of you, this is all you need to know.
• ~2eV FWHM is enough for BeEST experiment
• Interactions with Ta absorber affect spectral details
Ta Absorber
Si Substrate
Ta
Al
Al
• High efficiency  Thick, large gap absorber
• Fast tunneling  Thin, small gap trap
STJ Cross Section
The BeEST Experiment
Photon or 7Be
Al2O3
Ta-STJ

## Slide 4
The Alternative: Al-Based STJs
• Need thick Al absorber for high efficiency
 Slow tunneling  small signal  low resolution
STJ Cross Section
Al-STJ
Photon or 7Be
Al Absorber
Si Substrate
Al
Al2O3

## Slide 5
The Alternative: Al-Based STJs
With STJs from two materials, we are I think in pretty good shape.
• Need thick Al absorber for high efficiency
 Slow tunneling  small signal  low resolution
STJ Cross Section
Al-STJ Performance
• Not great, but good enough
• Can be improved (thinner barrier) if needed
Photon or 7Be
Al Absorber
Si Substrate
Al
Al2O3

## Slide 6
The Third Option: Nb-Based STJs
Nb Absorber
Si Substrate
Nb
Al
Al
• High efficiency  Thick, large gap absorber
• Fast tunneling  Thin, small gap trap
STJ Cross Section
Photon or 7Be
Al2O3
Nb-STJ
Possible reasons to develop Nb-STJs: 1) Yet another material. 2) Speed.

## Slide 7
The Third Option: Nb-Based STJs
Possible reasons to develop Nb-STJs: 1) Yet another material. 2) Speed.
Nb Absorber
Si Substrate
Nb
Al
Al
• High efficiency  Thick, large gap absorber
• Fast tunneling  Thin, small gap trap
STJ Cross Section
Photon or 7Be
• We do have good Nb-STJs from the 1990s
• Current Nb-STJs have (so far) lower resolution
Al2O3
1990’s Nb STJ Performance
[Friedrich 1998]
[Friedrich 2002]

## Slide 8
Events at “Non-Standard” Locations Cause Spectral Artifacts
Nb-STJ (1990s)
Edge
Wire
Surface Oxide
Via

Wire
Wire
above
STJ

Base layer
Absorber
Oxide
Wire above STJ
Wire
Si substrate
Wire
Surface Oxide
Artifacts are much worse in Nb-STJs where life-time is much shorter

## Slide 9
Artifacts (1): Line Splitting Due to Base Layer Events
Events in bottom electrode have different responses from top electrode.  Avoid
Remedies:
1) High-Z absorber (Nb  Ta)
2) Thick absorber (165  300nm  ?)
3) Low E implantation or low E photons
Top/bottom electrode
Top (absorber)
Bottom electrode
X-rays or 7Be

## Slide 10
Artifacts (2): Edge Events Can Produce Tails
Remedies:
1) Minimize edge area
2) Do not expose edge to radiation
(Si collimator or photoresist mask)
Top
X-rays or 7Be
Charge recombination in edge of base electrode causes tail.  Minimize!
Edge
Edge
Edge
Edge
Top (absorber)
Bottom electrode edge

## Slide 11
Artifacts (3): Wire on Top of STJ is Bad
Remedies:
1) Minimize insulator (SiO2  anodization)
2) Minimize wiring overlap
3) Do not expose edge to radiation
(Si collimator or photoresist mask)
Top
Top lead
X-rays or 7Be
Events in wiring have different responses.  Minimize!
Top (absorber)

## Slide 12
Artifacts (4): Surface Oxides are Bad (Native Ta2O5 Seems OK)
Residual SiO2 at surface produces broad background.  No SiO2!
Remedies:
1) No SiO2 on top of absorber
2) Native Ta2O3 seems ok
X-rays or 7Be
Surface SiO2

## Slide 13
Improved STJ Designs Minimize (but do not Fully Remove) Artifacts
Nb-STJs (1990s)
Ta-STJs (2020s)

Narrow edge
Small
wire
overlap


Narrow
contact
No SiO2
on surface

Wide edge

Wide
contact
Large
wire
overlap

Residual SiO2
on surface
SiO2
Anodization
Residual SiO2
Via

## Slide 14
Photoresist Masking Does Remove (Most) Artifacts
Ta-STJs (2020s)
Photoresist
mask
Ta-STJ 
Photoresist mask 
Removes all artifacts except those form e- escape.
e-
Ta-STJs with PR Mask

## Slide 15
Ta-STJs (2020s)
Photoresist
mask
One (out of 10) Ta-STJs with Ta Cap
Ta cap layer
Works! So far yield is small. (We know how to fix this.)
Capping Layer Suppresses Electron Escape

## Slide 16
Capping Layer Suppresses Electron Escape
Ta-STJs (2020s)
Ta cap layer
Works! So far yield is small. (We know how to fix this.)
One (out of 10) Ta-STJs with Ta Cap

## Slide 17
Ta-STJ Response Function
e-
e- escape tail
Tail in Low-E Response

## Slide 18
Ta-STJ Response Function
Tail in Low-E Response
Line Splitting at Higher Energy
e-
7Be implantation in Ta base is really bad!
e-
e- escape tail

## Slide 19
Summary: STJ Detector Status
Absorber | Status | Resolution | Speed
Ta-STJs | Work well | 1 – 2 eV FWHM | >1 kcps
Al-STJs | Work | 2 – 4 eV FWHM | >1 kcps
Nb-STJ | Could work | ? (2 eV in 1990s) | >10 kcps

## Slide 20
Summary: STJ Detector Status
Absorber | Status | Resolution | Speed
Ta-STJs | Work well | 1 – 2 eV FWHM | >1 kcps
Al-STJs | Work | 2 – 4 eV FWHM | >1 kcps
Nb-STJ | Could work | ? (2 eV in 1990s) | >10 kcps
Artifact Source | Consequence | Solution | Status
Base layer | Line splitting | Thick high-Z absorber | Works but restricts E range
Wiring + Edges | Low-E Structures | Minimize and Mask | Works (need to quantify?)
Electron escape | Low-E Tail | Capping layer | Doable (must address shorts)

## Slide 21
Summary: STJ Detector Status
Absorber | Status | Resolution | Speed
Ta-STJs | Work well | 1 – 2 eV FWHM | >1 kcps
Al-STJs | Work | 2 – 4 eV FWHM | >1 kcps
Nb-STJ | Could work | ? (2 eV in 1990s) | >10 kcps
Artifact Source | Consequence | Solution | Status
Base layer | Line splitting | Thick high-Z absorber | Works but restricts E range
Wiring + Edges | Low-E Structures | Minimize and Mask | Works (need to quantify?)
Electron escape | Low-E Tail | Capping layer | Doable (must address shorts)
I think we are in pretty good shape (but improvements are always possible).