## Slide 1
Exploration of High-Entropy Alloys (HEAs) for Irradiation Applications
Michael Moorehead, Calvin Parkin, Mohamed Elbakhshwan, Kumar Sridharan, Dan Thoma, Adrien Couet
University of Wisconsin-Madison

## Slide 2: Funding and Collaborations
Institute for Nuclear Energy Systems (INES)
Grainger Institute for Engineering (GIE)
Materials Science Center (MSC)
Financial Support:
Scientific Collaborations::

## Slide 3: High-Entropy Alloys (HEAs) Overview
(a) Conventional alloy, (b) High-entropy alloy (Miracle, Senkov | 2017)
Swelling of increasingly complex alloys under ion irradiation (Jin | 2016)
High-entropy alloys (HEAs) are alloys with multiple principal elements
Typically, no element >35 at%
Usually defined as being primarily a solid-solution matrix
Promising properties have been observed:
High-temperature strength
High specific strength
Enhanced radiation tolerance

## Slide 4: Radiation Damage in Metals
Primary Knock-on Atom (PKA)
Thermal Spike
Damage Cascade
Vacancies
Self-Interstitials
Incoming Particle (n, p+, etc.)

## Slide 5: Radiation Tolerant Microstructures
Typical approach to improving radiation tolerance: increase sink density
Oxide-dispersion strengthened (ODS) alloys
(Allen | 2008)
Nanocrystalline alloys
(Barr | 2018)
100 nm
Cold-worked alloys
(Alshater | 2018)
HOWEVER
These engineered microstructures are not stable under all temperature and damage regimes

## Slide 6: Radiation Tolerance in HEAs
Both modeling and experimentation have shown HEAs can exhibit enhanced radiation tolerance in the matrix
T = 500 °C
(Lu | 2016)

## Slide 7: Radiation Tolerance in HEAs
Proposed mechanisms:
Greater phonon scattering
Sluggish diffusion of interstitial loops
More trapping sites
Broad migration energies
And more!
…
(Lu | 2016)
Alloy with mobile interstitial loops
Alloy with sessile interstitial loops

## Slide 8: Challenges Investigating HEAs
Atomistically modeling many compositions is computationally expensive
CALPHAD modeling offers faster results, but not without problems:
  Dilute solution approximations
  Extrapolations from binary/ternary diagrams
  Extrapolations from high temperatures
Traditional metallurgy (e.g. arc melting) of many compositions is similarly time consuming
Arcast Arc200 arc melter

## Slide 9: Proposed Solution: Develop High-Throughput Capabilities
Use inexpensive modeling to predict stable phases and properties
Use high-throughput synthesis and experimentation to generate phase/property data

## Slide 10: Example: Cr-Fe-Mn-Ni Phase Stability
High-throughput CALPHAD calculations performed using PanDat, Computherm LLC
Stable phases and compositions were calculated for in the Cr-Fe-Mn-Ni family
0-50 at% for each element
Step size: 5 at%

## Slide 11: High-Throughput (HTP) Synthesis Techniques
Combinatorial Thin Films
Additive Manufacturing
Co-deposition schematic (Gebhardt | 2012)
In situ alloying schematic (Moorehead | 2019)

## Slide 12: LENS Additive Manufacturing Process
Cr
Fe
Mn
Ni
Argon
Powder Hoppers
Auger
Part
Build Plate
Laser
Nozzle
Flow Gas
Schematic of the LENS MR-7
Elemental powders are controlled independently
Powders are delivered to print head by argon flow gas
Laser down optic axis melts powders

## Slide 13: Step-by-Step Additive Alloy Synthesis
For aging compositional arrays, samples must be homogeneous throughout
To produce stubs, a powder composition is selected and flown as the laser rasters across surface
Following material deposition, one or more remelting passes is performed to homogenize material
Process is repeated for five build layers to distance from build plate

## Slide 14: Elements Alloyed In Situ with Additive

## Slide 15: Cr-Fe-Mn-Ni Aging Compositions

## Slide 16: Additively Manufactured Cr-Fe-Mn-Ni: As-Built
Stable phases at 700 °C

## Slide 17: Typical Cr-Fe-Mn-Ni As-Built Microstructure

## Slide 18: UHV Homogenization/Aging Furnace
UHV MRF vacuum furnace was used
  Water-cooled steel body allows for rapid cooling of samples
Additive plate was homogenized at 1000 °C for 24 hours
Furnace temperature was dropped to 700 °C and held for 24 hours
After aging, furnace was rapidly cooled to RT
Courtesy of John Perepezko | UW-Madison

## Slide 19: Aged Additive HEA Example: Cr35Fe15Mn15Ni35
Aging
As-Built: Single-Phase FCC
Aged: FCC + BCC

## Slide 20: Characterization Example: Cr35Fe15Mn15Ni35
As-built

## Slide 21: Characterization Example: Cr35Fe15Mn15Ni35
Aged

## Slide 22: Characterization Example: Cr35Fe15Mn15Ni35
As-built
Chart: 
2θ
XRD:

## Slide 23: Characterization Example: Cr35Fe15Mn15Ni35
Aged
Chart: 
2θ
XRD:

## Slide 24: Measured Phase Overview
FCC + Sigma
FCC
Sigma
BCC
FCC + BCC
FCC + BCC + Sigma
As-Built
Aged
X
X
X
X
Cr
Fe
Ni
Mn

## Slide 25: Comparison with CALPHAD
Aged
X
X
FCC + Sigma
FCC
Sigma
BCC
FCC + BCC
FCC + BCC + Sigma
CALPHAD: Computherm LLC
?
X
X

## Slide 26: Moving Forward
UW-Madison Ion Beam Laboratory (IBL)
  1.7 MV Tandem Accelerator
  Protons, He ions, heavy ions, etc.
High-throughput ion irradiations
  Use additively manufactured sample arrays to rapidly screen different HEA compositions

## Slide 28: Backup
Additively Manufactured
Arc Melted

## Slide 29: Backup
Additively Manufactured
Arc Melted

## Slide 30: Backup
Nb-Ta-Ti-V-W
Nb-Ta-V-W
Nb-V-W
V-W
0.2
1.0
1.8
(Körmann | 2017)