## Slide 1
Radiation induced effects in ISOL targets
Luca Egoriti
PhD Candidate, Target & Ion Sources - TRIUMF
TRIUMF – December 10th, 2019
6th RaDIATE Collaboration Meeting

## Slide 2
ARIEL Electron Target East (AETE)
30 – 50 MeV electrons
Radioactive Ion Beam
e-
RIB
γ

## Slide 3
Converter, Target and Ion source assembly

## Slide 4
Converter
Objectives:
  Maximize photon production to target
  Stopping all electrons
First high-Z layer
Second low-Z water-cooled bulk
Which high-Z and low-Z materials?
How to bond them?
Radiochemical effects?
Radiation damage?

## Slide 5: ARIEL e-γ Converter Test Stand (CTS)
e-
Testing conditions:
Electron current = 1.6 mA
Electron energy = 300 kV
Integrated 500 h (~ 3 weeks)
At least 50 heating cycles per sample
12 W/mm2
a) Au-Al Expl. Weld
d) Ta-Al Expl. Weld
c) Au-Al E.D.
b) Au-Al E.D. + Ni

## Slide 6: Pre-Acceptance Tests Au
a) Au-Al Expl. Weld
d) Ta-Al Expl. Weld
c) Au-Al E.D.
b) Au-Al E.D. + Ni
Outcome:
Temperature increase during irradiation
Au-Al diffusion and intermetallic formation
Pristine sample
3.5%
51%
97%
Irradiated sample
    1.5%
    28%
    32%
    98 %

## Slide 7: Acceptance Tests on Tantalum
a) Au-Al Expl. Weld
d) Ta-Al Expl. Weld
c) Au-Al E.D.
b) Au-Al E.D. + Ni
    Outcome:
    Temperature stable over the irradiation period
    No evident damage by eye inspection or SEM
    Temperature stable over 500 h of irradiation
    Surface microscopy shows no damage
    Operational 24/7
Pristine
Irradiated

## Slide 8
Converter, Target and Ion source assembly
Kunz, P. et al, J. of Nuc Mat 440 (2013) 110–116

## Slide 9
ISAC/ARIEL: porous carbide target materials
Kunz, P. et al, J. of Nuc Mat 440 (2013) 110–116
Tantalum target container
Water-cooled copper Heat Shield
Ion Source
ARIEL - AETE
ISAC

## Slide 10
Radioisotope extraction from an ISOL target
Kunz, P. et al, J. of Nuc Mat 440 (2013) 110–116
In target production
Release efficiency

## Slide 11
Release tests: procedure
Room
Temperature
Procedure developed at ALTO/IPNO1
Neutron/photon facilities
Systematic tests on UCx release
Tests procedure at TRIUMF:
Proton 500 MeV
  More materials
  Diverse inventory
Mildly irradiated pellets and spent ISAC targets
Systematic tests on several ISOL target materials

## Slide 12
Isotope Production Facility (IPF)
P+ beam

## Slide 13
Target design
Target disc:
Ø = 19mm
Ceramic of interest = 0.25 mm(UCx, SiCx, ZrCx)
Graphite layer = 0.13mm
Target design and testing: Louis Moskven

## Slide 14
Chamber for Heating Investigations (CHI-stand)
Vacuum stand equipped with:
Exchangeable sample flange
Glass windows
Thermocouple feedthrough (type K-C)
Nuclear ventilation
Plastic glovebag handling

## Slide 15
CHI - Release studies
Vacuum furnace for release tests:
Current delivery up to 500 A
Target heating up to 2000 °C
Fast insertion extraction of test sample

## Slide 16
Thermal conductivity studies
Tantalum target container
Water-cooled copper Heat Shield
Ion Source
ARIEL - AETE
ISAC
Picture from Target Production & Operation, Remote Handling groups
See Mia Au’s poster
Temperature gradients too high and broad
Max temperature too high

## Slide 17
CHI - Thermal conductivity studies
Hot cathode
Accelerating grid
Material disc
Axial thermal gradients
Time-dependent measurements
 Model-independent kth measurement

## Slide 18
Summary
Tantalum target container
Water-cooled copper Heat Shield
Ion Source
Converter Test Stand (CTS):
Material pairing identified (Ta-Al)
Tested under same thermal loads
Release from target materials
Irradiation procedure to be tested soon
Vacuum furnace under commissioning
Activated samples tests in Summer 2020
Thermal conductivity tests
Essential input for target design
Measurements on actinide samples in Spring 2020

## Slide 19: Thank you Merci

## Slide 20
Ucx #27 retrieval

## Slide 21
Ucx beam heating curve
s

## Slide 22
CHI

## Slide 23
RED
Recoil nucleus kicked off the grain
 Enhanced release
 Diffusion length avoided

## Slide 24
Electron-to-photon: radiation yield

## Slide 25
Photon flux and Photo-fission cross sections

## Slide 26
Aluminum % pre-post irradiation: Au-Al explosion bonded
Pristine sample
3.5%
51%
97%
Fig. 4. Sample 1 before (b) and after (c) irradiation for 50 h. Al % in pristine sample (a): 1) 3.5% 2) 51% 3) 97% Al % in irradiated sample (d): 1) 1.5% 2) 28% 3) 32%
4) 98% Zoomed-out SEM interface where gold gaps are evident after irradiation (e).
Irradiated sample
    1.5%
    28%
    32%
    98 %

## Slide 27
Aluminum % pre-post irradiation: Au-Al electroplated
Fig. 6. Sample 2 (top) and sample 3 (bottom). Pristine samples (a), (d) and their interface microstructure (b), (e). Pictures of both post-irradiation samples are shown in (c) and (f).

## Slide 29
Target material disc
Neutral radioisotopes to ion source
Incoming beam

## Slide 31
SiCx beam heating curves
s

## Slide 32
ZrCx beam heating curves
Chart: Calculated Central Target Temperature of ITE-TM2-ZrC#8-LP-SIS target for a Series of p+ Beam Currents
| 580 | 560 | 550 | 540 | 520 | 500 | 480 | 460 | 440 | 420 | 400 | 380 | 360 | 340 | 320 | 300 | 280 | 260 | 240 | 220 | 200 | 180 | 160 | 140 | 120 | 100 | 80 | 60 | 40
no beam | 1612.8083 | 1584.9647 | 1570.6678 | 1556.1084 | 1526.163 | 1495.0429 | 1462.6523 | 1428.883 | 1393.6123 | 1356.7005 | 1317.9875 | 1277.2883 | 1234.3881 | 1189.0352 | 1140.932 | 1089.7232 | 1034.9802 | 976.1784 | 912.6678 | 843.6277 | 768.0029 | 684.4035 | 590.9474 | 484.9956 | 362.6832 | 218.0183 | 40.9629 | -187.3014 | -509.0217
5 uA | 1770.031 | 1730.4336 | 1690.582 | 1650.4779 | 1610.1249 | 1569.5294 | 1528.7011 | 1487.6542 | 1446.4083 | 1404.9901 | 1363.4352 | 1321.7905 | 1280.1172 | 1238.4951 | 1197.0264 | 1155.8427 | 1115.1113 | 1075.0439 | 1035.9062 | 998.0271 | 961.8076 | 927.726 | 896.3349 | 868.2467 | 844.1004 | 824.509 | 809.9891 | 800.8856
10 uA | 1812.2399 | 1774.7862 | 1737.2588 | 1699.678 | 1662.0688 | 1624.4611 | 1586.8906 | 1549.4003 | 1512.0414 | 1474.875 | 1437.9736 | 1401.4229 | 1365.3241 | 1329.796 | 1294.9771 | 1261.028 | 1228.1328 | 1196.5002 | 1166.3633 | 1137.9774 | 1111.6153 | 1087.5596 | 1066.0912 | 1047.4749 | 1031.942 | 1019.6721 | 1010.777 | 1005.2882
15 uA | 1852.5958 | 1817.0332 | 1781.5363 | 1746.137 | 1710.8722 | 1675.7847 | 1640.9234 | 1606.3447 | 1572.113 | 1538.3019 | 1504.9951 | 1472.2872 | 1440.2849 | 1409.1072 | 1378.886 | 1349.766 | 1321.9038 | 1295.4664 | 1270.6284 | 1247.5681 | 1226.4626 | 1207.4809 | 1190.7768 | 1176.481 | 1164.693 | 1155.4745 | 1148.8442 | 1144.7755
20 uA | 1891.3033 | 1857.423 | 1823.7174 | 1790.2251 | 1756.9898 | 1724.0605 | 1691.4924 | 1659.3469 | 1627.6925 | 1596.6055 | 1566.1697 | 1536.4773 | 1507.6287 | 1479.732 | 1452.903 | 1427.2637 | 1402.9409 | 1380.0639 | 1358.762 | 1339.1605 | 1321.3775 | 1305.5185 | 1291.6728 | 1279.9085 | 1270.2692 | 1262.7707 | 1257.3995 | 1254.1126
25 uA | 1928.5335 | 1896.1607 | 1864.0487 | 1832.2397 | 1800.7807 | 1769.7233 | 1739.1245 | 1709.0468 | 1679.5582 | 1650.7325 | 1622.6496 | 1595.3947 | 1569.0584 | 1543.7358 | 1519.5258 | 1496.5293 | 1474.8481 | 1454.5824 | 1435.8286 | 1418.6765 | 1403.2065 | 1389.4865 | 1377.5691 | 1367.4896 | 1359.2631 | 1352.8845 | 1348.3268 | 1345.5425
30 uA | 1964.4311 | 1933.4181 | 1902.7342 | 1872.4234 | 1842.5338 | 1813.1174 | 1784.2308 | 1755.9349 | 1728.295 | 1701.3807 | 1675.2657 | 1650.0273 | 1625.7457 | 1602.5035 | 1580.3843 | 1559.4716 | 1539.847 | 1521.5887 | 1504.7693 | 1489.4541 | 1475.6986 | 1463.5466 | 1453.0288 | 1444.161 | 1436.943 | 1431.3586 | 1427.3751 | 1424.9443
35 uA | 1999.1199 | 1969.3403 | 1939.9446 | 1910.9771 | 1882.4855 | 1854.5211 | 1827.1386 | 1800.3961 | 1774.3553 | 1749.0806 | 1724.6391 | 1701.1001 | 1678.5344 | 1657.013 | 1636.6067 | 1617.3845 | 1599.4122 | 1582.7513 | 1567.4569 | 1553.5768 | 1541.1493 | 1530.2024 | 1520.7524 | 1512.8032 | 1506.3457 | 1501.3575 | 1497.8036 | 1495.6367
40 uA | 2032.7062 | 2004.0513 | 1975.8243 | 1948.0689 | 1920.8317 | 1894.1623 | 1868.1129 | 1842.7385 | 1818.0962 | 1794.2454 | 1771.2469 | 1749.1623 | 1728.0538 | 1707.9826 | 1689.0085 | 1671.1889 | 1654.577 | 1639.2214 | 1625.1641 | 1612.44 | 1601.0753 | 1591.0872 | 1582.4821 | 1575.2565 | 1569.3954 | 1564.8733 | 1561.6545 | 1559.6931
45 uA | 2065.2825 | 2037.6581 | 2010.4968 | 1983.8413 | 1957.7367 | 1932.2305 | 1907.372 | 1883.2127 | 1859.8054 | 1837.2044 | 1815.4645 | 1794.6406 | 1774.787 | 1755.9566 | 1738.2003 | 1721.5656 | 1706.0958 | 1691.8293 | 1678.7983 | 1667.028 | 1656.5358 | 1647.3309 | 1639.4133 | 1632.774 | 1627.3949 | 1623.2486 | 1620.2994 | 1618.5031
50 uA | 2096.9298 | 2070.2532 | 2044.0682 | 2018.416 | 1993.34 | 1968.885 | 1945.0976 | 1922.0257 | 1899.7181 | 1878.224 | 1857.5929 | 1837.8735 | 1819.1136 | 1801.3587 | 1784.6521 | 1769.0334 | 1754.5379 | 1741.1958 | 1729.0317 | 1718.0635 | 1708.302 | 1699.7505 | 1692.4044 | 1686.2514 | 1681.2709 | 1677.4348 | 1674.7077 | 1673.0474
55 uA | 2127.7191 | 2101.9178 | 2076.6309 | 2051.8981 | 2027.7607 | 2004.2612 | 1981.4431 | 1959.3509 | 1938.0294 | 1917.5235 | 1897.8775 | 1879.135 | 1861.3377 | 1844.5252 | 1828.734 | 1813.9974 | 1800.344 | 1787.7977 | 1776.3769 | 1766.0938 | 1756.9543 | 1748.9573 | 1742.0951 | 1736.3525 | 1731.7079 | 1728.1327 | 1725.5923 | 1724.0461

## Slide 34
Disposal
Once Dose@10cm < 10 µSv/h:
Place target container in plastic bag
Bring target in a plastic bag into Hot-Lab fumehood
  Take a swipe
Undo IPF target screws
SiC pellet:
  Extract SiC pellet and place it two sealed plastic bags
  Bring it to ISAC hot cell: to be disposed of in ISAC pale
Openable target assembly:
  Take a swipe
  Place this in a plastic sealed bag
  Bring it to a RPG disposal area
  If Dose@10cm< 10 µSv/h: ready to reuse
Ø = 4”

## Slide 35
Window vacuum suction

## Slide 36
Unshielded doses of target container + 2 pellets
FLUKA: proton flux (top view)
Target container + 2 pellets