## Slide 1: Measurement of displacement cross section in J-PARC for proton kinematic energy range from 0.4 GeV to 30 GeV
RaDIATE 2019 meeting at TRIUMF 9 -13 Dec 2019
(JAEA/J-PARC) Shin-ichiro. Meigo,
H. Matsuda, Y. Iwamoto,
S. Hasegawa, F. Maekawa,
H. Iwamoto
(KEK/J-PARC) M. Yoshida, T. Nakamoto, T. Ishida,
and S. Makimura
Present study includes the results of “Measurement of displacement cross section at J-PARC for structural material utilized at ADS” entrusted to JAEA by MEXT

## Slide 2: Outlook
Introduction
Measurement of displacement cross section experiment in J-PARC
Comparison with calculation by PHITS
Plan of experiment at other facilities
Summary

## Slide 3
Neutron beam lines (23)
Bird’s eye photo
Transmutation
Facility (TEF)
(Phase II）
Hadron Experiment Facility
Neutrino Exp. Facility
(294km to Super KAMIOKANDE)
Materials & Life Science Facility (MLF)
3GeV Synchrotron
RCS (25Hz,1MW)
Linac
400MeV(50mA)
JRR-3M
800m to MLF
30GeV Synchrotron
MR (0.75MW)
J-PARC = Japan Proton Accelerator Research Complex
JFY2007 Beam
JFY2008 Beam
JFY2009 Beam

## Slide 4
Target for high-intensity hadron accelerator and superconductor in high radiation area
Proton beam window in J-PARC spallation neutron source: Aluminum alloy (f 0.6 m)
T2K beam window
Titanium alloy (Ti-6Al-4V)
SC magnet system in beam line of COMET (J-PARC)
For damage estimation of beam intercepting material, DPA is utilized based on displacement cross section.
High accuracy of the displacement cross-section is required.
Proton
3 GeV
Proton 30 GeV
Resistivity change due to radiation is crucial for Superconductor(SC) magnet sustaining damage.

## Slide 5: Transmutation Experimental Facility (TEF)
For R&D of ADS, 0.4 GeV beam by LINAC will be delivered to TEF.
Soviet submarine (LBE)

## Slide 6: Beam transport from RCS to MLF
3NBT
3-50BT
3-GeV RCS
50-GeV MR
Neutrino line
Material and Life Science Experimental Facility (MLF)
Neutron target
Muon target
road to coast
Ep: 3GeV
Power: 1MW
Already demonstrated
Rep.: 25Hz
JSNS
MUSE
FWHM ~150ns
600ns
600ns
Dump

## Slide 7: PKA and DPA
DPA (Displacement per Atom) is estimated by calculation based on PKA (Primary Knock-on Atom)
    Damage characteristics may be described as a function of DPA, gas production and temperature.
    DPA = flux × Displacement cross section

## Slide 8: DPA and displacement cross section
Although DPA is widely utilized to estimate damage, displacement cross section has not been enough validated.
  Cross section exp. data for Ep>20 MeV are scarce.
    Only 5 Data (Cu: 3, W: 2)
    No data for Al, Fe
  Showing large discrepancies among calculation models
N. Mokhov HPTW2016
x8 times

## Slide 9
Measurement of displacement cross section
for 0.4～3 GeV proton
Experiment at the RCS with change of radiation license
Vacuum chamber with
4 K cryo-cooler
1 m
Beam
To sustain damage, sample was cooled to cryo-temperature (~ 4 K).
Displacement cross section(s) can be obtained by increase of resistivity
(Δρ = ΔR∙A/L) due to proton irradiation with average flux ().
ρFP: Resistivity change by a Frankel pair (Cu: 2.2x10-6 Ωm±23%)
Beam dump
From RCS
To MLF
Vertical view

## Slide 10: Al, Fe, Cu and W samples
3NBT for 0.4 – 3 GeV
Cascade scheme of 4 pieces (Al, Fe, Cu, W) with Φ0.25 mm were applied
Samples were annealed ~Tmelt before installation.
Wire direction
  3NBT: Horizontal
  MR: Vertical
  After trial and error, the temperature was achieved <4 K.
  To obtain resistance accurately, 4 wires with delta mode switching polarity with 10 Hz and averaging was applied.
MR for 3 – 30 GeV
40 mm
V+
V-
I+
I-
Sample
MUX
(2700 Keithley)
Nano-V meter
(2182A Keithley)
PC
Source ±0.1A (2182A Keithley)
x16
L<30 m

## Slide 11
Result of experiment
Resistance and temperature during irradiation
Experiment was carried out for protons of 0.4, 0.8, 1.3, 2.2 and 3.0 GeV by changing of acceleration time in RCS.
Vertical beam profile
Obtained by multi wire profile monitor placed in front of the sample
Scanned at sample position by steering magnet
∆R

## Slide 12: Experiment for 30-GeV protons
GM cryo-cooler
Beam was misaligned ~10 mm at sample due to fit the position toward T2K.
Even full strength of steering magnet, the position was not centralized without adjustment of EXT KM.
Data acquisition PC malfunctioned 2 times. Cryo-cooler malfunctioned by unknown reason.
After recovery, do again w/ orbit correction (hopefully Dec 20).
Resistance w/ beam for W
Using the scan result the average flux and cross section obtained.
Dump
T2K
STR 0A
STR MAX
Obs. X-sec

## Slide 13: Calculation with PHITS code
Displacement cross section with PHITS implemented following models
  Norgett-Robinson-Torrens (NRT) model: Widely utilized
  Athermal recombination corrected (arc) model
    Nordlund parameter : Nature comm. 9 1084 (2018)
NRT (Cu Ed 33 eV):
Nd: Number of displacement
Td: Displ. energy
arc-Nordlund (Cu Ed 33 eV):
ー NRT
ー arc Nordlund
Nd different for Td>83 eV
X 3

## Slide 14: Comparison Calc. vs Exp.
NOTE: 30 GeV experiment very preliminary result

## Slide 15: Displacement cross section ~30 GeV
As increase proton kinematic energy, heat density on material (W) increase
Regardless of increase heat deposition for Ep~30 GeV, displacement cross-section sustains almost constant . Why?
● Heat density
ー Bethe-Bloch
30 GeV
On Wed, Y. Iwamoto’s talk

## Slide 16: Isochronal recovery result
To observe recovery dependence of temp., irradiated sample heated to certain temp and cooled cryotemp (~4 K) again.

## Slide 17: Experiment at FNAL for 120 GeV
Budget already approved by MEXT for some of our collaborators
Experiment will start for 120 GeV proton in next JFY 2020.
120 GeV proton
Cryo chamber and beam instruments will be placed
MT3

## Slide 18: Ep 400 GeV at HiRadMat in CERN (plan)

## Slide 19: Summary
To understand the damage on beam intercepting materials, displacement cross section was obtained for Al, Fe, Cu, and W for proton 0.4 - 30 GeV.
  NRT model: 4 times overestimation
  arc model: good agreement with present results.
To obtain the cross section, similar experiment will be carried out at FNAL and HiRadMat for 120 and 400 GeV protons.

## Slide 20: Thank you for attention
Memorial snap shot completed beam test of 1MW for 1 h.
This year successfully completed for 10 h. Next year 1 week?
Successfully completed 1 MW beam test!
2018 July 3rd

## Slide 22: 1 MW beam operation at MLF
Last year memorial snap shot at 1MW for 1 h test (2018/7/3)
Result of this year
Beam intensity trend at 1MW for 10.5 h test (2019/7/3)
Availability ~ 98%
1 MW

## Slide 23: Proton Beam Window at MLF (A5083)
Lifetime estimation based on Post Irradiation Examination (PIE) for safety shroud (AlMg3) at SINQ in PSI
Considering difference of proton energy, to predict lifetime of the PBW with high accuracy for validation of calculation
Result at SINQ/PSI for 0.6GeV
Y. Dai, et al, J. Nucl Mat. 343 184 (2005)
Height: 3.8m
Weight：10t
Lifetime of PBW: Determined by He gas production (1200 appm) 2 years*
By recent PIE result of the SINQ (2400 apmm), lifetime may be applicable to 3 years.
* S. Meigo, et al, J. Nucl Mat. 450 141 (2012)

## Slide 24: Targets in Material Life Experimental Facility (MLF)
Muon production target
  Carbon graphite
  Highest μ- intensity
Neutron production target
  Mercury (Hg)
Thick. 2cm
Diam. Φ33cm
L 2m
W 34cm
SS container
Ptron
Hg
Light water
Safety hull
Double wall: Helium layer observed radiation
Highest pulse intensity in the world
8% beam loss

## Slide 25: ADS proposed by JAEA
~ 30 MW
Beam window
Beam window: 20 dpa/year. Accuracy of dpa is required for damage estimation.
Belgium ADS program MYRRHA at SCK・CEN (Mol) approved 558 M€

## Slide 26: Contribution for displacement
Fission and spallation fragment dominating