## Slide 1: Calculations of damage energy of nuclear reaction products and experimental plan for DPA cross section using 120 GeV protons at FNAL
1. JAEA, 2. KEK, 3. FNAL
6th RaDIATE Collaboration Meeting, 9th-13th Dec. 2019 at TRIUMF
Y. Iwamoto1, S. Hashimoto1, M. Yoshida2, H. Iwamoto1, S. Meigo1,
K. Yonehara3, T. Spina3 and P. Hurh3
This work is supported by JSPS KAKENHI Grant Number JP19H02652.
Present study includes the results of “Measurement of displacement cross section at J-PARC for structural material utilized at ADS” entrusted to JAEA by MEXT.

## Slide 2: Outline
1. Introduction
2. DPA calculation method in high-energy region
3. Calculations of DPA cross sections and damage energy
4. Plan for DPA measurements using 120 GeV protons
5. Summary

## Slide 3: Introduction
Prediction of usable lifetime of materials under high-energy (E>100 MeV) particle irradiation is essential for the design.
Displacement per atom (DPA) value is used as a damage-based exposure unit.
2nd target in J-PARC MLF (W)
Beam window in neutrino facility (Ti alloy)
Beam windows in J-PARC MLF (Al alloy)
CERN LHC superconducting magnet (Nb alloy)

## Slide 4: Microscopic effects on material
sd : displacement cross-section (m2)
: irradiation fluence (particles/m2)
DPA=
DPA: average number of displaced atoms per atom of a material
vacancy
Interstitial atom
Frenkel-pairs cause cascade damage.
Primary Knock-
on Atom (PKA)
G. S. Was, Fundamentals of Radiation Materials Science, New York, USA: Springer Press, 2017
Conventional method: NRT model (Norgett, Robinson, Torrens)
Damage energy transferred to lattice atoms
Threshold displacement energy
The number of atomic displacement
Nuclear Engineering and Design 33 (1975) 50.
15 – 90 eV

## Slide 5: Problem for dpa calculations in high-energy
New method: athermal recombination correction (arc)
K. Nordlund et al., Nature Communications 9 (2018) 1084.
PHITS
NRT and arc dpa cross sections for p-W.
Monte Carlo codes with nuclear reactions.
e.g. PHITS, MARS, FLUKA, MCNP
Relationship between nuclear products and their damage energies are unclear.
Contribution of relativistic Coulomb scattering cross section between proton and target is not considered in PHITS.
No data with proton energy over 30 GeV
High-energy region above 100 MeV
T. Sato et al., J. Nucl. Sci. Technol., 55 (2018) 684-695.

## Slide 6: Purpose
Implementation of relativistic differential Coulomb scattering cross section for DPA calculation in PHITS
Calculations of arc-dpa cross sections and damage energy up to 120 GeV protons
Introduction of plan for DPA cross section measurements with 120 GeV protons at FNAL

## Slide 7: Outline
1. Introduction
2. DPA calculation method in high-energy region
3. Calculations of DPA cross sections and damage energy
4. Plan for DPA measurements using 120 GeV protons
5. Summary

## Slide 8: DPA calculation method in PHITS
(1) Nuclear interaction
(2) Energy transfer
with Coulomb scattering
Y. Iwamoto et al., Nucl. Instr. Meth. B 274 (2012) 57-64.
target atom
Proton or
nuclear products
Nuclear products
(3) Cascade damage
approximation
Proton
DPA=
Differential Coulomb scattering cross section
Defect production efficiency
Number of displacement
DPA cross section
Intra-nuclear cascade
(INCL4.6 and JAM)
Ionization: ATIMA
Evaporation (GEM)
t: dimensionless transferred energy

## Slide 9: Differential Coulomb scattering cross section
t: dimensionless transferred energy
Ep :kinetic energy of proton or nuclear products
T: transferred energy to target atom
Screening functions:
:dimensionless energy
Tmax: maximum T
Large t large T in close collisions
Small t small T in distant collisions
(Z1, M1)
(Z2, M2)
l=1.309, m=1/3, q=2/3

## Slide 10: Relativistic differential Coulomb scattering cross section
t: dimensionless transferred energy
Ep :kinetic energy of high-energy (>100 MeV) proton
T: energy transferred to target atom
Relativistic differential Coulomb scattering cross section:
Tmax: maximum T
(Z1=z, M1=m)
(Z2=Z, M2=M)
Relativistic correction for high-energy proton
implementation into PHITS
Impact parameter
Next: Damage energy to lattice atom
I. Jun, IEEE Trans. Nucl. Sci. 48 (2001) 162.

## Slide 11: Damage energy transferred to the lattice atom
Td :damage energy is the energy available to generate atomic displacements by elastic collisions
Relationship between PKA energy and damage energy
Damage among same atoms
The energy lost in the cascade by electron excitation is subtracted.
Number of displaced atoms using phenomenological approach by Lindhard.
T
Td
1 MeV
J. Lindhard et al., Dan Vidnsk Selsk Mat Fyf Medd 33:1 (1963).
Next: Defect production efficiency
Damage energies are saturated with PKA energy over 1 MeV.

## Slide 12: Athermal recombination correction
Figure 2 : K. Nordlund et al., Nature Comm. 9 (2018) 1084.
NRT damage model
Actual damage production
Molecular dynamic simulation study
Defect production efficiency
Schematic illustration of the damage for the case of ~1 keV damage energy in a metal
Interstitial atom
Vacancy
Cu: b = -0.68, c = 0.16
W: b = -0.56, c = 0.12
Efficiency function based on tabulated parameters

## Slide 13: Outline
1. Introduction
2. DPA calculation method in high-energy region
3. Calculations of DPA cross sections and damage energy
4. Plan for DPA measurements using 120 GeV protons
5. Summary

## Slide 14: Arc-dpa cross section for proton irradiation
Nuclear reaction product is dominant with proton energy over 100 MeV.
Contribution of Coulomb scattering for p+target increases with Ep over 1 GeV.
i.e. 9% at 1 GeV, 19% at 30 GeV, 29% at 100 GeV for tungsten
Arc-dpa cross sections for p+Cu and p+W
Next slide: arc-dpa cross section of nuclear interaction product

## Slide 15: Arc-dpa cross section of nuclear interaction product
Arc-dpa cross sections are widely distributed with increasing proton energy.
This trend is strong for heavier target material.
Next slide: Damage energies for 1 GeV protons incident on W.
Arc-dpa cross sections of nuclear interaction product

## Slide 16: Damage energy of each nuclear product for 1 GeV p+W
For target nucleus (tungsten), contribution of nuclear elastic scattering is dominant below 50 keV.
In-elastic scattering components are dominant for 50 keV – 5 MeV.
Average damage energy distribution
Energy spectra of W, Ho and Sn
Damage energy is smaller than kinetic energy because the energy lost in the cascade by electron excitation is subtracted.
Nuclear elastic
Nuclear in-elastic
Next slide: Damage energies for 50 GeV protons incident on W.

## Slide 17: Damage energy of each nuclear product for 50 GeV p+W
Damage energy range are almost same in the proton energy region from 1 to 120 GeV.
Average damage energy distribution
Energy spectra of W, Ho and Ag
Nuclear elastic
Nuclear in-elastic
Damage energies of nuclear products also range from 50 keV to 5 MeV.

## Slide 18: Outline
1. Introduction
2. DPA calculation method in high-energy region
3. Calculations of DPA cross sections and damage energy
4. Plan for DPA measurements using 120 GeV protons
5. Summary

## Slide 19: Measurement method of dpa cross section
We have developed liquid cryogen-free cooling system and measured dpa cross sections at accelerator facilities in Japan.
Irradiation on metal at cryogenic temperature
Δρmetal: Electrical resistivity change(Ωm)
Φ: Average Beam fluence(1/m2)
ρFP: Frenkel-pair resistivity (Ωm)
Recombination of Frenkel pairs by thermal motion is well suppressed.
Damage rate
Resistivity increase is the sum of resistivity per Frenkel pair
In BNL experiments, cryostat assembly for sample irradiation consisted of
complicated system to deliver a flow of liquid cryogen.
Before our experiments, the data have been measured using 1 – 2 GeV protons at BNL.
G.A. Greene et al., Proc. of AccApp '03, 1-5 Jun 2003. San Diego.

## Slide 20: dpa cross section measurements
RCNP, Osaka Univ.
FFAG facility, Kyoto Univ.
Y. Iwamoto et al., J. Nucl. Mater., 508, (2018) 195-202.
Y. Iwamoto et al., J. Nucl. Mater., 458, (2015) 369-375.
125 - 400 MeV proton + Al, Cu, W
J-PARC
0.4 - 30 GeV proton+Al,Cu,Fe,W
Dr. Meigo will present at this workshop
Experimental plan with 120 GeV proton at FNAL.
No experimental data above 30 GeV

## Slide 21: Fermilab Test Beam Facility (FTBF) located on FNAL
Tevatron
Main injector
MS3/M03
21/26

## Slide 22: Experimental area in M03 beam Line
158.75 cm
Quad Magnet
Collimator
62 cm
f32 cm
Beam structure
60 sec
120 GeV protons
Irradiation chamber used at RCNP
Experimental area
1011 proton/min
4.2 sec
24 h irradiation: 8.64 x 1015 protons
RMS beam size can be 4 mm for protons
22/26
Segmented Wire Ionization Chambers (SWICs) will be installed.

## Slide 23: Irradiation chamber and target assembly
GM refrigerator
RDK-408D2, Sumitomo Inc.
Helium gas
Supply
Return
1st stage of cold head (40K)
2nd stage of cold head (4K)
542 mm
1mm thick thermal shield
OFHC
Al
Resistance thermometer
140 mm
Sample assembly
Measure the changes in electrical resistivity of sample under proton irradiation
Schematic of the cryogenic irradiation chamber

## Slide 24: Improvement of samples
25 mm
Beam loss permits less than 3 % of interaction length in area at M03.
1.2 cm for 120 GeV proton on Al.
Total thickness of AlN and Al plates:2.2 cm
Sample used in RCNP
Four wire samples
Wire sample with 125 mm diameter
Production method of four wire samples (Al, Fe, Cu, W) was established.
Trend of electrical resistance with 30 GeV protons
6th Nov. 2019
Time
Electrical resistance
W
Success to measure change of resistance.
This method will be applied to the FNAL expt.
J-PARC MR
Source:6221
Nano-voltmeter
2182A Keithley Inc.
Four point technique
PC
Labview
V+
V-
I+
I-
±100 mA
Precision
±0.001μΩ @ 3 K

## Slide 25: Outline
1. Introduction
2. DPA calculation method in high-energy region
3. Calculations of DPA cross sections and damage energy
4. Plan for DPA measurements using 120 GeV protons
5. Summary

## Slide 26: Summary
Contribution of Coulomb scattering for proton + target increases with proton energy over 1 GeV.
Damage energy to the lattice atom ranges from around 50 keV to 5 MeV for high-energy proton irradiation over 1 GeV.
Production method of four wire samples (Al, Fe, Cu, W) was established for DPA cross section measurements with 120 GeV protons at FNAL.
i.e. 29% at 100 GeV.

## Slide 27: Back-up

## Slide 28
Scale on total irradiation effect
10-2
10-6
10-10
10-14
10-18
10-20
10-15
10-10
10-5
100
105
1010
Nuclear reaction
Atomic collisions
Diffusion and growth process
Nuclear reaction model
Molecular
Dynamics
K-Monte Carlo
Dislocation dynamics
Size (m)
Time (sec)
Voids
Interstitial atom
Vacancy
Primary Knock-on Atom (PKA)
DPA focuses on primary damage.
Irradiated
Not irradiated
Property changes
Strain
Notes: First, I’d like to show you scale on total irradiation effect.

## Slide 29
Particle and Heavy Ion Transport code System
Capability
Transport and collision of various particles over wide energy range
in 3D phase space
neutron, proton, meson, baryon electron, photon, heavy ions
up to 1 TeV/u
Accelerator Design
Radiation Therapy
Space Application
Development
JAEA (Japan), RIST (Japan), KEK (Japan), Technische Universitat Wien(Austria)
Overview of PHITS
Application Fields
RIKEN (Japan), CEA (France), Kyushu Univ. (Japan)
nSv/h
600
20
T. Sato et al., J. Nucl. Sci. Technol., 55 (2018) 684-695.

## Slide 30: Proton energy dependency of damage energy for nuclear products
Damage energy for p+Cu
Damage energy for p+W
Damage energy of target nucleus (Cu, W) :10 keV – 100 keV.
Decreasing with proton energy.
Damage energy of nuclear reaction products:100 keV – MeV order.
Almost constant with proton energy.