## Slide 1: Blister study in W irradiated MeV protons Fracture morphology & Mechanical properties
I Gavish Segev1,2, E Yahel3, I Silverman2 and G Makov1
1Dept. of Materials Engineering, Ben-Gurion University of the Negev,
Beer Sheva 84105, Israel
2 Soreq NRC, Yavne, Israel
3 Dept. of Physics, NRCN, Beer Sheva 84190, Israel

## Slide 2: Talk Outline
Introduction:
  SARAF Accelerator
  Protons radiation damage in W
  keV Vs MeV
Experimental
Results
  Blisters morphology
  Mechanical properties
Summary
Protons radiation damage at Cu collimator at PSI
Be cracking at JUDITH e beam

## Slide 3
*SARAF Phase-I Accelerator
 | MeV | mA
Protons | 4 | 2 CW
Deuterons | 5 | CW1
*Soreq Applied Research Accelerator Facility (SARAF)

## Slide 4
SARAF Phase-II Accelerator
 | MeV | mA
Deuterons/ Protons | 40 | 5 CW
LEBT
RFQ
MEBT
CM1
CM2
CM3
ion source
0.04
2.6
2.6
6.8
11.5
24.5
40.0
Deuteron energy (MeV)
Beam
GaIn flow
Proton beam

## Slide 5
2.2 MeV
50keV
Tungsten
Irradiated
surface
0.1µm
17µm
Protons radiation damage

## Slide 6: Hydrogen in W
Migration E[eV] | 
0.005 | SIA in W
0.26 -0.39 | D in W
1.78-1.8 | Vac. in W
Trapping E | H trapped in…
1.4eV | 1. vacancy
1.3-1.5eV | 2. Dislocation and grain boundaries
1.4eV | 3. Gas in voids
1.8-2.1eV | 4. Chemisorption sites on the wall of voids
30-130K – only SIA is mobile
T>130K – Deuterium is also mobile
T>600K- vacancies are also mobile
Different sinks with similar binding energies which makes it more difficult to distinguish between the sinks using TDS approach.
When H penetrate into W it enhanced defects production
which may serve as trapping sites
The accumulated damage depend on the ion energy, flux, temperature etc.

## Slide 7: Hydrogen Blisters at low E(keV)
Blistering threshold dose 1018–1020 cm-2
Temperature:
As T Blister Height & Density
Above 700K no blister formation
At very low T – cracks instead of blisters
Increasing T- increase in H diffusion- far from surface
High T- traps can no longer able to hold H

## Slide 8: Hydrogen Blisters at low E(keV)
The mechanism to blister formation and growth is not clear in the case of H (as opposed to He)
In He forms gas bubbles form with pressure >> surface tension. Blister cap ~= He stopping range.
In H : Blister cap >> proton stopping range
Enomoto et al. 2009
Inter bubble fracture and loop punching model

## Slide 9: keV vs. MeV protons
The ability to compare drives from E lose processes of protons
T affects diffusion processes
Therefore MeV Vs. keV is expected to differ in hydrogen retention, radiation damage evolution and blistering conditions
MeV | keV | 
Microns scale | nm scale | Implantation range
Minor sputtering | Intensive sputtering | Sputtering
High | Low | Irradiation temperature
??? | 1018-10 20protons/cm2 | Blister formation critical dose

## Slide 10: Research goals
The main goal of this research is to explore the effect of irradiation by high energy protons (MeV’s) on blister formation and growth in W.
At these high energies we expect deeper penetration of the protons in W, greater energy transfer and thus higher temperatures, all of which should affect the nature, density, and evolution of the radiation induced defects in the material.
In particular, we shall focus on Nucleation and growth of hydrogen blisters, and the material and irradiation parameters controlling it.

## Slide 11: Experimental
10mm
1.5
mm
2.2 MeV protons beam
In situ back wall Temperature measurement
In situ current measurement
Polycrystalline& Single crystal (110)
W discs
8mm
Beam diameter
0.1-10µA | Proton current
3×1012– 2×1014 Protons/cm2s | Beam flux
1×1017-7×1018 protons/cm2 | Total dose

## Slide 12: Experimental-Cooled Target Cell

## Slide 13
Very large and shallow blisters obtained at PC & SC
At a low critical proton dose - 3·1017protons/cm2
Results- Blisters

## Slide 14: Blister shape – Role of T & GB
I. Gavish Segev et al. Journal of Nuclear Materials 513 (2019) 209
keV: (R.T)
PC
Height/area 0.1-10
SC
Height/area 0.2-0.6

## Slide 15
Cross section by FIB drilling
Cross section of a blister

## Slide 16: PC Morphology study of blisters
PC 300K
dose 7.7X1017cm-2
PC 670K dose 4.3X1017cm-2
PC 340K dose 4.5X1017cm-2
PC 540K dose 8X1017cm-2
I. Gavish Segev et al. Journal of Nuclear Materials 525 (2019) 40

## Slide 17: SC Morphology study of blisters
SC 300K dose 6.5X1017cm-2
SC 300K dose 12.9X1017cm-2
SC 590K, dose 69X1017cm-2
I. Gavish Segev et al. Journal of Nuclear Materials 525 (2019) 40

## Slide 18: Inner PC blister cap
Blister’s cap was removed from a 540K irrad. PC sample, via FIB drilling.
An electric fiber was glued to the upper surface allowed the elevation of the cap

## Slide 19
Inner PC blister cap
Ductile transgranular surface
Intergranular fracture surface
I. Gavish Segev et al. Journal of Nuclear Materials 525 (2019) 40

## Slide 20
Cross sections show that the blisters cap depth is in the same depth as protons stopping range ± few microns,
regardless of
irradiation temperature
irradiation dose
tungsten crystallinity
Ductility increases with temperature for both PC and SC samples.(it is emphasized in SC samples)
Correlated to our results of increased height/area ratio with T. (largest ratio obtained to HT SC samples).
The increased ductility in HT SC versus PC ,may be correlated to the transient H inventory in SC – which facilitate dislocation movement[*]
Morphology study of blisters
*S. Lindig, M. Balden, V.Kh Alimov, T. Yamanishi, et al., Subsurface morphology changes due to deuterium bombardment of tungsten, Phys. Scr. T138 (2009) 014040.
*B. G. Butler, et al., Mechanisms of deformation and ductility in tungsten – A review, Inter. J. Ref. Met. & Hard Mater. 75 (2018) 248-261.

## Slide 21: mechanical properties of blisters
Nano-indentation was done to a cross section of R.T irradiated (110) single crystal
Ra< 50nm
Hardness values were taken as an average value in depth range of 700-750nm
8 µm
-25 µm-----
-45 µm-----
-65 µm-----

## Slide 22: mechanical properties of blisters
7.8GPa- obtained 8µm from irrad. Surface- both in blister’s cap and at a non blister zone.
All other measurements showed hardness value of non irrad. Reference sample. (6.2GPa)
7.8±0.2GPa
6.2±0.2GPa
I. Gavish Segev et al. Journal of Nuclear Materials 525 (2019) 40

## Slide 23
Increase in hardness values was seen in the irradiated tungsten, as expected (Irradiation hardening effect).
The increased hardness values are similar at a non blister zone and a blister zone.
The increased hardness is independent to the elevation of the cap.
At 25microns ±2.5microns, the hardness reaches its reference value. Only ~3micron from the end of blister hole.
mechanical properties of blisters

## Slide 24: mechanical properties of blisters
Hardness upon cap cross section was measured to lower depth (450nm)
Indentation region is X7 with indentation depth.
Each indentation is taken from its center position ±1.5micron.

## Slide 25: mechanical properties of blisters
Vacancy production profile plus Hardness

## Slide 26: mechanical properties of blisters
R.G. Abernethy, Predicting the performance of tungsten in a fusion environment: a literature review, Mater. Science and Tech., 33:4 (2017) 388-399
4000C-8000C
RT
Notes: This graph is of neutrons from:
FFTF and JOYO (fast reactors): En>0.1MeV and from JMTR with a mixed n spectrum
JOYO { fluence 10^25n/m2 , dpa-0.17 (400C)- up to 1.54dpa (750C)

## Slide 27
Blisters cap depth is in the same depth as protons stopping range
Ductility increases with T for both PC and SC.
At HT SC we obtained largest ratio of height/area. Which is also correlated with high stresses
Increased hardness values are similar at a non blister zone and a blister zone
In blister cap, hardness increase with good correlation to vacancy production
In our case, Protons have better similarity in increased hardness to neutron radiation damage than to self ion radiation damage.
Summary

## Slide 28
Thank you for listening

## Slide 29
Damage profiles for 3.2MeV protons & 5MeV Ni ions in stainless steel
G.S. Was, Fundamentals of radiation material science second ad., springer 2017