## Slide 1: Development of ultrasonic meso-scale fatigue testing of irradiated titanium alloys for proton beam window applications
6th RaDIATE Collaboration Meeting TRIUMF, Vancouver, Canada
Presenting Author: Phil Earp
University of Manchester / University of Oxford / Culham Monday 9th December 2019
Jason Hess, Dr Jicheng Gong, Prof. Angus Wilkinson, Dr Chris Densham, Dr Slava Kuksenko

## Slide 2: Outline
T2K Neutrino Experiment
  Proton Beam Window
  High Cycle Fatigue
  Radiation Damage
Scientific Question
Experimental Plan
  Ultrasonic Meso-Fatigue Testing
  Radioactive Samples at the Culham Science Centre, UK
UFR Development at Culham MRF

## Slide 3: T2K Neutrino Experiment
https://t2k-experiment.org/t2k/
Chris Densham, STFC (2010 Presentation)
SOURCE
DETECTOR
Decay Volume
Beam Dump
Helium Vessel
L=110m, V=1,500m3
OA
2o
2.5o
[3o]
Target Station
Graphite
Outer tube / beam window (Ti6Al4V)
T. Ishida et al., J-PARC Accelerator, Japan (2019 Presentation)
T. Ishida et al., J-PARC Accelerator, Japan (2019 Presentation)
Proton Beam
Pions
Pulsed Proton Beam
30 GeV Energy
protons per pulse
750 kW Beam Power

## Slide 4: Proton Beam Window
Pulse length ~ 5 s
8 58 ns bunches per pulse
Graphs from Matt Rooney, STFC (2006 Presentation)
Kavin Ammigan (Fermilab) (2017 Presentation)
Delay of ~ 2 s
Each pulse causes local heating spikes of ~150 degrees C
Thermal shock wave rings through material
Stress waves ‘Ringing’ – typically 150 MPa amplitude
Rapid thermal shock

## Slide 5: Titanium Alloys
  Typical commercial alloy
  ELI – Extra Low Interstitials
Titanium and Titanium Alloys
Wiley-VCH, Weinheim (2003)
Zheng, Yufeng. (2013). Thesis - Nucleation mechanisms of refined alpha microstructure in beta titanium alloys.
-phase (hcp)
-phase (bcc)
CP-Ti (Commercial Purity Ti) - only
Ti-6Al-4V - alloy
Ti-15V-3Cr-3Al-3Sn – metastable alloy
  Good cold formability
  Good cold formability
High specific strength
Relatively low thermal expansion coefficient
Vanadium is a -stabiliser

## Slide 6: High Cycle Fatigue of Ti-6Al-4V
Yield stress @ operating T (200C) = 630 MPa
Stress Amplitude ~ 50 – 150 MPa
‘High Cycle Fatigue’ Regime
  Crack initiation is important
Properties depend on Radiation Damage
Fatigue of Beta Processed and Beta Heat Treated Titanium Alloys
Wanhill & Barter, (Springer, 2012)
Wu, G.Q., Shi, C.L., Sha, W., Sha, A.X., Jiang, H.R., Effect of microstructure on thefatigue properties of Ti-6Al-4V titanium alloys, Materials and Design (2012), doi: http://dx.doi.org/10.1016/j.matdes.2012.10.059

## Slide 7: Radiation Damage
Mechanical properties change:
Hardening
Tensile strength
Ductility
Creep rate
Swelling
Proton beam interacts with material
Radiation damage accumulates
>1 dpa per year!
T. Ishida et al.
Hoffelner W. (2015) Irradiation Damage in Nuclear Power Plants
Incomingproton
Microstructural changes:
Dislocation loops
Dissolution of precipitates
Void formation
Neutron irradiation – data exist up to 0.3 dpa
Proton irradiation
V. high dose rate
Radionuclide generation
  H & He gas  interstitials or bubbles
Mechanism for high-energy protons?

## Slide 8: Scientific Question
“What is the effect of proton irradiation on the high-cycle fatigue behaviour of the Ti-6Al-4V alloy?”
This allows STFC (beam window manufacturer) to predict the component lifetime:
“After how long should the beam window be replaced?”
“Are there more suitable alloys for this purpose?”

## Slide 9: Experimental Plan
Specimens manufactured
Microstructural investigation
HCF Testing
Irradiation in medical isotope production factility
Optical Microscopy
EBSD – Grain size, texture
EDX – Chemistry
Nanoindentation Hardness Measurement
Change in fatigue life with irradiation
Post-test fractography
Hardness change after irradiation
Compare candidate alloys
Ti-6Al-4V T2K Material
4x Candidate Grades
BLIP – Brookhaven Linac Isotope Producer

## Slide 10: Ultrasonic Meso-Fatigue
Operates at 20 kHz
  cycles in 14 hours (c.f. cycles conventional fatigue testing)
Jicheng Gong et al. (2017 Presentation)
Von Mises Stress
Small laser-cut specimens
  Diameter = 3.4 mm
  Thickness = 100 m - 150 m
  Can only irradiate small volumes of material
  Low radioactivity due to small volume (easier to handle)

## Slide 11: Microstructural analysis

## Slide 12: Microstructural analysis
#001
#106
#115
#058

## Slide 13: Microstructural analysis (2)
#001
#106
#115
#058
x
y
z
DOUBLE CHECK ORIENTATIONS

## Slide 14: Ultrasonic Meso-Fatigue
Measure cantilever deflection with laser reflection
Jicheng Gong et al. (2017 Presentation)
To accept radioactive specimens
  Remote specimen mounting
  Optics to detect laser position – cannot be observed directly by operator

## Slide 15: Experimental Challenges
Specimen
Laser
Sample at 100 kHz
?
Laser Detector
?
Incoming laser at normal incidence
!
Small spot size on specimen
?
Large spot size on detector
?
Angular beam deflection  linear motion on detector
?
Sample contained after failure
?
Remote Handling Capability
?
Transparent Window
Detect large specimen deflections
?
Detector
Detector
Optics
Specimen Mounting
?

## Slide 16: Proposed solution
Laser
Lenses
Beamsplitter
Detector
Specimen
Laser
Beam
Diameter Reduction
Specimen
Alignment Camera
Linear Polariser
plate
Rotates polarisation
plate
Linear to Circular polarisation
 Circular to 90 rotated Linear polarisation
Beam stop
‘4f lenses’
Quadrant Photodiode Detector
Polarising Beamsplitters

## Slide 17: Commissioning
Chart: Applied Specimen Tilt (degrees)
| 0.5 | 1.25 | 2 | 2.75 | 3.5 | 4.25 | 5
 | 0.67424 | 2.1083 | 3.6086 | 5.0525 | 6.5242 | 7.9364 | 9.3389
Optics
Design, Prototype and Test
Alignment procedure
Calibrate
Assess sensitivity of detector
Hardware
Software and UI
Optics mounted on 6-axis translation stage for alignment
Cooling air provided for extended ultrasonic use
Remote controlled camera & specimen illumination
Data logging and real-time processing
Diagnostics
Implemented in LabView
Use of Fourier Transform to assess changes in oscillation

## Slide 18: Raw Data
Ultrasound OFF
Ultrasound ON
20 kHz
Frequency (kHz)
Time (s)

## Slide 19: Integration into the MRF
Hot Cells (Active sample preparation)
Research rooms
(Contain instruments)
SEM inside Research Room 3
Remote handling robot on left

## Slide 20: Summary
Ti-6Al-4V beam window operates in challenging environment
  High Cycle Fatigue (HCF) from thermal spikes
  Radiation damage from proton irradiation may alter mechanical properties
Specimens of Ti Alloys irradiated in proton beam
Ultrasonic meso-fatigue testing will identify radiation-induced changes to HCF life
Ultrasonic Fatigue Rig (UFR) with continuous amplitude (stress) measurement of amplitude at 20 kHz developed at the Materials Research Facility (MRF) at Culham

## Slide 21: Thank you for your attention Any questions?
Phil Earp Monday 9th December 2019