## Slide 1: Irradiation Induced Failure Analysis of NuMI Target
Sujit Bidhar
Dec 11, 2019

## Slide 2: Outline
Background NTO2 Target fin
Fin material properties and response under irradiation
Swelling empirical formula
Finite element implementation and results
Failure analysis

## Slide 3: Background- NT02 Target Fin
95 cm
Segmented Fins- 47 pieces
Individual target fin
20mm x 15 mm x 6.6 mm
Material : POCO ZXF 5Q graphite
Isotropic

## Slide 4: Background- Fracture fin
y
z
x
z
Beam Parameters:
Energy :120 GeV
Beam sigma : 1.1mm
Spill duration : 10µsec, 4x1013 protons/pulse
Duty cycle :1.87sec
Peak fluence : 8.6x1021 protons/cm2
Bulk swelling of ~2%

## Slide 5: POCO ZXF 5Q Graphite microstructure
Carbon 1971. Vol. 9, pp. 697444.
Pores
Less Mrozowski cracks
Randomly oriented grains
  isotropic
Pores & particles ~ microns
Particles packed with many grains
  Fine grains (~30nm)
Grain
c
a
c
a
HCP structure
Hexagonal Basal plane
(1 0 0)
(2 0 0)
d-spacing
Particles

## Slide 6
Graphite Swelling Fluence factor
Kelly, J. Vac. Sci. Technol. A 4 (3), 1986
C-axis expansion is more than a-axis contraction
Swelling f(fluence, temperature)
  More swelling at lower temperature
XRD – Pyrolytic carbon

## Slide 7
Graphite Swelling XRD- POCO ZXF5Q
150 C
150 C
C-axis expansion is more than a-axis contraction  net expansion
Interstitial  expansion
Vacancy contraction
c
a
a
N. Simos, PRAB 20, 071002 (2017)

## Slide 8
Swelling factor function
Local Swelling factor =f(fluence)*g(temperature)
sw(Ø,T)= f(Ø).g(T)
Initial guess for f(Ø)
f(Ø)=exp{-b(u/σ)2}
u=u(x,y,z)

## Slide 9
Swelling factor function
∂(sw)= g(T). ∂f(Ø) + f(Ø).{∂ g(T)}.
At constant fluence swelling factor follows a polynomial function with temperature (next slide)
(a)
Neutron dose, p/cm2
Swelling %
0
2
4
6
8
10
12
14
16
5
10
15
20
25
30
∂ g(T)/ ∂T at f(Ø)
Attempting to find form of the function from the swelling trend

## Slide 10
Swelling Temperature Factor
Pronounced swelling at lower temperatures
D. Schweitzer, Physical Review, Vol 128 (2), 1962, pp .556-559
1 MWD = 7e16 nvt
Chart: Temperature factor
| 20 | 30 | 38 | 42 | 57 | 65 | 75 | 90 | 120 | 160 | 190
normalized data | 1 | 1.0326 | 0.97826 | 0.94565 | 0.92391 | 0.86957 | 0.86957 | 0.73913 | 0.54348 | 0.3587 | 0.19565
∂g(T)=-7 T3 - -5 T2 + -3 T+1.0083
NTO2 steady state operating temperature range

## Slide 11
Steady State Thermal Analysis
Path-y
Beam direction
Path-x
(a)
Chart: Distance from beam center, mm
| 0 | 6.8750000000000006E-2 | 0.13750000000000001 | 0.20624999999999999 | 0.27500000000000002 | 0.34375 | 0.41249999999999998 | 0.48125000000000001 | 0.55000000000000004 | 0.61875000000000002 | 0.6875 | 0.75624999999999998 | 0.82499999999999996 | 0.89375000000000004 | 0.96250000000000002 | 1.0313000000000001 | 1.1000000000000001 | 1.1688000000000001 | 1.2375 | 1.3063 | 1.375 | 1.4438 | 1.5125 | 1.5812999999999999 | 1.65 | 1.7188000000000001 | 1.7875000000000001 | 1.8563000000000001 | 1.925 | 1.9938 | 2.0625 | 2.1313 | 2.2000000000000002 | 2.2686999999999999 | 2.3374999999999999 | 2.4062999999999999 | 2.4750000000000001 | 2.5436999999999999 | 2.6124999999999998 | 2.6812 | 2.75 | 2.8188 | 2.8875000000000002 | 2.9563000000000001 | 3.0249999999999999 | 3.0937999999999999 | 3.1625000000000001 | 3.2313000000000001 | 3.3
path x | 87.04 | 87.027 | 86.989 | 86.925 | 86.837 | 86.724 | 86.588 | 86.429 | 86.25 | 86.05 | 85.832 | 85.596 | 85.345 | 85.079 | 84.801 | 84.512 | 84.214 | 83.909 | 83.597 | 83.282 | 82.964 | 82.645 | 82.327 | 82.01 | 81.696 | 81.389 | 81.088 | 80.794 | 80.508 | 80.231 | 79.964 | 79.709 | 79.466 | 79.235 | 79.016 | 78.81 | 78.618 | 78.44 | 78.277 | 78.128 | 77.995 | 77.876 | 77.773 | 77.685 | 77.613 | 77.557 | 77.516 | 77.492 | 77.484
path y | 87.04 | 86.944 | 86.66 | 86.195 | 85.559 | 84.768 | 83.843 | 82.796 | 81.65 | 80.426 | 79.142 | 77.813 | 76.453 | 75.075 | 73.687 | 72.301 | 70.924 | 69.558 | 68.202 | 66.86 | 65.53 | 64.214 | 62.91 | 61.617 | 60.335 | 59.061 | 57.793 | 56.531 | 55.273 | 54.017 | 52.764 | 51.512 | 50.261 | 49.01 | 47.758 | 46.505 | 45.251 | 43.994 | 42.736 | 41.474 | 40.211 | 38.944 | 37.674 | 36.402 | 35.126 | 33.848 | 32.568 | 31.285 | 30
Chart: Time, sec
Transient Temp. at beam center
Steady state thermal
1/8th symmetry model
Average irradiation temperature 30C~87C

## Slide 12
Swelling factor combined function of fluence and temperature
sw(u,T)=}
Chart: Distance from beam centre (x), mm
Swelling is reduced at center due to relatively high irradiation temperature

## Slide 13
XRD data NTO2
Assumption
Experimental swelling = ∂(d/d0)
3.37
3.621
d-spacing, A0
XRD scan spot size is 50µm x 50µm x 10mm
In FEA, element size is made ~ 50µm so that it would match to XRD scan volume
3.542
3.618

## Slide 14
Determining Swelling Coefficient
Equating sw(u,T) to ∂(d/d0)  C
U (mm) | Temperature | sw | d-spacing | ∂(d/d0) | C
0 | 88 | 0.779 | 3.621 | 0.074481 | 0.000894
1.1 | 84 | 0.686 | 3.618 | 0.073591 | 0.001073
2.2 | 81 | 0.442 | 3.542 | 0.051039 | 0.001211
3.3 | 78 | 0.210 | 3.45 | 0.023739 | 0.001245
Chart: 
| 0 | 1.1000000000000001 | 2.2000000000000002 | 3.3
C | 0.095604 | 0.1073 | 0.11541 | 0.11292
XRD
u
Multi-variate regression analysis:
Varying “b” and “σ”to get C curve as flat as possible
 b= 0.155, C = 0.00107, σ =1.11
sw(u,T)=}
sw(u,T)
=}

## Slide 15
Young’s Modulus variation with Fluence Ø
“E” varies with Ø
Ø varies with location.
This two relationship is used to map “E” as a function of location
Chart: Distance from beam centre(x-axis), mm
Chart: Fluence, x1020
Chart: Fluence, x1020
Analytical function fit f1
Ø = Ø0 exp{-0.5(u/1.1)2}
E=E0[1+f1(Ø) ]
Peak fluence 8 x1020 p/cm2

## Slide 16
Model- Geometry
1/8th Model Symmetric in x, y, and z direction
Beam along Z-direction
3.3mm
7.5mm
10 mm
Gaussian Beam in x-y
Cooling water temperature 30C
Fixed support
Symmetric Boundary Condition on x, y and z plane
ui,i =0
θi ,j = 0 i≠ j
= free i=j

## Slide 17
FE Model
Mesh Optimization
Finer elements at the beam center
Progressively larger elements
30 elements within 1-σ of beam
Minimum distorted elements
Curvature and proximity refinement.
15000 elements 68,0000 nodes
Larger temperature gradient within beam center
Jacobian Ratio (Gauss points)
Check element quality
High Jacobian ratio  spurious stress values
Keep J-R as close to 1
JR > 10 can lead to increase in stress by 20%

## Slide 18
FEM Implementation of Empirical Formula
Total Strain
Swelling Strain
Linear swelling model
APDL Scripts
APDL Scripts
No shear, only volume change

## Slide 19
Simulation Frame-work
Static structural analysis
swelling factor as function of fluence,temperature sw(Ø,T)
Young’s modulus=f(fluence)
CTEf(Temperature)
Solve stress, strain , deformation states
New
After years of operation
One beam pulse
Transient Thermal-Dynamic analysis
Initialize domain with σ,ε, u from static structural
Turn off g(T) portion of sw(Ø,T)
Young’s modulus=f(fluence)
CTEf(Temperature)
Beam Parameters
Number of protons pulse: 4x1013
Pulse duration : 10µsec
Beam σ : 1.1 mm
Energy deposited/ pulse : 480 J/cm3
Deformed
Dynamic stresses
Steady State Thermal Analysis
Few micro-secs of high temperature is not enough to influence any swelling (annealing)

## Slide 20
Static Structural analysis – σyy Distribution
State just before beam pulse after number of years of exposure to neutrons
Path-x
Beam direction
2.45 mm
Compressive
Tensile
Path-x
Path-x
Beam direction
Path-x
Without Swelling
With Swelling

## Slide 21: Simulation validation- failure strength
Swelling formulation raised the stress level up to 150 MPa
N. Simos, PRAB 20, 071002 (2017)

## Slide 22: Simulation Validation- amount of swelling
Deformed location
From Simulation
(3.323-3.3)*100/3.3= 0.7 %
3.3 mm
Observed bulk swelling at that location ~ 2%
Difference of factor of 2 is not too bad…?
Measurement technique
Assumptions in empirical formulation

## Slide 23: Simulation Validation- Stress states
Transition of d -spacing
state of stress from compression to tension
XRD Scan NTO2
Predicted by swelling simulation
Undeformed crystallite d-spacing 3.37

## Slide 24: Simulation Validation- Mohr-Coulumb’s factor of safety
Fracture plane
Beam
FS distribution
FS <1
79 MPa
175 MPa
Probable crack initiation sites
Fractography suggest crack starting from inside and propagating outward

## Slide 25
Dynamic stresses- σyy
Chart: Time,µs
Chart: Time,µs
X=2.4mm
R=-1 Sever form of fatigue
Two fatigue loading 1) 11MPa with 1.87sec 2) 5MPa with 4µsec
Fracture plane
Beam

## Slide 26
Fatigue Crack growth stages
Slip lines
Tension
Blunting
compression
Sharp
Crack initiation significant portion of fatigue life
Int. J. Fatigue Vol. 20, No. 10, pp. 737–742, 1998
compressive stress in (R<-1)
Regain sharp crack
Sharp crack tip
Cyclic Max shear stress
 intrusion protrusion of slip lines
Tensile stressmicrocrack growth
Pores and microcracks local stress concentration
Crack initiation in crystallites nano-scale, slow
Crack growth/propagation between the particles micro-scale, fast

## Slide 27: Conclusions
Thermal stresses alone could not have caused crack
Implementing swelling strain effectively raised the stress state close to failure strength.
Simulation could explain probable crack initiation region
  Regions with Factor of safety <1
Dynamic stresses due to beam heating  potential fatigue crack
  High amplitude low frequency 11 Mpa 15 million cycles per year
  Low amplitude high frequency  5 Mpa Gigacycles per year
  Regions of complete load reversal at about 2.45mm from beam center
Graphite has low endurance limit ~14 Mpa (@1million cycle
  Low amplitude gigacycle load can cause fatigue failure

## Slide 28
Summary
Developed an empirical formula for local swelling (Temp, fluence)
Simulation results bulk swelling reasonable agreement with measurement
Combined swelling stress and dynamic stress due to beam loading caused failure
Did not take into account
Stress, creep effect on swelling.
Dislocation distribution and type, grain boundary segregation etc.
In Future Make the model predictive
Obtain parameters from mechanism of swelling rather than XRD

## Slide 29
Thank You!