## Slide 1: Material irradiation and investigation capabilities at ISAC-TRIUMF
Ferran Boix Pamies
December 12th, 2019

## Slide 2: ISAC
RIB Production (since 1995)
2 target stations
Highest power ISOL driver with 50 kW 500 MeV protons
IAMI
TR24

## Slide 3: ISAC targets
Ta
SiC
500 MeV protons 7 mm FWHM
Target materials:
UCx
UO2
ThO
Nb
Ta
TaC
NiO
ZrC
TiC
SiC

## Slide 4: ISAC operation
4400µAh
19800µAh
3300µAh
36500µAh
13000µAh
35000µAh
3800µAh
16700µAh
23100µAh
36500µAh
UCx
UCx
UCx
Ta
Ta
Ta
Ta
Ta
SiC
SiC
144500µAh
47600µAh
4400µAh
5300µAh
23500µAh
4000µAh
2500µAh
3800µAh
21500µAh
3800µAh
2200µAh
UCx
UCx
UCx
Ta
Ta
nSiC
UCx
UCx
Nb
54100µAh
16900µAh
2017
2018
Irradiation subordinated to the scheduled ISOL experiment
  Opportunistic planning necessary
Online
Maintenance
Conditioning
Target in
TM1
TM2
Ref irrad. 50000 µAh 1.125E+21 protons 4.5E+20 protons on sample

## Slide 5: Can we do something with them?
DPA- downstream from a SiC target
DPA-rates downstream from a SiC target
in Fe, X-Y in cm
[DPA/primary proton]
[DPA@50000µAh]
Chart: Distance to center [mm]
| 10.5 | 9.5 | 8.5 | 7.5 | 6.5 | 5.5 | 4.4999999999999902 | 3.4999999999999898 | 2.4999999999999902 | 1.49999999999999 | 0.5
Be | 0.00043589 | 0.0006427 | 0.00087723 | 0.0018198 | 0.0041423 | 0.0077838 | 0.010597 | 0.016063 | 0.023387 | 0.028766 | 0.0324
C | 0.0010292 | 0.0015175 | 0.0020712 | 0.0042969 | 0.0097804 | 0.018378 | 0.025022 | 0.037927 | 0.055219 | 0.067919 | 0.0765
Al | 0.0048977 | 0.0072215 | 0.0098567 | 0.020448 | 0.046543 | 0.087459 | 0.11907 | 0.18049 | 0.26278 | 0.32321 | 0.36405
Ti | 0.0075675 | 0.011158 | 0.01523 | 0.031595 | 0.071915 | 0.13513 | 0.18398 | 0.27888 | 0.40603 | 0.4994 | 0.5625
Cr | 0.0086421 | 0.012742 | 0.017392 | 0.036081 | 0.082127 | 0.15432 | 0.21011 | 0.31848 | 0.46368 | 0.57032 | 0.64238
Fe | 0.011107 | 0.016377 | 0.022353 | 0.046371 | 0.10555 | 0.19834 | 0.27003 | 0.40931 | 0.59592 | 0.73297 | 0.82558
V | 0.009081 | 0.01339 | 0.018276 | 0.037914 | 0.086298 | 0.16216 | 0.22078 | 0.33465 | 0.48723 | 0.59928 | 0.675
Co | 0.011381 | 0.016782 | 0.022905 | 0.047518 | 0.10816 | 0.20324 | 0.27671 | 0.41943 | 0.61066 | 0.7511 | 0.846
Ni | 0.015438 | 0.022762 | 0.031069 | 0.064453 | 0.14671 | 0.27568 | 0.37533 | 0.56891 | 0.82829 | 1.0188 | 1.1475
W | 0.013712 | 0.020218 | 0.027596 | 0.057249 | 0.13031 | 0.24486 | 0.33338 | 0.50533 | 0.73572 | 0.90492 | 1.0192
Ta | 0.022551 | 0.033251 | 0.045384 | 0.094152 | 0.21431 | 0.4027 | 0.54827 | 0.83106 | 1.21 | 1.4882 | 1.6763
Notes: Material science:
Radiation damage in materials
Full penetration
Thermal spike – closer damage to high energy environments / reference grain growth
Full penetration (simulate thickness)

## Slide 6: Can we do something with them?
Chart: Distance to beam center [mm]
| 0 | 1.25 | 2.5 | 3.75 | 5 | 6.25 | 7.5 | 8.75 | 10
Be | 122.6306 | 116.0927 | 97.1513 | 73.5836 | 57.028 | 40.9935 | 24.9576 | 13.5645 | 6.2
C | 127.5809 | 120.7791 | 101.0731 | 76.554 | 59.3301 | 42.6483 | 25.9651 | 14.1121 | 6.4503
Al | 207.2229 | 196.1751 | 164.1676 | 124.3426 | 96.3667 | 69.2714 | 42.1737 | 22.9215 | 10.4768
Ti | 192.499 | 182.2362 | 152.503 | 115.5076 | 89.5196 | 64.3494 | 39.1771 | 21.2929 | 9.7324
Cr | 186.7225 | 176.7677 | 147.9267 | 112.0415 | 86.8333 | 62.4185 | 38.0015 | 20.6539 | 9.4404
Fe | 180.5743 | 170.9472 | 143.0558 | 108.3523 | 83.9741 | 60.3632 | 36.7502 | 19.9738 | 9.1295
V | 190.3327 | 180.1855 | 150.7868 | 114.2078 | 88.5122 | 63.6253 | 38.7362 | 21.0532 | 9.6229
Co | 170.5495 | 161.4569 | 135.1139 | 102.337 | 79.3122 | 57.0121 | 34.71 | 18.865 | 8.6227
Ni | 183.4033 | 173.6254 | 145.2971 | 110.0498 | 85.2897 | 61.3089 | 37.326 | 20.2868 | 9.2726
W | 242.4549 | 229.5288 | 192.0794 | 145.4833 | 112.751 | 81.0489 | 49.344 | 26.8186 | 12.2581
Ta | 229.9266 | 217.6684 | 182.1541 | 137.9658 | 106.9248 | 76.8609 | 46.7943 | 25.4328 | 11.6247
He-rates downstream from a SiC target in Fe
Transmutation also generates interesting radionuclide for medical applications
Ti44 - 40MBq

## Slide 7: How: Target considerations
Remote handling compatible
Vacuum compatible:
  No outgassing
  No virtual leaks
Thermo-mechanical stability under proton irradiation
Water-cooled heat shields
target container ~2000 °C
(Ø 20 mm, 60 cm3)
Target ion source service connections

## Slide 8: How: Materials Irradiation Studies Target
Sample disc containers
Graphite handle
Graphite thread
Al bolts
Belleville washers
Al nut
Low energy deposition in graphite structure
Open volumes for venting
Tele-manipulator compatible handle and thread
Disc stack allows for re-organization of samples for different irradiations

## Slide 9: 2 Disc Prototype

## Slide 10: Temperatures under irradiation
Energy deposition simulation in FLUKA
Imported results in ANSYS as heat generation
[GeV/cm3/pr]

## Slide 11: Temperatures in irradiation target
Stainless steel/Aluminum/Graphite as sample materials
100µA
1178W
70µA
824.6W
Beam current: 15µA
Power deposited: 176.7W

## Slide 12: Ongoing studies
Beam intensity independent temperatures
Thermocouples
Heating elements

## Slide 13: Sample doses
Chart: Decay time [days]
Ta sample (simulated dose) | 154045.0096 | 4831.6393 | 2684.1695 | 1979.054 | 1633.0118 | 1416.0271 | 1257.8104
Chart: 
| 0 | 0.5 | 1 | 1.5 | 2 | 2.5 | 3
Cr | 288.6202 | 66.7356 | 35.8432 | 20.4175 | 12.2465 | 7.797 | 5.3028
Ta | 1540.4501 | 48.3164 | 26.8417 | 19.7905 | 16.3301 | 14.1603 | 12.5781
Ti | 157.6401 | 13.0742 | 9.6894 | 7.9167 | 6.6655 | 5.7185 | 4.9645
Ni | 607.9319 | 111.7611 | 70.3807 | 54.0951 | 44.5129 | 37.6854 | 32.3885
SiC | 62.5926 | 0.56986 | 0.53646 | 0.50823 | 0.48429 | 0.46385 | 0.44633
Mo | 1112.4733 | 59.4112 | 40.1636 | 32.6233 | 27.5771 | 23.9284 | 21.1972
Be | 0.14973 | 0.12319 | 0.10135 | 0.083384 | 0.068606 | 0.056445 | 0.046441
W | 1355.5943 | 38.5506 | 22.5406 | 16.8506 | 13.8603 | 11.9283 | 10.5191
C | 95.3355 | 0.33358 | 0.27446 | 0.22581 | 0.18578 | 0.15285 | 0.12576
Al | 43.2505 | 0.55341 | 0.53618 | 0.52116 | 0.50791 | 0.49615 | 0.48562
Dose @40000µAh & 10cm [µSv/h/mm3]
[µSv/h/mm3]
Chart: 
| 0 | 0.5 | 1 | 1.5 | 2 | 2.5 | 3
C | 80.3971 | 0.48127 | 0.39596 | 0.32577 | 0.26803 | 0.22052 | 0.18143
Cr | 248.7511 | 63.701 | 35.4597 | 21.1824 | 13.4896 | 9.1909 | 6.69
Ta | 1242.9307 | 59.3235 | 39.9145 | 32.5528 | 28.3877 | 25.4836 | 23.2237
Ti | 136.2045 | 18.2241 | 14.5602 | 12.3304 | 10.623 | 9.2463 | 8.099
Ni | 542.6696 | 143.6192 | 103.3531 | 83.8673 | 70.8386 | 60.8994 | 52.8651
Fe | 301.6461 | 56.8208 | 28.4813 | 18.3055 | 13.4128 | 10.6686 | 8.9796
Mo | 910.7464 | 82.0638 | 63.4586 | 54.647 | 48.3082 | 43.4249 | 39.5158
Mg | 27.8515 | 2.6096 | 2.5713 | 2.535 | 2.5007 | 2.4679 | 2.4365
Al | 27.0385 | 1.0069 | 0.98344 | 0.96239 | 0.94342 | 0.92615 | 0.91032
Decay time [Month]
Dose @40000µAh & 1m
Dose @100000µAh & 1m
Simulated doses benchmarked with target data
Module operation “time loss” is less significant than expected
Resume dose range accepted

## Slide 14: Sample preparation
Inside hotcell (“big sample”)
Disc stack (several cm3)
  Sample Separator
Glovebox (“medium sample”)
Raw individual sample (some mm3)
  Mechanical grinding
  Electropolishing
  Ion milling
Outside glovebox (“small sample”)
Reduced sample (some µm3)
By N.Fedrigo

## Slide 15: Electropolishing

## Slide 16: PIE
  Glovebox-Hot-cell (“medium sample”)
  SPT
  Optic microscope
Outside glovebox (“small sample”)
SEM,TEM
Inside hotcell (“big sample”)
Big samples for “close to conventional” mechanical testing?

## Slide 17: Summary
Radiation damage:
(0.1 – 1) DPA
(100-300) appm of He
New materials will be developed
These materials final experimental test will have to be performed under real High power beam conditions
Inside hotcell (“big sample”)
Disc stack (several cm3)
  Sample Separator
Load frame
Glovebox (“medium sample”)
Individual sample (some mm3)
  Mechanical grinding
  Electropolishing
  Ion milling
PIE: SPT
Outside glovebox (“small sample”)
Reduced sample (some µm3)
PIE: SEM/TEM
Irradiation temperatures:
(150-600)ºC beam intensity dependent
Ongoing studies to increase temperature boundaries

## Slide 18
Thank you
Acknowledgments
Alexander Gottberg, Ricardo Manuel dos Santos Augusto, Fernando Maldonado, Marla Cervantes, Mia Au, Luca Egoriti, Anders Mjos, Chad Fisher, Aaron Schmidt, Darwin Ortiz Rosales, Valery Radchenko, Thomas Day Goodacre, Carla Babcock, Roger Caballero, Matthew Gareau