## Slide 1
High Field Magnets
for accelerators
Frédérick Bordry
Tevatron
HERA
RHIC
LHC

## Slide 2
Beam energy
Dipole field
Bending radius
Beam size at the quadrupole
Emittance
Integrated quadrupole gradient
Lorentz factor
Focal length
Beam size at the collision point
Peak coil field
High field accelerator magnets : B 
Design for the largest feasible and economic integrated field to achieve the smallest beam size at the IP
  Design for the largest feasible and economic B to reduce the accelerator radius.
  To push and invest in Technology instead of civil engineering !
Dipoles
relativistic synchrotron
Final focus quadrupoles

## Slide 3: Superconducting accelerators : dipoles
High Field magnets ≥ 9T
Design and tested at 9T
In operation

## Slide 4
HFM LHC: it works !
1232 dipoles and 400 quadrupoles
produced and in operation

## Slide 5
j
w
Dipole field generated by a current distribution with constant current density J over a sector of inner radius Rin, outer radius Rout, coil width w = Rout-Rin and opening angle j
J 
n ≈ 1…2
In the range of typical magnet designs considered n≈1.5
B | (T) | 16 |  |  | 16
J | (A/mm2) | 300 |  |  | 600
w | (mm) | 76 |  |  | 38
Acoil | (mm2) | 20,000 |  |  | 7000
Factor 2
Factor 3
Rin
Superconducting magnets : current density 
w 
B = Cte
and space

## Slide 6
Courtesy of P. Lee, D. Larbalestier and D. Abraimov
Superconductor landscape
600 A/mm2
REBCO (EuCARD2, B-HTS)
Bi-2212 (B-OST)
Nb-Ti
LHC
(8.33 T)
Nb3Sn
FCC
(16 T)
REBCO
The grand challenge of today is to develop the technology of high-field conductors getting the maximum by minimising the cost:
Jc increase

## Slide 7: LTS performance: Jc increase
US-CDP
EU-FP6/FP7
ITER wires
HL-LHC
wires
SSC R&D
Data by courtesy of J. Parrell (OST)
1300 tons of Nb-Ti
CDP: Conductor Development Program

## Slide 8
Lorentz forces in the plane of a thin coil of radius Rin generating a dipole field B (thin shell approximation), referred to a coil quarter
Fy
Fx
Progression of Fx:
LHC MB(8.33T) ≈ 1700 kN/m
LHC MBH(11T) ≈ 3200 kN/m
FRESCA2(13T) ≈ 7600 kN/m
FCC MB(16T) ≈ 8000 kN/m
HE-LHC MB(20T) ≈ 10000 kN/m
Mechanics at high fields: Lorentz force 

## Slide 9
The challenge of mechanics:
  - Appropriate support concepts for the coil (bladder-and-key, stress management, canted-cosinus-theta, …)
  - Manage the Increasing stress on the conductor (limit of materials !)
  - Limit mechanical energy release (=> training)
LHC
11T
QXF
FCC
HE-LHC
Unconstrained scaling
Stress limited
reducing J
Stress in high field magnets: peak stress 

## Slide 10
Tevatron
HERA
RHIC
LHC
Stress in high field magnets: past and present accelerators
all cos, all Rutherford cables

## Slide 11
Tevatron
HERA
RHIC
LHC
Rutherford cable Collars Aust. Steel
Warm iron
Collars Al alloy
Cold iron
Cold yoke as collar
Collars Aust. Steel + yoke
Twin apertures
Stress in high field magnets: but different structures

## Slide 12
2002, LBNL: Bladder and keys
R.R. Hafalia, et al., IEEE TAS, 12(1) (2002), pp. 47-50.
2014, LBNL: CCT
S. Caspi, et al., IEEE TAS (2014), p. 4001804.
2017, FNAL: SM cos(q)
V. Kashikin, et al., Proc. IPAC, Copenhagen (2017), pp. 3597-3599.
Stress in high field magnets: new structures
LBNL
FNAL
135 MPa
on the conductor
Canted-Cosinus-Theta (CCT) option

## Slide 13
    ramp with a short to ground appearing 1.5s after the1st magnet quench
Earth Fault Burner !
capacitive current discharge
LHC Training Dipoles
172 training quenches
600 secondary quenches
Only 1 quadrupole quench
Each Sector Trained to 6.55TeV (11080A)
(100 A above the operational field)
≈ 7.82 T
2015
End of 2016
2017

## Slide 14
Energy per unit length in a sector coil of inner radius Rin, outer radius Rout, coil width w = Rout-Rin producing a dipole field B
JC ≈ 1000…1250 (A/mm2)
dT/dt ≈ 1000…2000 (K/s)
t(300 K)≈ 0.15…0.3 (s)
Iop ≈ 15 (kA)
E/l ≈ 1000 (kJ/m)
V/l ≈ 500…1000 (V/m)
It is not possible to protect accelerator magnet strings using an external dump
Voltage per unit length for an external dump with time constant t
HFM must support its own quench !
Stored Energy and Protection at high fields: E

## Slide 15
In the range of typical magnet designs considered n≈1.5
Ultimate
hot-spot limit
Typical energy densities e:
LHC MB(8.33T) ≈ 50 MJ/m3 (one 15m magnet 7 MJ)
LHC MBH(11T) ≈ 85 MJ/m3
FRESCA2(13T) ≈ 100 MJ/m3
The challenge of protection:
  - Fast detection and internal dump (spread the energy)
  - Material and coil limits (hot-spot, thermal stress, voltage)
  - Energy extraction for magnet string (interconnections, energy extraction,
  massive quenches,...)
Stored Energy and Protection at high fields: E

## Slide 16
Io = 13 kA
Discharge time constant = 120 s
Protection of LHC sector (154 magnets in series)
Circuit time constant = 23’000 s
Notes: Possible suppression ?

## Slide 17
NbTi mature but limited to 9T
Is Nb3Sn mature ? Yes, and no
  Performance of Nb3Sn wires has seen a great boost in the past decade (factor 3 in JC w/r to ITER)
  However, Nb3Sn accelerator magnets were never built nor operated in accelerators.
  Manufacturing, strain tolerance, protection, quench, training, field quality are the focus today to make this new technology a reality
LTS (NbTi ; Nb3Sn)
  Solid and aggressive R&D in Nb3Sn High Field Magnet for accelerators must be intensified to increase further critical current Jc (up to 16 T)

## Slide 18: The HL-LHC Project: 300 fb-1 → 3000 fb-1
New IR-quads Nb3Sn
(inner triplets)
  New 11 T Nb3Sn
  (5.5 m dipoles)
  Crab Cavities
  Collimation upgrade
  Cryogenics upgrade
  Cold powering
  Machine protection
  …
Major intervention on more than 1.2 km of the LHC

## Slide 19
12.37 T
MBHSP101
MBHDP101
Aperture | 60 | (mm)
Field | 10.8 | (T)
Current | 11850 | (kA)
Peak field | 11.35 | (T)
40 strands cable
(14.7 mm x 1.27 mm)
RRP strand (0.7 mm,108/127)
JC: 2450 A/mm2 (12 T, 4.2 K)
Cu:non-Cu: 1.15
Courtesy of F. Savary, J. C. Perez, G. Willering, CERN
HL-LHC 11T dipole (MBH) R&D

## Slide 20
Aperture | 150 | (mm)
Gradient | 132.6 | (T/m)
Current | 16.47 | (kA)
Peak field | 11.4 | (T)
40 strands cable
(18.15 mm x 1.52 mm)
RRP strand (0.85 mm,108/127)
JC: 2450 A/mm2 (12 T, 4.2 K)
Cu:non-Cu: 1.2
Courtesy of G. Ambrosio, G. Chlachidze, US-LAUP and CERN
The challenge for high field magnets:
  - Limit the training and keep memory !
  - Increase Jop/JC (presently at ≈ 40 % for Nb3Sn at 1.9 K)
HL-LHC quadrupole R&D

## Slide 21
Nb3Sn quadrupole: 1st long prototype under construction
Courtesy of Frédéric Savary
Second short (1.5 m) under preparation for test at CERN
Insertion of coil package inside mechanical structure of the first IT quad prototypes (4.2 m long) in LBNL-USA

## Slide 22
LS2
LS3
LHC Run II
≈ 100 fb-1
LHC Run III
≈ 300 fb-1
Opportunity for first industry experience on Nb3Sn accelerator magnets
HL-LHC Nb3Sn magnets planc

## Slide 23
 | LHC | FCC
Circumference (km) | 26.7 | 97.5
Dipole field (T) | 8.33 | 16
C.o.M. energy (TeV) | 14 | 100
Future Circular Collider

## Slide 24
Nb3Sn conductor program
Nb3Sn is one of the major cost & performance factors for FCC-hh and is given highest attention
Main development goals until 2020:
Jc increase (16T, 4.2K) > 1500 A/mm2 i.e. 50% increase wrt HL-LHC wire
Reference wire diameter 1 mm
Potentials for large scale production and cost reduction
3150 mm2
~1.7 times less SC
~10% margin
HL-LHC
~10% margin
FCC ultimate
5400 mm2
Notes: New slide from Davide.
Showing that conductor development is launched at international level, Russia, Japan, (Korea and Europe in preparation)
Underline importance of that development as main cost driver for the hadron collider machine.

## Slide 25
Established worldwide activities for development:
Procurement of state-of-the-art conductor for prototyping: Bruker (OST)– European/US =>1500 A/mm2 @ 16T, 4.2K
Stimulation of conductor development with regional industry:
  CERN/KEK – Japanese contribution. Japanese industry (JASTEC/KobeSteel, Furukawa) and laboratories (Tohoku Univ. and Tokai University)
  CERN/Bochvar High-technology Research Inst. – Russian contribution. Russian industry (TVEL) and laboratories
  CERN/KAT – Korean industrial contribution
Characterization of conductor & research with universities:
  Europe: Technical Univ. Vienna, Geneva University, University of Twente
  Applied Superconductivity Centre at Florida State University
collaborations FCC Nb3Sn program
Notes: New slide from Davide.
Showing that conductor development is launched at international level, Russia, Japan, (Korea and Europe in preparation)
Underline importance of that development as main cost driver for the hadron collider machine.

## Slide 26
16 T dipole design activities and options
Cos-theta
Blocks
Common coils
Short model magnets (1.5 m length) will be built from 2017 - 2021
Swiss contribution
Canted
Cos-theta
H2020
INFN
CEA
CIEMAT
PSI
LBNL
FNAL

## Slide 27
L1-L2: 28 strands, 1 mm RRP 150/169
L3-L4: 40 strands, 0.7 mm RRP 108/127
Assembly and test expected in 2018
Simplify assembly, reduce cost
Courtesy of A. Zlobin, FNAL
Cos-theta, 4 layers, 15 T dipole

## Slide 28: The US Magnet Development Program is progressing with the development of high-field superconducting accelerator magnets on multiple fronts
Wang, MT25
Marchevsky, EUCAS17
Novitski MT25
Dev. of Canted Cos-theta (CCT) concept
Achieved 86% short sample with 2 layers;
- 9.14T bore-field, 90mm bore
Significant training
- focus of ongoing research
Arbelaez, MT25
Steady progress on 4-layer Cosine-theta at FNAL
First use of CORC® cable in CCT geometry
- Focusing on technology issues, enhancing JE

## Slide 29
16 T cryo-dipole integration approach
Description | ID in mm | OD in mm
Iron yoke | - | 600
Aluminium shrinking cylinder | 600 | 740
Stainless steel He tight shell | 740 | 760
Al radiation shield | 934 | 940
Vacuum vessel (magnetic steel) | 1120 | 1220
Example magnetic cryostat
coldmass 40t, total mass 62t
Design strategy: develop a single 16 T magnet, compatible with both HE LHC and FCC-hh requirements:
  Goal is reduction of external diameter to ~1200 mm (16 T cryostat design based on “classical” approaches gives ~1500 mm diameter!)
  Options und consideration:
    Allow stray-field and/or cryostat as (partial) return-yoke
    Active compensation with (simple) shielding coils
    Optimization of inter-beam distance (compactness of coils)
    (QRL integrated in magnets,  negative impact on integral field because of longitudinal space required for service module (5%))
   Smaller diam. also relevant for FCC-hh cost optimization
   Design optimization for specific project after decision

## Slide 30
 | LHC | FCC | SppC
Circumference (km) | 26.7 | 97.5 | 100
Dipole field (T) | 8.33 | 16 | 12…24
C.o.M. energy (TeV) | 14 | 100 | 70…125
Courtesy of Q. Xu, IHEP
Super proton-proton Collider (SppC)

## Slide 31
Baseline design
  Tunnel circumference: 100 km
  Dipole magnet field: 12 T, iron-based HTS technology (IBS: Iron-Based Superconductor)
  Center of Mass energy: >70 TeV
Upgrade phase
  Dipole magnet field: 20…24T, IBS technology
  Center of Mass energy: >125 TeV
Development of high-field superconducting magnet technology
  Starting to develop required HTS magnet technology before applicable iron-based wire is available
  ReBCO & Bi-2212 and LTS wires be used for model magnet studies and as an option for SppC: stress management, quench protection, field quality control and fabrication methods
Conceptual design of common coil 12T dipole
Top priority: reduce cost!
Instead of increasing field
Courtesy of Q. Xu, IHEP
China high-field magnet R&D

## Slide 32
Can HTS displace LTS (NbTi, Nb3Sn) ?
Not today (performance and cost)
  Much needs to be done to bring this technology to a point where it can be sold as “mature”
    Materials have potential that can be exploited
      OPHT for BSCCO-2212
      Thicker layer for YBCO tapes
      The Holy Grail of a round YBCO wire
      ….
  Production quantities, homogeneity and cost need to evolve
  Step-up application demands, from self-field (SC-link is an ideal test-bed) to high-field accelerator magnets (feasibility)
HTS

## Slide 33: Ideas for 20 T
A 20 T HE-LHC dipole
L. Rossi & E. Todesco, (CERN)
HTS
Nb3Sn
Nb-Ti
Cost optimized, graded winding
All options are based on an LTS winding (outsert), and an HTS field booster (insert)
A 24 T LHC Tripler
P. McIntyre (TAMU)
Stress managed winding

## Slide 34
REBCO option (Roebel)
BSCCO-2212, CERN provides precursor powders, US program produces wire and cable
EuCARD2 program, targeting a 5 T, 40 mm aperture demonstrator, in collaboration with EU laboratories and industry
US-BSCCo program, testing alternative materials and coil configurations (CCT)
Sample of US BSCCO-2212 cable
HTS for 20 T

## Slide 35
HTS
20 T
US high-field magnet R&D
Nb3Sn
16 T
Improvements in Bi2212 powder, overpressure processing, and magnet fabrication now yielding
Shen, EUCAS17
Jiang, EUCAS17
JE,cable=730 A/mm2
Competitive with Nb3Sn at ~14T

## Slide 36
- To increase the critical current Jc
- To sustain larger forces
- To protect those magnets (large numbers in series)
To train those magnets faster
To keep the memory after installation and thermal cycles
Global optimization: magnet and powering
current leads, superconducting links, energy extraction, power converters
High Field Magnet challenges

## Slide 37: Superconducting magnet market
Sources: [1] from market report at Conectus.org, converted from repored 5.3 BEUR in 2013
[2] Report to the CERN Finance Committee, 2008, reported 1.7 BCHF(2008) escalated to 2013
[3] DOE Assessment of the ITER Project Cost Estimate, reported 1.09 BUSD(2002) escalated to 2013
JT60SA
ITER
LHC
NMR
MRI
At present, the vast majority of the use of superconductors is for magnet applications:
  MRI (NbTi): 5.5 BUSD/year[1];
  7.0 BUSD/year in 2017
  NMR, science and research: (Nb3Sn)
   1 BUSD/year[1]
Large scale projects (HEP, Fusion) represent only a fraction of the total market and discontinuities:
  Evaluated cost of LHC magnet system (material): 2 BUSD[2]
  Quoted cost of ITER magnet system (material): 1.4 BUSD[3]

## Slide 38
Superconducting conductor production
NbTi in the world :  600 tons/year, driven by MRI production
Nb3Sn :  10 tons/year, driven by NMR magnets and laboratory solenoids
All of HTS (BSCCO, YBCO,…) and MgB2: around 100...200 km of 4-10 mm wide tape per year, presently driven by R&D applications and delivered by around 10 worldwide producers,
In total below 1 ton/year
LHC required 1300 tons of Nb-Ti (300 t/year peak production) (30% cost of the magnet)
ITER required 300 tons of Nb-Ti and 600 tons of Nb3Sn (250 t/year peak production)
HL-LHC requires: 30 tons Nb3Sn and about the same for NbTi
HE-LHC will require :  3’000 tons Nb3Sn
FCC-hh will require :  9’000 tons Nb3Sn (between 50% to 60% cost of the magnet)

## Slide 39: Conductor cost
16 Tesla
€/kA.m
15 m
≈ 30-100
Nb3Sn: HE-LHC, FCC:
Goal 3.5 €/kA.m
at 16 T and 1.9 K
500...600 EUR/kg, i.e. a factor 2.5...3 better than what the present cost 1300...1500 EUR/kg for HL-LHC (RRP)

## Slide 40
Large-scale science, and HEP, have driven major advances in conductors, by consistently pushing performances beyond the state of the art of industrial production, striving to achieve high and stable JC, small filament diameter, high homogeneity, and demanding quality standards
But due to long period (longer !) between project it’s problematic to maintain high performance productions and competition.
Now only ONE conductor qualified (Jc) for HL-LHC (Bruker acquired Oxford Instruments -Nov. 2016- and stopped PIT [Powder In Tube] cable production, now only RRP [Restack Rod Process]): high risk !
How to develop R&D and to prepare production for future high energy accelerator and fusion tokamak (DEMOs,…in spite of lower Jc performance) :
Proposal of a Global R&D superconductor center: To develop and maintain the know how and to transfer it to industry when a project is approved (industries are assemblers and not responsible for the performance but for the Q&A production)
HE-LHC, FCC, SppC
DEMOs
ITER
LHC
Tevatron
HERA and RHIC
HL-LHC

## Slide 41
The LHC High-Luminosity Upgrade is the foundation for new HFM magnet technology for accelerators, and provides an interesting opportunity for industry
Nb3Sn accelerator magnet development and production
  Production in 2018-2023
  First use ever of Nb3Sn in a running accelerator ! (8T to 12T)
The next step is the development of magnets for high energy accelerator : 12T to 16T
(SppC, FCC, HE-LHC,...)
  Model activities are planned in European, US and China laboratories in 2018-2022
  Prototyping in industry (full length, ≈ 5-10 magnets), in 2023-2026
  Performance (Jc), stress, stored energy management, field quality, and cost
  This is the logical sequence of the HL-LHC production, profiting from Nb3Sn technology established in laboratories and industry (Global Approach)
HTS is only in its infancy, but is the disruptive HFM technology of the further future
  HTS for special applications (energy distribution and current leads for SC magnets) and as option for the 20T (24T ?) programme (insert)
  Niche magnets for next accelerators (as final focussing magnets,…)
  Requires high-tech R&D, spanning from material science to electromechanical engineering, 5-10 years program defined
  More producers than Nb3Sn: medical, energy (production and transport),… markets
  HTS is the high-risk/high-return investment of the future
A tentative summary: HFM roadmap for accelerators
Notes: Please convey my apologies and best wishes for a successful workshop

## Slide 42
Acknowledgements and sincere thanks to all the people from whom I have begged, borrowed or stolen slides, especially Luca Bottura, Lucio Rossi, Qingjin Xu, Steve Gourlay and US colleagues, … and many unidentified persons from laboratories and industries.
Cos-theta
"La fonction la plus élémentaire de l'être humain, c'est de créer de l'avenir"
"The task of the mind is to produce future"
Paul Valéry
Thanks for your attention

## Slide 43: Objectives of the HFM network
Have an open forum that meets regularly to be able to discuss common scientific and technical issues in a targeted way
Make and maintain a comprehensive map of the HFM landscape, independently of participation to specific projects (EU or non-EU)
Disseminate the plans, progress and issues of the HFM projects to all the partners
Offer intellectual support to the projects
Provide access to the above forum to students and staff of all educational institutions independent of participation to a specific project (EU or non-EU)
Find and co-opt new partners, with relevant interest and contribution in HFMs, whether active in accelerator or other fields

## Slide 44: HFM Network Founding meeting on 22 September
17 institutes and universities voted to to join the provisional network
  CEA, CERN, Bochvar, PSI, Ubologna, INFN-Mi, INFN-Ge, EMFL, ASC-FSU, INP-Grenoble, ASIPP, KIT-ITEP, Utwente, EPFL-SPC, LBNL, FNAL, UNIGE
A provisional Steering Committee was elected with 5 members from:
  CEA, CERN, LBNL, PSI, Utwente for a period of 6 months
  A provisional Spokesperson was elected (Gijs de Rijk) for a period of 6 months
A set of provisional bylaws was commented, edited and approved
  The provisional SC will update and adjust the provisional bylaws
  The provisional General Assembly (17 members) will approve and propose further bylaw modifications during the 6 months
The next GA will take place in March
When the provisional bylaws are finalised they can be send to the legal departments of the members for verification, proposed modification and approval. We will probably need an iteration on the bylaws to get them in line with the legal requirements of the members
After that the network members can confirm their membership with a confirmation letter and the network becomes permanent
For the time being CERN will serve as repository for the confirmation letters
This process will probably take up to next summer

## Slide 45: MgB2
20+20 m

## Slide 46
Courtesy of RTE (Réseau de Transport d'Électricité )
Electricity transmission system operator in France
Major stakes for the energy needs of the future

## Slide 47
Nb3Sn production for ITER
Jc lower than
for FCC,
but large
scale
production
Large
scale
production

## Slide 48
e.g. HFM markets
NMR: 28.2T (?)
4 mm YBCO tape
DEMO